## Slide 1: CHART HTS program at PSI
Jaap Kosse, Henrique Rodrigues, Michal Duda, Bernhard Auchmann, Stephane Sanfilippo
Paul Scherrer Institute
13/12/21
Work supported by the Swiss State Secretariat for Education, Research and Innovation SERI
CHART2/MagDev Results and Roadmap - Technical Review

## Slide 2: Contents
NI test coil program
NI superbend for SLS
NI racetrack demos
NI solenoid for
P3 experiment at PSI
NI solenoid for
FCC-ee positron source
Accelerator dipoles
time
Racetrack demos
explore insulation
/cable concepts
Non-insulated solenoids
x-insulated racetracks
1)
2)
2)
2024
3)
3)
4)
4)
Non-insulated racetracks

## Slide 3: Contents
NI test coil program
NI superbend for SLS
NI racetrack demos
NI solenoid for
P3 experiment at PSI
NI solenoid for
FCC-ee positron source
Accelerator dipoles
time
Racetrack demos
explore insulation
/cable concepts
Non-insulated solenoids
x-insulated racetracks
1)
2)
2)
2024
3)
3)
4)
4)
Non-insulated racetracks

## Slide 4: Test coil program
Greg Brittles
NI coil technology license agreement with Tokamak Energy
Rapidly develop infrastructure for HTS coil
manufacturing and testing
1 coil
2 coils
4 coils
3 coils
2 coils
LN2
15 K
Stacked pancakes approach
Modular!
Aim: 4-coil stack, 14 T
done
soon

## Slide 5: Test coil design
Stacked, single layer pancakes
Axial joints to get current in and out
Patent G. Brittles WO2020/079412 A1
2-coil stack

## Slide 6: Test coil program
Commissioning of infrastructure at PSI
Winding
Soldering
Testing
Modeling
Cryogen-free test station (2 kA)
Tensioning system developed by
Francois-Olivier Pincot,
Jacky Mazet, CERN

## Slide 7: Winding
Feed spools
Flux bath
Winding table
Flux foamer
1980’s method to flux PCBs

## Slide 8: Soldering
Oxygen-free environment promotes solder wetting
PPM O2
Copper trace
Solder
J.C. Ivankovits

## Slide 9: Soldering
Soldering in argon overpressure
<1 ppm O2

## Slide 10
Manufacturing ready to go:
1 coil takes 2 days

## Slide 11: LN2 test results
So far:
Coil 1 0.8 T
Coil 2 0.8 T
Stack of coil 1 +2 1.3 T

## Slide 12
Single coil in LN2

## Slide 13
1 fit parameter: turn-turn contact resistance. 1 ohm*cm2
Single coil in LN2

## Slide 14
Coil fully
superconducting
Current partly driven in radial path
V=1e-5[V/m]*L
Single coil in LN2

## Slide 15: 2-stack LN2 test
1.3 T reached
1 coil
2 coils
3 coils
2 coils
LN2
15 K
done
soon

## Slide 16
Cryostat insert with two cryocoolers
Radiation shield
with MLI
Vacuum chamber
with pumps (not visible)
Electronic rack
vacuum control
temperature monitoring
voltage signals recording
quench detection system
2kA power converter
Water chillers
(for compressors and power converter)
Power cables
(500A single cables)
2 kA cryogen-free test stand at PSI

## Slide 17: Modeling
Modeling technique
COMSOL
based on Ratu Mataira 2020 Supercond. Sci. Technol. 33
Homogenized anisotropic winding pack
Time-dependent 2D axisymmetric
Electromagnetic + thermal coupled
Mechanics in separate step
Capabilities
Dynamic behaviour
Saturation
Screening currents
z
r

## Slide 18: Modeling
Modeling technique
COMSOL
based on Ratu Mataira 2020 Supercond. Sci. Technol. 33
Homogenized anisotropic winding pack
Time-dependent 2D axisymmetric
Electromagnetic + thermal coupled
Mechanics in separate step
Capabilities
Dynamic behaviour
Saturation
Screening currents
z
r
movie

## Slide 19
z
r
z
r
movies

## Slide 20: Test coil program
Commissioning of infrastructure at PSI
Winding
Soldering
Testing
Modeling
Cryogen-free test station (2 kA)
Tensioning system developed by
Francois-Olivier Pincot,
Jacky Mazet, CERN

## Slide 21: Contents
NI test coil program
NI superbend for SLS
NI racetrack demos
NI solenoid for
P3 experiment at PSI
NI solenoid for
FCC-ee positron source
Accelerator dipoles
time
Racetrack demos
explore insulation
/cable concepts
Non-insulated solenoids
x-insulated racetracks
1)
2)
2)
2024
3)
3)
4)
4)
Non-insulated racetracks

## Slide 22: Positron source
Option 2: NI HTS solenoid
State-of-the-art:
Pulsed NC magnet
SuperKEKB, Y. Enomoto et al
FCC-ee injector studies
Option 1: improved pulsed NC magnet
Pavel Martyshkin et al, BINP
Yield 0.58
Yield ~2.4
Yield 4+
DC
Radiation
NI magnet

## Slide 23: NI solenoid for positron source
22 coils
1500 A, 20 K
7 km tape
Stored energy ~ 1.6 MJ
Inductance ~ 0.7 H
Time constant ~1 h
Yield 4.7 (Y. Zhao, CERN)
Radiation load
Power acceptable (B. Humann , CERN)
Dose margins TBD
Limited by axial compressive stress
B [T]
r [m]
z [m]
target
e-
e+

## Slide 24: Proof-of-concept positron source experiment
Amorphous target
HTS solenoid
3 GHz SW RF structures
Spectrometer (horiz. Dipole)
Faraday cup / beam dump
Shielding
Girder
NC solenoids
Fast detecting cavity
L = 11.5 m
Zrel = 0
W = 3.6 m
1 m
1 m
R. Zennaro, PSI
SwissFEL PSI 2024

## Slide 25: Contents
NI test coil program
NI superbend for SLS
NI racetrack demos
NI solenoid for
P3 experiment at PSI
NI solenoid for
FCC-ee positron source
Accelerator dipoles
time
Racetrack demos
explore insulation
/cable concepts
Non-insulated solenoids
x-insulated racetracks
1)
2)
2)
2024
3)
3)
4)
4)
Non-insulated racetracks

## Slide 26: Swiss Light Source (SLS) superbends
Generate hard X-rays for TOMCAT beamline
LTS superbends under construction (C. Calzolaio, PSI)
SLS
2.9 T
SLS 2.0
5 T

## Slide 27: Swiss Light Source (SLS) superbends
SLS 2.0
5 T
4 K
SLS 2.x
NI HTS (or metal-insulated?)
Jeroen van Nugteren
8+ T
20 K
6 T
40 K
14 T

## Slide 28: Swiss Light Source (SLS) superbends
Jeroen van Nugteren
~1 km tape for both racetrack poles
Pancakes have nice dimensions (~130 m tape each)
for practical demo coils (test solenoids are ~80 m)
Field quality (field integral)
Mechanical support
Charging time
Quench behaviour
14 T

## Slide 29: Contents
NI test coil program
NI superbend for SLS
NI racetrack demos
NI solenoid for
P3 experiment at PSI
NI solenoid for
FCC-ee positron source
Accelerator dipoles
time
Racetrack demos
explore insulation
/cable concepts
Non-insulated solenoids
x-insulated racetracks
1)
2)
2)
2024
3)
3)
4)
4)
Non-insulated racetracks

## Slide 30: Contents
NI test coil program
NI superbend for SLS
NI racetrack demos
NI solenoid for
P3 experiment at PSI
NI solenoid for
FCC-ee positron source
Accelerator dipoles
time
Racetrack demos
explore insulation
/cable concepts
Non-insulated solenoids
x-insulated racetracks
1)
2)
2)
2024
3)
3)
4)
4)
Non-insulated racetracks

## Slide 31: Initial starting points
Cabling
Insulation

## Slide 32: Non-twisted soldered tape-stacks
Greg Brittles
Zachary Hartwig
Both major HTS users are
choosing same approach

## Slide 33: Smart insulation
dx.doi.org/10.1016/0032-3861(83)90201-X
Ramp time
Stability
resistivity
Best of both worlds by using
insulator/metal transition?

## Slide 34: Smart insulation
T. Mulder
500-1000x increase in resistivity
Smart insulation
Idea: create axial bypass instead of radial
Combine
milled soldered NI coil
carbon-based smart insulation
Deposit flat layer on flat surface

## Slide 35: Smart insulation

## Slide 36
NI coil
Milled NI coil
Milled NI coil
with axial bypass
fast ramp stability
NO
YES
YES
YES
YES
Heater activated
NO
Thermal runaway
Quench

## Slide 37: Smart insulation
Reproduce literature thin-layer resistivity
Small coils to demonstrate positive effect
Address mechanical issues (showstopper?)
Extrapolation to large dipoles (showstopper?)

## Slide 38: Contents
NI test coil program
NI superbend for SLS
NI racetrack demos
NI solenoid for
P3 experiment at PSI
NI solenoid for
FCC-ee positron source
Accelerator dipoles
time
Racetrack demos
explore insulation
/cable concepts
Non-insulated solenoids
x-insulated racetracks
1)
2)
2)
2024
3)
3)
4)
4)
Non-insulated racetracks