## Slide 1
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation
F. Gömöry, M. Solovyov
Institute of Electrical Engineering, Slovak Academy of Sciences, Bratislava, Slovakia
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland

## Slide 2
Introductory remarks
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Research focus of our group:
Electromagnetic behaviour of devices from CC tapes
mainly AC loss
Methodology: Modelling and experimental verification
using electric masurements

## Slide 3
Outline
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Introduction
Inspiration
Novelty
Application

## Slide 4
Introduction
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Device
(e.g. coil from CC tapes)
Icoil
local values
Modelling of AC loss

## Slide 5
Introduction
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Device
(e.g. coil from CC tapes)
local values
Modelling of AC loss

Ucoil
Ups
Ips
Icoil
Measurement of AC loss
(electric method)
derivation of Ucoil in modelling of AC loss  better comparison with experiment

## Slide 6
Inspiration
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
superconductor:
metals:
Example of using macroscopic quantities derived from numerical model – transport AC loss in CC tape

## Slide 7
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
macroscopic (measurable) quantity:
electric field intensity:
x
y
E. Pardo and F. Grilli, F.: Electromagnetic modeling of superconductors. In Numerical modeling of superconducting applications, World Sci Publ. Co. Pte. Ltd., 2023, Chapter 1.1.3
Inspiration
Example of using macroscopic quantities derived from numerical model – transport AC loss in CC tape

## Slide 8
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
Itape
[A]
t [s]
t [s]
t [s]
P [W/m]
Ej,compItape
Inspiration
Example of using macroscopic quantities derived from numerical model – transport AC loss in CC tape

## Slide 9
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
Itape
[A]
t [s]
Removing of purely inductive signal
t [s]
P [W/m]
Ej,compItape
Inspiration
Example of using macroscopic quantities derived from numerical model – transport AC loss in CC tape

## Slide 10
t [s]
Ej,comp
Ej
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
Itape
[A]
t [s]
t [s]
P [W/m]
Ej,compItape
[V/m]
Inspiration
Example of using macroscopic quantities derived from numerical model – transport AC loss in CC tape

## Slide 11
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
t [s]
P [W/m]
Check of correctness and precision:
=
Ej,compItape
t [s]
Ej,comp
Ej
[V/m]
Inspiration
Example of using macroscopic quantities derived from numerical model – transport AC loss in CC tape

## Slide 12
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
y
x
T = 0
T = Icoil/tSC
N = 10 turns, superconductor wSC = 12 mm  tSC = 10 µm, Bean model with Ic = 800 A,
wturn = wSC
tturn = 1 mm
homogenization (not necessary for 10 turns):
Loss density [J/m3]:
AC excitation [A]:
Loss per cycle [J/m]:
x
y
z
N, Amemiya, S. I. Murasawa, N. Banno N and K. Miyamoto,”Numerical modelings of superconducting wires for AC loss calculations,” Physica C 310 (1998) 16–29
E. Berrospe-Juarez, V. M. R. Zermeno, F. Triallaud and F. Grilli, “Real-time simulation of large-scale HTS systems: multi-scale and homogeneous models using the T–A formulation,” Supercond. Sci. Technol. 32 (2019) 065003
Inspiration – T-A formulation

## Slide 13
Novelty
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
how to extract the Ej ?
in ComsolMultiphysics, mf module:
then:
set as „external current density“,
Jz
ESC
Ez,mf
Ej
wt = 3.74

## Slide 14
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
voltage on coil terminations:
averaging over coil cross-section
similar approach applicable to H- fomulation:
F. Gömöry and J. Sheng.: Two methods of AC loss calculation in numerical modelling of superconducting coils. Supercond. Sci Technol. 30 (2017) 064005
representative:
is constant in each (fictive) turn
Novelty
Ej

## Slide 15
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
results for 50 Hz, Imax = 560 A
Chart: 
t [s]
Ecoil [V/m]
Qloss, j*E = 0.823 J/m
Qloss, I*E = 0.912 [J/m]
1st cycle:
Qloss, j*E = 1.06 J/m
Qloss, I*E = 1.07 [J/m]
2nd cycle:
Ecoil,comp [V/m]
Novelty

## Slide 16
Example of use: superferric accelerator magnet
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Chart: 
x
y
Superconducing coil
(upper double pancake)
Superconducing coil
(lower double pancake)
Magnet yoke
50 turns in each pancake
(200 turns in total)
12 mm wide CC tape
generating 1.6 T at
Imax = 530 A

## Slide 17
Example of use: superferric accelerator magnet
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Chart: 
t [s]
Ucoil [V/m]
Ucoil,comp [V/m]
Qloss, j*E = 178 J/m
Qloss, I*U = 181 [J/m]
2nd cycle:
1) Ic = const. = 1350 A, non-magnetic yoke
Loss per 1 m of winding (100 turns)
computations for Imax = 560 A, 50 Hz

## Slide 18
Example of use: superferric accelerator magnet
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Chart: 
t [s]
Ucoil [V/m]
Ucoil,comp [V/m]
Qloss, j*E = 156 J/m
Qloss, I*U = 162 [J/m]
2nd cycle:
2) ; magnetic yoke r = 600
computations for Imax = 560 A, 50 Hz

## Slide 19
Example of use: superferric accelerator magnet
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Chart: 
t [s]
Ucoil [V/m]
Ucoil,comp [V/m]
Qloss, j*E = 157 J/m
Qloss, I*U = 163 [J/m]
2nd cycle:
3) ; magnetic yoke r = r(B)
computations for Imax = 560 A, 50 Hz
B[T]

## Slide 20
Conclusions
It is possibe to extract the voltage on terminations of a superconducting CC pancake coil in electro-magnetic simulations utilising T-A formulation
Interpretation of the „loss voltage signal“ could provide better insight into coil operation
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Thank you

## Slide 21
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
Example of using macroscopic quantities derived from numerical model – AC loss in CC tape
macroscopic (measurable) quantities:
electric field intensity:
magnetic moment:
x
y
E. Pardo and F. Grilli, F.: Electromagnetic modeling of superconductors. In Numerical modeling of superconducting applications, World Sci Publ. Co. Pte. Ltd., 2023, Chapter 1.1.3
AC-AC case

## Slide 22
AC-AC case
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
Itape
[A]
Bappl
[T]
t [s]
t [s]
Example of using macroscopic quantities derived from numerical model – AC loss in CC tape
P [W/m]
t [s]
Ej,compItape

## Slide 23
AC-AC case
Voltage signals on the terminations of an HTS magnet modelled in A-T formulation HTS 2024 Modelling Workshop/ 10-13 June 2024, Bad Zurzach, Switzerland
Ag top
REBCO
buffers
Hastelloy
Ag side
Ag bottom
Cu top
Cu bottom
A- formulation in 2D
Example of using macroscopic quantities derived from numerical model – AC loss in CC tape
m [Am]
B [T
Check of correctness and precision:
=
7 mJ/m
22.5 mJ/m
32.5 mJ/m
Ej,comp
Ej
t [s]
[V/m]