## Slide 1
Electrothermal modeling of HTS coils
using homogenization and different formulations
A. Dadhicha, F. Grillib, K. Bergerc, G. Hajiric, F. Trillaud Pighid, D. Sotnikove, T. Salmif, G. dos Santosg, B. M. O. Santosg, F. G. R. Martinsh, T. Benkeli, A. Hussaina, E. Pardoa
  a Institute of Electrical Engineering, Slovak Academy of Sciences, Bratislava, SLOVAKIA b Karlsruhe Institute of Technology, Karlsruhe, GERMANY c Université de Lorraine, GREEN, Nancy, FRANCE d Instituto de Ingeniería, UNAM, Mexico City, MEXICO e Paul Scherrer Institut PSI, Villigen, SWITZERLAND f Tampere University, Tampere, FINLAND g Rio de Janeiro State University, Rio de Janeiro, BRAZIL h Universidade Federal Fluminense, Rio de Janeiro, BRAZIL i Atled Engineering, Oxford, UK

## Slide 2: Current applications
Ship Propulsion
Wind generator
MRI machines
Particle accelerators
Electric aircraft
High field magnets
Notes: Ship: https://global.kawasaki.com/en/corp/newsroom/news/detail/?f=20130529_1100
Wind: https://www.theva.com/applications/
Hyperloop:
https://zeleros.com/2019/06/19/zeleros-and-siemens-cooperate-to-develop-technology-for-the-hyperloop/

## Slide 3: Future applications
Hyperloop
Maglev trains
Fusion
Space propulsion
Notes: Ship: https://global.kawasaki.com/en/corp/newsroom/news/detail/?f=20130529_1100
Wind: https://www.theva.com/applications/
Hyperloop:
https://zeleros.com/2019/06/19/zeleros-and-siemens-cooperate-to-develop-technology-for-the-hyperloop/

## Slide 4
Racetrack coil
Application: Rotating machines, high field magnets
Pancake coil

## Slide 5
Modeling superconductors is tough and time consuming
Complicated non-linear multiphysics (specially for quench analysis)
Need for a fast and efficient method
Developed a novel and fast homogenization method!
Development and benchmark of various numerical models
14 models or combinations for different cases!
Collaboration between research teams within superconductor community
8 countries, 9 institutes!
Motivation

## Slide 6
Electrothermal modeling of HTS coils
using homogenization and different formulations
A. Dadhicha, F. Grillib, K. Bergerc, G. Hajiric, F. Trillaud Pighid, D. Sotnikove, T. Salmif, G. dos Santosg, B. M. O. Santosg, F. G. R. Martinsh, T. Benkeli, A. Hussaina, E. Pardoa
  a Institute of Electrical Engineering, Slovak Academy of Sciences, Bratislava, SLOVAKIA b Karlsruhe Institute of Technology, Karlsruhe, GERMANY c Université de Lorraine, GREEN, Nancy, FRANCE d Instituto de Ingeniería, UNAM, Mexico City, MEXICO e Paul Scherrer Institut PSI, Villigen, SWITZERLAND f Tampere University, Tampere, FINLAND g Rio de Janeiro State University, Rio de Janeiro, BRAZIL h Universidade Federal Fluminense, Rio de Janeiro, BRAZIL i Atled Engineering, Oxford, UK

## Slide 7
Institute of Electrical Engineering, Slovak Academy of Sciences
Bratislava, Slovakia

## Slide 8
Problem statements
Material properties
Numerical models
Benchmark results

## Slide 9
Problem statements
Material properties
Numerical models
Benchmark results

## Slide 10
Racetrack coil
Application: Rotating machines
2D cross section

## Slide 11
Many turns/tapes
in cross section
We consider infinitely long half-coil for benchmark

## Slide 12: Tape geometry
5 tapes
Width= 4 mm
Initial temperature = 77 K
Critical temperature = 92 K
Initial Jc = 1.875 x 1010 A/m2
Homogenized Cv, k, and
Electrical insulation between turns via Stycast

## Slide 13: Input : AC current (170 A and more, 5 Hz)
Ic = 150 A

## Slide 14
Pancake coil (axisymmetric assumption)
Application: High field magnets

## Slide 15: Tape geometry
5 tapes
Width= 4 mm
Initial temperature = 77 K
Critical temperature = 92 K
Initial Jc = 1.875 x 1010 A/m2
Homogenized Cv, k, and
Electrical insulation between turns via Stycast

## Slide 16: Input : Current ramp (1 A/s) up to 160 A and more
Ic = 150 A

## Slide 17: Cooling
By Dr. Frederic Sirois
Polytechnique Montreal

## Slide 18
Problem statements
Material properties
Homogenization
Numerical models
Benchmark results

## Slide 19
Electrical and thermal properties
Considered constant for simplification

## Slide 20
Problem statements
Material properties
Homogenization
Numerical models
Benchmark results

## Slide 21: Homogenization of layers
Include Stycast or not?
Stycast

## Slide 22
Homogenized electrical properties
Comes from power law
Normal conductivity
Parallel resistivity
(Electric field)
Total thickness

## Slide 23
Mass density
Thermal capacity
Anisotropic conductivity
Homogenized thermal properties
Cp= Cv/ρm

## Slide 24
Problem statements
Material properties
Numerical models
Benchmark results

## Slide 25: Different formulations and combinations

## Slide 26: Coupling
q(J) = E(J).J(T)

## Slide 27
Standard mesh and inputs
Mesh elements in tape thickness: 1
Mesh elements in tape width: 50
Time step per cycle: 200 (racetrack)
Time step per second: 20 (pancake)

## Slide 28
Problem statements
Material properties
Numerical models
Benchmark results
Racetrack coil (Detailed vs Homogenized models) Racetrack coil (Homogenized models)
Pancake coil (Detailed vs Homogenized models)

## Slide 29
Racetrack coil

## Slide 30
Only minimum temperature is affected with Stycast in homogenization
170 A
Very good agreement in maximum and average temperatures

## Slide 31
Maximum temperature matters for studies like quench
Detailed model predicts quench slightly earlier?
180 A

## Slide 32
Problem statements
Material properties
Numerical models
Benchmark results
Racetrack coil (Detailed vs Homogenized models) Racetrack coil (Homogenized models)
Pancake coil (Detailed vs Homogenized models)

## Slide 33
170 A (adiabatic)
Very good agreement!

## Slide 34
170 A (cooling)
Very good agreement!

## Slide 35
Total Power
170 A (cooling)
170 A (adiabatic)

## Slide 36
180 A (adiabatic)
Good agreement!
Minor difference due to mesh

## Slide 37
180 A (cooling)
Differences arise between models
But why?
Some homogenized models also predict quench at 1.85 s, like detailed models!

## Slide 38
1 % difference in power accuracy
initiates quench differently
By H-phi + FEM

## Slide 39
Total power
Average temperature
1 % difference in power accuracy
initiates quench differently
Even a very small difference in models can be important for some cases!

## Slide 40
190 A (cooling)
Very good agreement!

## Slide 41
Problem statements
Material properties
Numerical models
Benchmark results
Racetrack coil (Detailed vs Homogenized models) Racetrack coil (Homogenized models)
Pancake coil (Detailed vs Homogenized models)

## Slide 42
Pancake coil

## Slide 43
Adiabatic case
Very good agreement!
Quench is initiated faster due to tougher conditions
(even after including copper!)

## Slide 44
Cooling case
Quench is predicted slightly earlier than detailed model
Very good agreement!

## Slide 45: Conclusion

## Slide 46
Various models are benchmarked for homogenized method
      Very good agreement with detailed method
      Very good agreement between each other
Including Stycast in homogenization only affects minimum temperature
Even 1-2% difference between models can affect quench prediction

## Slide 47: Future work
More development of models and comparison with experiments
Publication of paper (stay tuned!)
Join our collaboration or questions? Contact: 

## Slide 48: Thank you!

## Slide 49: Questions?

## Slide 50
Extras

## Slide 51
180 adia total power