## Slide 1: Critical current numerical characterization of 6-layers CORC® cables
Sofia Viarengo1,2, Fabio Freschi1,3, Laura Savoldi1,4

## Slide 2: Outline
Framework
Aim of the work
Electromagnetic-thermal model
Model set-up
Results
Conclusions and perspectives

## Slide 3: ReBCO tapes and CORC® cables
High working temperature
High Jc
High field achievable
Compact layout
ReBCO tape
[From D.C. Van der Laan et al, 2019]
Conductor-on-Round-Core (CORC®)
Copper stabilizer
ReBCO
1.6 μm
Buffer zone
Substrate
Silver layer
2 - 4 mm
100 - 40 μm
Icon from: https://www.flaticon.com
Strain sensitive
Anisotropic properties
Complex geometry
High flexibility
Electric and mechanical isotropy
High thermal stability

## Slide 4: CORC® for high field applications
C2 wire layout [Courtesy of LBL]
BEST Central Solenoid coil
Canted-cosine theta (CCT) Accelerator
[Courtesy of EUROFusion]
CORC® cables are insert in a cable-in conduit conductor or in grooves
Considering them as macro-strands and we need to lump its electric/mechanical/thermal behaviour
Lack of data for a scaling law for Ic(B,T,ε) for the CORC®s

## Slide 5: Modeling HTS cables
New paradigms are emerging for HTS magnets:
New cable layouts (different from LTS magnets)
Not only internal forced flow cooling (as for LTS magnets)
Non-insulated tape layouts
Increasing operating temperatures ( 20 K):
  higher energy efficiency
  different material properties (higher heat capacity of solids, lower cryogen inventory)
Higher fields and currents involved
There are new challenges to consider for modelling and design next generation of magnets based on HTS material!
[From IREF23, L. Savoldi, M. Breschi, L. Bottura, follow-up at ASC24]

## Slide 6: Modeling CORC® cables
 We need new model for a proper description of the cable and prediction of Ic
Only round geometry HTS cable
No insulation between tapes
Tape and layers are electrically, thermally and mechanically coupled
What aboout CORC® cables? Which are the issues to tackle?
Multiphysics model needed
Electromagnetism
Heat transfer
Strain evaluation
Terminations strongly affects the VI curves
Non-uniform current distribution among tapes and layers

## Slide 7: Aim of the work
Tape assumed as a homogeneous and single material
scaled on operating conditions , and
Validated and verified for tapes, simpler geometries CORC® geometries (straight and bended)
Full 3D multiphysics model aims at the evalutation of the critical current Ic, with a self-consistent current redistribution.
Current redistribution among tapes and layers
Coupling with the thermal module which properly considered the cooling of the cable and analytical definition of strain map

## Slide 8: Verification and validation
Homogenized single tape
6-tapes straight CORC®
6-tapes bended CORC®
Further information here:
Further information here:

## Slide 9: Numerical multiphysics model based on T-A formulation
A-formulation (Whole domain)
Free convection
T-formulation (SC domain)
Joule Losses
Conduction among tapes
CORC®
Air domain
Heat conduction equation (SC domain)
Thin shell approximation
Homogenized properties weigthed on the cross section or on the mass

## Slide 10: Current-sharing boundary condition
Minimum domain: a CORC® pitch
Self-consistente current sharing condition!
Periodic boundary conditions (PBC) avoid edge effects!
Self-consistent condition in strong form!
Total current imposed in the last boundary
is unknown, equal and uniform along the edges.
Further information here:

## Slide 11: Model set-up
: intrisic strain due to the tape winding on the copper core.
[Bending of corc® cables and wires: Finite element parametric study and experimental validation, Anvar V.A., at el. SUST, 2018]
Strain map
Geometry 12-tapes CORC®

## Slide 12: Critical current scaling
Power Law
[2] From D.C. Van der Laan et al, 2019

## Slide 13: Results: current distribution
Joule power not relevant before the transition!

## Slide 14: Results: magnetic field distribution
Outermost layers shield the inner ones!

## Slide 15: Results: VI curve comparison
Electric field computation:
Where and
N-value largely overestimated,
Termination effect
[Ref: Weiss J., at el. SUST, 2017]

## Slide 16: Conclusion and future perspectives
Full 3D multiphysics model for CORC® cables based on T-A formulation has been developed in COMSOL Multiphysics
Implementation of a new boundary condition for the current distribution among tapes and geometrical strain consideration
Extend to more than 3 layers CORC®
Ic well-capture, overestimation of the n-value related to the terminations
In perspective:
Replicate the termination effect
Coupling with a mechanical module

## Slide 17
THANK YOU FOR YOUR ATTENTION!

## Slide 18
Back-up slides

## Slide 19: Appendix A: Thermal model for CORC®
Thermal model