## Slide 1
Xiang Kong1, Theo A. Tervoort1, Andre Brem2, Douglas Martin Araujo2, Michael Daly2, Bernhard Auchmann2,3
Department of Materials, ETH Zürich, Switzerland
Paul Scherrer Institution (PSI), Villigen, Switzerland
CERN, Geneva, Switzerland
11.10.2023
Mechanical modelling and failure identification of impregnated Nb3Sn Rutherford cable stacks
CHART Workshop 2023

## Slide 2: Introduction
Future Circular Collider (FCC)
CHART project
Daly et al. 2018
CERN website
Ferracin et al. 2015 Transactions on Applied Superconductivity (Volume: 26, Issue: 4, June 2016)
Daly et al. 2018 Transactions on Applied Superconductivity (Volume: 28, Issue: 3, April 2018)
20 mm
15 mm
15 mm
Transverse
Radial
Axial
Ferracin et al. 2015
Notes: CERN-FCC  CHART  scale to 10-stack

## Slide 3: Multiscale structure  heterogeneous
10-stack cable
Cubic level
Nb3Sn filament
Copper matrix
Void
Filament level
~15 mm
~ 1 mm
~750 μm
~50 μm
Ebermann et al. 2018
Epoxy
Strand
Insulation
Stainless-steel core
Stack level
Copper matrix
Nb3Sn micro filaments
Strand level
Ebermann et al. 2018, Supercond. Sci. Technol. 31 (2018) 065009
Rutherford cable stack
Vallone, MDP Meeting 2022
Notes:  Mechanical compressive testing

## Slide 4: Bibliography
‘Strain – stress’ identification
Fichera et al. 2019
Scheuerlein et al. 2019
Limitation:
Homogenization: 1D information
Hardly measure at cryogenics (e.g., LN2)
LVDT: Linear Variable Differential Transformer
Nonlinear  unloading  modulus
Vallone et al. 2018
Homogenization
Scheuerlein et al. 2019 Supercond. Sci. Technol. 32 (2019) 045011
Vallone et al. 2018 Transactions on Applied Superconductivity (Volume: 28, Issue: 4, June 2018)
Fichera et al. 2019 Transactions on Applied Superconductivity (Volume: 29, Issue: 7, October 2019)
Clip-on extensometer

## Slide 5: Structure
FEM modeling
[Nunio 2019]
Experiment
Component characterization
2D octagon
3D mesh
10-stack
Epoxy (CTD101K)
Annealed Copper
Fiber glass etc.
Transverse
Axial/radial/other loads
20 mm
15 mm
15 mm
Digital Image Correlation (DIC)
- Displacement field
- Strain field
‘Strand’ tracking
Measure by marker
Postprocess strain
Strain εyy field
Displacement Uy
Image analysis
Local measurement
Set-ups at LN2
Strain εyy field

## Slide 6: Image analysis: optical extensometer
Digital image correlation (DIC)
Courtesy of Tancogne-Dejean @MAVT-Mohr’s lab
1440x1080 px2, 17.1 μm/px
60 pixels ~1 mm
VIC2d
t0
t1
Yang, Bhattacharya, Exp Mech (2019)
Subset size  measure at stack level
Step size  control nodal points within one subset
Measure local displacement by undeformed markers at cubic level (15 mm)
2 mm
Notes: DIC technique  local or global methods  Experimental set-ups as optical extensometer  stack level: in situ measurement

## Slide 7: Image analysis: optical extensometer
Cubic level
Vertical displacement Uy [mm]
Stack level
Displacement-controlled: 10 μm/s ~ 1 kN/s
Image capture rate: 1 s-1 (273 images)
1D information
2D information

## Slide 8: Displacement fields at low force (20 MPa)
Horizontal displacement Ux [mm]
Vertical displacement Uy [mm]
CERN, 11T dipole magnet (2013)
 start from 20MPa as pre-loading
Reference
Deformed

## Slide 9: DIC results up to 150MPa
Strain εyy (-)
Vertical displacement Uy [mm]
Reference
Deformed
Sample edges (top/bottom) are the most deformed region (6%)
Some insulation layers are 1-2% strain level
The strain values depend on ‘mesh-equivalent’ parameters (subset, step)
Strain εyy (-)
Notes:  Find a ‘mesh-free’ approach to compare with different tests (camera, resolution etc)

## Slide 10: Particle tracking
1.7 mm
15 mm
Trackpy: python package for particle tracking
Strand core as natural mark (d~10 pixels)
Trajectory of each strand-core
Most (380/400) strands are tracked during the loading
There is a horizontal rigid body motion
Trackpy

## Slide 11: Fields comparison
VIC2d: subset:35, step:5, 17.1um/px
Uy (mm)
AL-DIC: 1440x1080 px2, subset:20 px, step:5 px
Uy (mm)
Particle track method
Uy (mm)
εyy
Reference
Deformed
There is a good agreement of displacement fields between two approaches.
Strand-based mesh

## Slide 12: Strain field
εyy
Conclusion
Strain localization at inter-stack and intra-stack
Local tensile state (red) exists
Deformation gradient F
Green-Lagrangian strain E
-1.5%
-1.0%
0
0.5%
-0.5%
1.0%

## Slide 13: From RT to LN2
Ceramic plate
Liquid nitrogen
(Tb = –196°C, 77 K)
Ceramic plate
Liquid nitrogen
(Tb = –196°C, 77 K)
Ceramic plate
Liquid nitrogen
(Tb = –196°C, 77 K)
Still developing:
Liquid boiling affects image capture
Notes: Sample in the liquid nitrogen  constant temperature;

## Slide 14: Conclusion & Outlook
An in situ full-field deformation measurement is performed at the level of cable stacks via two different image-based analyses
Compressive strain localization can be measured both at inter-stack and intra-stack, even tensile state at few positions
The approach will be applied at cryogenic temperature
The deformation measurement can be compared with the numerical results at multiscale

## Slide 15: Strand-like Azulejo (ceramic tilework) in Porto
Any questions?

## Slide 16: Correction
Due to less stiff of Zwick-50 machine, the unload-displacement (hysteresis loop?) is not corrected properly.
=150 kN/mm
= 60 kN/mm
Zwick100

## Slide 17: Machines with different measurements
Zwick050@D496
Zwick100@D467
Instron250@MAVT-Mohr
DIC
DIC
DIC
MacroExtenso
LaserExtenso
Global correction
Global correction
Global correction
laser

## Slide 18: Ongoing work @Z100-D467

## Slide 19: Aims
MagComp: Mechanical modelling and failure identification of impregnated Nb3Sn Rutherford cable stacks
Experiment
Numerical simulation
Characterize mechanical properties of each components at ambient and cryogenics temperature
Perform compressive tests on 10-stack sample
Implement the constitutive model in finite element software
Working with D. M. Araujo, M. Daly (PSI)
Cube level
Stack level
20 mm
15 mm
15 mm
Transverse
Radial
Axial