## Slide 1
Developments on muonic X-ray measurement system
for historical-cultural heritage samples
in Japan Proton Accelerator Research Complex (J-PARC)
Y. Miyake, T.Kutsuna, T.Saito, S. Takeshita, I. Umegaki, S. Doiuchi,
Y. Ishikake, A. Hashimoto, K. Shimomura
Motonobu Tampo (RCNP Osaka Univ)

## Slide 2
mKa-X ray of Al
~360keV
e-Ka X-ray :1.2 keV
Bound state for electrons
（no drop down）
Potential well in Al
Cu
Al
Depth profile of composition ratio
can be revealed
Muon as charged particle
can be selectively stopped
in target material
by changing muon energies
Muonic Xray from Au
Muonic X-ray from Ag
Muonic X-ray is unique and strong probe beam in non destructive elemental analysis
Incident muon
Muonic X-ray energy
is high, and easily penetrate
a sample surrounded with
thick covering layer
Muon captured in atom generates
a hard X-ray determined by quantum
transitions in atomic shell structures
Bound state for muon

## Slide 3
What is inside a glass bottle ?
What was the material
at the time it was made ?
Surface is oxidized !!
Nondestructive elemental analysis for historical heritage samples
How purity is
on surface ?
Different interests bring many samples and
different survey regions (depth, area)
Muon study for archeology samples has been started in J-PARC since 2017
We have been dedicating and developing beam character, detectors, chamber,
and safe sample holders for increasing detection efficiency
Is it letter used
in prehistory ?

## Slide 4
With one pulse,
X-rays
Germanium semiconductor detector
takes few tenth m sec for
signal processing so that in multi-hitting
X-rays energies are summed up !!
Segmented or small detector collections
can be individually measure
X-ray energies as single photon
0.1msec
(2 bunch)
Large solid angles with many small detectors
can increase detection efficiency
Muons
sample

## Slide 5
20MeV/c on 20mm diameter Carbon
Beam flux is controlled by using slits up and down stream
We choose LEGe detector (GL0110) with 100mm2 area and 10mm thick crystal
GL0110
GL0515
500mm2
100mm2
~25mm f
~10mm f
15mmt
10mmt
0.04~0.06count/pulse
Since each Ge has different solid angle,
the observed intensities are divided
with solid angles
0.05~0.07count/pulse

## Slide 6
MGe
Vacuum Al Chamber
(2014-2020)
2 LEGe can be placed from up stream side of beam
beam port with 380mm
diameter that was designed because
beam size was big
Inner diameter of chamber is
600mm
This chamber is also used for
Japanese old coins

## Slide 7
Atmosphere detection system
4 small and 2 big HPGe detectors can be placed
(2016~2021)
Kapton window 50mm thick and 50mm diameter is allowed to use muons from 13 MeV/c
Small one is called to LowEnergyGe(LEGe)

## Slide 8
muons
Ingredients of a drag used in 19th in a bottle that can not opened, are revealed with muons
From Osaka Univ Museum
Medical scientists
who became
the founder of
the Osaka University School of Medicine used this botte.
Glass
wall
Mercury Chroride with NaCl can be indicated !
Na(3-2)
47.12keV
Ca(4-3)
54.65keV
Cl(5-3)
57.71keV
Hg(9-8)
59.2keV

## Slide 10
LEGe
LEGe
MGe
MGe
MAGe
MGe
MAGe
9 Ge detectors can get closer
The sample can be covered with
larger solid angle of detectors
X-ray detection chamber rebuilding into Half Spherical Chamber
(2014-2020)
(2021- )
Only 2 Ge detectors can get closer to a sample.
Other detectors is put far from a sample.
Vacuum or He-gas environment
is compatible
For obtaining higher detection efficiency,
We have developed new detection chamber

## Slide 11
Up to 4.5MeV/c (=0.4mm)
Hemisphere Chamber system revealed that gold concentration in Kisei coin was enriched in depth at less than 1mm
41.6
18
10.7
10.2
6
6 hour
Error bar is decreased 3 times less than before
8.2
33.1
20.8
13
2.4
7.3 hour
22.3

## Slide 12
2020Dec～
2022May～2023June
2 LEGe(GL0110), and 2 MGe(GL0515)
5 LEGe(GL0110) 2 MGe
Edo silver coin(2nd)
16th gold sword decoration
16th gold coin
Edo silver coin(3rd)
Okinawa gold coin（syuli）
Bronz Dolphin in Nagoya castle
Gold Dolphin in Nagoya castle
Roman silver coin
Okinawa gold coin（nakagusuku）
CdTe（岡田）
LIB（豊田中研）
SRAM(ソシオネクスト）
SRAM
CdTe
5th Lettred stone
15th gold Lion
LIB
Half Spherical Chamber Developments; Increasing Ge detectors from 4 into 7.
and, also beam duct has been changed it with large diameter (See detail in poster session!)

## Slide 13
2021Feb（620kW)
2022Dec (730kW)
～1.2times
Same sample (Japanese Silver Coin) experiment
were able to provide detection efficiency difference between before and after upgrading
2 LEGe(GL0110), and 2 MGe(GL0515)
5 LEGe(GL0110) 2 MGe

## Slide 14
10hour＠5MeV/c
2hour＠5MeV/c
5times increase of detection efficiency compared to before up grade.
Measured peaks: Ag140keV/Cu115keV

## Slide 15
ch1
ch2
ch3
ch4
ch5
ch6
ch7
ch8
ch9
2hours
Roman Coin @20MeV/c
Present Status in Half Spherical Chamber system
We have increased totally 9 Ge detectors, 7 LEGe and 2 MGe.
Detector increases provide increases of detection
efficiency but do not provide 9times increase.

## Slide 16
Cu(5-4)53.2keV
Cu(4-3)115.1keV
Muons were stopped at 64um depth from surface
As muon impinging depth increases, observed intensity
of low-energy X-rays varied with the angle of detectors.
CH3,6,7 (72deg)
CH8,9
(65deg)
CH1,2,4,5
(43deg)
ch1
ch2
ch3
ch4
ch5
ch6
ch7
ch8
ch9
Beam axis

## Slide 17
We would like to place many detectors at an angle as close to
the beam axis as possible, but geometry no longer allows this.
Aiming to further increase detection efficiency….

## Slide 18
4million yen per detector
Modification of GL0110 to a 4-element detector
Removing each end-cap part, and converting 4-element detector
(~2.35x10^4 CHF)
Since each crystal is covered with metal end cap,
electrical noises are prevented such as cross-talk
If we rely on all to Canberra, it takes almost 10 times money. The modifications should be as simple as
possible, so that they can be done by other production company.

## Slide 19
「24eyes」: new detection system for future development
48mm
~50mm
Every detectors are placed at an angle of less than
50 deg.
The endcap can be close up to 60mm

## Slide 20
Summary
We have been developing detection systems of muonic X-ray suitable
for strong pulsed muon source.
In present, We have placed 9 Ge detectors and achieved 5 times increase
of detection efficiency compared between before and after upgrade.
Aiming further increase of detection efficiency,
We are planning to develop 4-elemental Ge detector by modifying 4 Ge detectors

## Slide 21
Yamanashi Prefectural
Museum
National Museum
of Nature and Science
T. Kutsuna
M. Saigan
Collaborators
National Museum
of Japanese history
T. Saito
Okayama Univ
A. Seike
N. Matsumoto
M.Tampo, Y. Miyake, S. Takeshita, I.Umegaki, and K. Shimomura
KEK MUSE
M. K. Kubo
K. Ninomiya
K. Takahashi
K. Takaura, A Sato
Osaka Univ
International
Christian Univ

## Slide 22
My suggestions for PSI and J-PARC collaborations in Muonic X-ray measurements.
In pulsed muon source, it is now big issue for measuring muon numbers precisely
knowing absolute efficiency observed
Muonic X-rays per muon is very important
Issue.
There are two ways to measure muon numbers
1. Measuring decay electrons
2. Measuring Muonic X-rays of Lyman alpha

## Slide 23
If we know production efficiency from muon absorbed Mg to 24Na,
from Mg activation measurements , we can know muon number.
2754keV
1368keV
24Na (T1/2 : ~15hours)
In PSI, precise muon number measuring can be done with
activation measurements. (I believe !)
I want to ask you is there such
shielding staffs in PSI muon?