## Slide 1: Measurement of Electromagnets and Tuning of Permanent Magnets based on Rotating Coils for the Upgrade of the Swiss Light Source (SLS2)
C. Zoller, M. Duda, T. Ernst, G. Montenero, R. Riccioli, V. van de Vijfeijken
IMMW23, Bad Zurzach, 08/10/2024

## Slide 2: Outline
Context
Rotating coils measurement system
Exemplary results electromagnets
Exemplary results permanent magnets
Conclusion
2
SLS2 magnets installed in the tunnel

## Slide 3: Context: Upgrade of the Swiss Light Source (SLS2)
Aim:
Increase electron beam energy from 2.4 GeV to 2.7 GeV
Improvement in emittance and brightness by factor 40
Maintain locations of undulator based beam lines and circumference 287.25 m
Resulting challenges for magnets:
Extremely dense Multi Bend Achromat lattice arrangement with
  888 electromagnets
  450 permanent magnets
  2 superconducting magnets
Installation of all magnets in the tunnel until end of 2024
3
More information see presentations of
S. Sanfilippo
M. Aiba
R. Riccioli
G. Montenero
and visit of SLS2 on Wednesday
SLS2 magnets installed in the tunnel

## Slide 4: Outline
Context
Rotating coils measurement system
Exemplary results electromagnets
Exemplary results permanent magnets
Conclusion
4
SLS2 magnets installed in the tunnel

## Slide 5: Measurement system: Rotating Coils (RC)
PCB with 5 radial coils (1 spare), each 120 turns (in collaboration with Elettra Synchrotron Trieste)
Shaft with hexagonal cross section
Reference radius: 18 mm
Active coil length: 500 mm
Digital bucking of dipole and quadrupole field components
Front view
Rear view

## Slide 6: Outline
Context
Rotating coils measurement system
Exemplary results electromagnets
Exemplary results permanent magnets
Conclusion
6
SLS2 magnets installed in the tunnel

## Slide 7: Specs electromagnets (EM)
Name | SOQ = HS2-A/B/G/H/K/L/M and OS2-A/B/E/F | HS2F-SXQ | SS2A-CH(S)/CV
Subtypes | 8 HS2i and 4 OS2i |  | 2 CH(S) and 1 CV
Length / mm | 230= 90 (SX) + 50 (OC) | 140, 90 (SX) | 105
/ mTm | - | - | 3.6
/ T/m2 | 5850 | 5850 | -
Amount | 264 | 24 | 112
Drawing |  |  | 
Name | SOQ = HS2-A/B/G/H/K/L/M and OS2-A/B/E/F | HS2F-SXQ | SS2A-CH(S)/CV
Subtypes | 8 HS2i and 4 OS2i |  | 2 CH(S) and 1 CV
Length / mm | 230= 90 (SX) + 50 (OC) | 140, 90 (SX) | 105
 | - | - | 3.6
 | 5850 | 5850 | -
Amount | 264 | 24 | 112
Drawing |  |  | 
7

## Slide 8: Measurement program EM:
Some magnets: Pre-heating of magnet (cooling water, nominal current) over night
Some magnets: Measurement of magnet position on bench with FARO or laser tracker
Some magnets: Degaussing
Measurement of Loadline (0 A -> +/- nominal current -> 0 A)
Measurement of roll angle, reference position, nominal current
Measurement of roll angle, flip position, nominal current
8
Determination of
Transfer Function (TF)
Harmonics
Magnetic axis
Roll angle
(1-σ repeatability < 0.05 %)
In case of combined-function- OC-NQ-SQ

## Slide 9: Results 82 OC with RC
Chart: Abs. Current [A]
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1 | 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
Avg TF | 0.064348 | 0.066388 | 0.067042 | 0.067379 | 0.067605 | 0.068335 | 0.068971 | 0.069837 | 0.071841 | 0.064192 | 0.066356 | 0.067026 | 0.067363 | 0.067578 | 0.068303 | 0.068935 | 0.069794 | 0.071762
Chart: Abs. Current [A]
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1 | 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
Avg TF | 0.059983 | 0.061995 | 0.062614 | 0.062959 | 0.063191 | 0.063897 | 0.064514 | 0.065387 | 0.067314 | 0.059904 | 0.062001 | 0.062639 | 0.062975 | 0.063191 | 0.063899 | 0.064522 | 0.065394 | 0.067332
9
Av. TF of NQ
Chart: Abs. current [A]
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1 | 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
Avg TF | 678.792 | 697.9116 | 703.1819 | 705.2807 | 706.324 | 716.3012 | 723.0842 | 731.3908 | 749.2819 | 677.265 | 697.832 | 703.4087 | 705.4946 | 706.3201 | 716.2997 | 723.125 | 731.4877 | 749.4761
Average Transfer function (TF) of OC
Av. TF of SQ
Integr. Strength | Meas. Average (T/m2) | s (unit) | Meas. vs. Sim. (%)
OA/OB | 3530 | 23 | +1.5
OE/OF | 3531 | 25 | +1.7
Integrated field strength: small spread, discrepancies with simulation ~1.6 %

## Slide 10: Results 82 OC with RC
Chart: 
Chart: an and bn in 10-4 of main field [units]
| b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8 | b9 | a9 | b10 | a10
Lebels | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12
 | 20.7687 | -0.15986 | 5.1599 | -2.1598 | 6.0044 | 1.0605 | 7.4696 | -0.22321 | 4.9679 | 0.31367 | 4.6042 | 0.46887
10
Harmonics, OC
Roll angle, OC
Small multipole values
Roll angles below 0.5 mrad (few higher)

## Slide 11: Results 82 OC with RC
Chart: 
Chart: an and bn in 10-4 of main field [units]
| b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8 | b9 | a9 | b10 | a10
Lebels | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12
 | 20.7687 | -0.15986 | 5.1599 | -2.1598 | 6.0044 | 1.0605 | 7.4696 | -0.22321 | 4.9679 | 0.31367 | 4.6042 | 0.46887
11
Harmonics, OC
Roll angle, OC
Small multipole values
Roll angles below 0.5 mrad (few higher)
Due to good quality, individual measurements stopped after 82 magnets
all magnets measured with vibrating vire system (talk of M. Aiba)

## Slide 12: Results 116 SX/SXQ with RC: exemplary HS2A and -B
12
Chart: Current [A]
| 10 | 20 | 30 | 40 | 50 | 40 | 30 | 20 | 10
6A | -12.3874 | -12.3576 | -12.3605 | -12.2525 | -11.1095 | -12.3266 | -12.4341 | -12.4783 | -12.5812
2A | -12.393 | -12.3624 | -12.366 | -12.2616 | -11.1163 | -12.3356 | -12.4403 | -12.4842 | -12.5871
1A | -12.3705 | -12.3402 | -12.3323 | -12.1812 | -11.0791 | -12.2648 | -12.4058 | -12.4635 | -12.5756
7A | -12.3758 | -12.3421 | -12.3443 | -12.2362 | -11.1002 | -12.3121 | -12.4247 | -12.4727 | -12.5839
9A | -12.3845 | -12.3536 | -12.3558 | -12.2461 | -11.1154 | -12.3182 | -12.4326 | -12.4805 | -12.5866
4A | -12.3753 | -12.3427 | -12.3444 | -12.2362 | -11.1071 | -12.3124 | -12.4249 | -12.4737 | -12.5846
8A | -12.3875 | -12.3572 | -12.3605 | -12.2547 | -11.1137 | -12.3285 | -12.4347 | -12.4792 | -12.5822
5A | -12.3795 | -12.3474 | -12.3501 | -12.2433 | -11.1081 | -12.3188 | -12.4252 | -12.4709 | -12.5762
3A | -12.3826 | -12.3494 | -12.3513 | -12.244 | -11.1092 | -12.3173 | -12.4253 | -12.472 | -12.5765
5B | -12.3924 | -12.3627 | -12.3652 | -12.253 | -11.1207 | -12.327 | -12.4393 | -12.4845 | -12.586
8B | -12.3983 | -12.3652 | -12.3665 | -12.2552 | -11.1176 | -12.3256 | -12.4408 | -12.4877 | -12.5937
1B | -12.3855 | -12.3551 | -12.3587 | -12.2522 | -11.1072 | -12.3247 | -12.4331 | -12.4785 | -12.5819
Chart: Current [A]
| 10 | 20 | 30 | 40 | 50 | 40 | 30 | 20 | 10
15A | 12.3964 | 12.37 | 12.3726 | 12.26 | 11.1244 | 12.3413 | 12.4517 | 12.4985 | 12.602
16A | 12.3912 | 12.3627 | 12.361 | 12.2344 | 11.1061 | 12.3193 | 12.4425 | 12.4932 | 12.6005
17A | 12.3835 | 12.3557 | 12.3516 | 12.2205 | 11.1006 | 12.3043 | 12.4335 | 12.4857 | 12.5925
18A | 12.3865 | 12.3565 | 12.3508 | 12.2055 | 11.0866 | 12.298 | 12.4372 | 12.4954 | 12.6105
13B | 12.3846 | 12.3564 | 12.3554 | 12.2271 | 11.0941 | 12.3156 | 12.4413 | 12.4951 | 12.609
14B | 12.3867 | 12.3594 | 12.3584 | 12.2225 | 11.0884 | 12.3144 | 12.4459 | 12.5016 | 12.6159
11B | 12.3848 | 12.3594 | 12.3602 | 12.2432 | 11.1204 | 12.3231 | 12.4391 | 12.4877 | 12.5895
12B | 12.3853 | 12.3603 | 12.3635 | 12.2514 | 11.1079 | 12.3322 | 12.4469 | 12.4948 | 12.6009
10B | 12.3845 | 12.357 | 12.3531 | 12.2115 | 11.0882 | 12.3025 | 12.439 | 12.4957 | 12.6103
TF, negative polarity
TF, positive polarity
Integrated field strength: small spread – Meas. values ~3 % above the computed ones

## Slide 13: Results 116 SX/SXQ with RC: exemplary HS2A and -B
13
Chart: an and bn in 10-4 of main field [units]
| b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8 | b9 | a9 | b10 | a10
Lebels | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12
 | 2.5338 | -1.4221 | -3.2304 | -0.43378 | 0.3079 | -1.1567 | -0.8948 | -0.32819 | 0.19671 | -0.83131 | 18.9287 | 0.87907 | -0.17076 | -0.92274
Harmonics, negative polarity
Chart: an and bn in 10-4 of main field [units]
| b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8 | b9 | a9 | b10 | a10
Lebels | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12
 | 5.1985 | -3.4263 | -1.9906 | -0.823 | 1.3695 | 0.1143 | -1.2936 | -0.08832 | 0.9358 | 0.032811 | 18.9487 | 0.92589 | -0.46396 | -0.53262
Harmonics, positive polarity
Higher b9 by design
Chart: Magnet ID
| 6A | 2A | 1A | 7A | 9A | 4A | 8A | 5A | 3A | 15A | 16A | 17A | 18A | 13B | 14B | 11B | 12B | 10B | 5B | 8B | 1B | 4B | 9B | 3B | 2B | 6B
Roll HS2AB [mrad] | 0.12468 | -0.23136 | -0.96379 | -0.11416 | -0.0093447 | -0.064891 | 0.075038 | -0.065588 | -0.32927 | -0.36055 | -0.15462 | 0.0068223 | -0.065136 | 0.050525 | 0.0020084 | 0.099064 | -0.036577 | -0.15795 | -0.15538 | -0.54796 | -0.36465 | -0.41181 | -0.081924 | -0.039957 | -0.26273 | -0.30682
upper limit | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5
lower limit | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5
Roll angle
First magnet produced, manufacturing corrected after
All other multipoles
< 10 u, small spread
Roll angles below 0.5 mrad

## Slide 14: Results 116 SX/SXQ with RC: exemplary HS2A and -B
14
Chart: an and bn in 10-4 of main field [units]
| b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8 | b9 | a9 | b10 | a10
Lebels | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12
 | 2.5338 | -1.4221 | -3.2304 | -0.43378 | 0.3079 | -1.1567 | -0.8948 | -0.32819 | 0.19671 | -0.83131 | 18.9287 | 0.87907 | -0.17076 | -0.92274
Harmonics, negative polarity
Chart: an and bn in 10-4 of main field [units]
| b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8 | b9 | a9 | b10 | a10
Lebels | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12 | -12
 | 5.1985 | -3.4263 | -1.9906 | -0.823 | 1.3695 | 0.1143 | -1.2936 | -0.08832 | 0.9358 | 0.032811 | 18.9487 | 0.92589 | -0.46396 | -0.53262
Harmonics, positive polarity
Higher b9 by design
Chart: Magnet ID
| 6A | 2A | 1A | 7A | 9A | 4A | 8A | 5A | 3A | 15A | 16A | 17A | 18A | 13B | 14B | 11B | 12B | 10B | 5B | 8B | 1B | 4B | 9B | 3B | 2B | 6B
Roll HS2AB [mrad] | 0.12468 | -0.23136 | -0.96379 | -0.11416 | -0.0093447 | -0.064891 | 0.075038 | -0.065588 | -0.32927 | -0.36055 | -0.15462 | 0.0068223 | -0.065136 | 0.050525 | 0.0020084 | 0.099064 | -0.036577 | -0.15795 | -0.15538 | -0.54796 | -0.36465 | -0.41181 | -0.081924 | -0.039957 | -0.26273 | -0.30682
upper limit | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5
lower limit | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5 | -0.5
Roll angle
First magnet produced, manufacturing corrected after
All other multipoles
< 10 u, small spread
Roll angles below 0.5 mrad
Due to good quality, individual measurements stopped after 116 magnets
all magnets measured with vibrating vire system (talk of M. Aiba)

## Slide 15: Results 112 CH(S)/CV with RC: exemplary CH/CV
Chart: Abs I in A
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
TF CH (pos I) | 1.5953 | 1.6162 | 1.6184 | 1.6112 | 1.5919 | 1.6403 | 1.6608 | 1.6794 | 1.7131
TF CH (neg I) | 1.5896 | 1.6155 | 1.6183 | 1.6115 | 1.5922 | 1.6408 | 1.6611 | 1.6798 | 1.7139
Chart: Abs I in A
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
TF CV (pos I) | -1.055 | -1.0756 | -1.0812 | -1.0817 | -1.0795 | -1.1005 | -1.1129 | -1.1255 | -1.1543
TF CV (neg I) | -1.0503 | -1.0744 | -1.0811 | -1.0819 | -1.0798 | -1.1009 | -1.1133 | -1.1261 | -1.1553
15
Av. TF, CH
Av. TF, CV
Vertical steering & horizontal steering strength as expected

## Slide 16: Results 112 CH(S)/CV with RC: exemplary CH/CV
Chart: harmonic number
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Av b in u | -28.9896 | -196.7313 | 0.20598 | -4.5431 | 0.092975 | -0.31684 | 0.3629 | 0.30655 | 0.38222
Av a in u | -136.5153 | -8.4353 | 1.8324 | -0.23229 | -0.12242 | -0.065657 | 0.91651 | -0.045623 | 0.46234
Chart: harmonic number
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Av b in u | 56.546 | 9.9542 | -2.5135 | -0.64989 | -0.15962 | 0.16024 | 0.43716 | -0.33921 | -0.46627
Av a in u | -102.7633 | -196.2024 | -0.73403 | 5.4772 | -0.54037 | -0.087636 | 0.53741 | -0.41743 | -0.38121
16
Harmonics, CV
Multipoles as expected
Chart: magnet ID
| 20 | 39 | 43 | 63 | 41 | 6 | 3 | 37 | 8 | 59 | 4 | 68 | 19 | 42 | 31 | 5 | 47 | 70 | 17 | 112 | 89 | 51 | 69 | 7 | 98 | 72 | 27 | 48 | 57 | 33 | 25 | 28 | 16 | 67 | 15 | 35 | 38 | 30 | 26 | 100 | 34 | 44 | 22 | 32 | 61 | 36
CV (CH-CV series) | 0.37421 | 0.58163 | 0.6105 | 0.17885 | 0.59884 | 0.64953 | -0.0070511 | 0.3298 | 0.67099 | 0.65852 | 0.60461 | 0.56671 | 0.82254 | 0.55409 | 0.72304 | 0.65933 | 0.33735 | 0.52129 | 0.84985 | 0.65132 | 0.50101 | 0.3394 | 0.6211 | 0.61765 | 0.95634 | 0.42109 | 0.56274 | 0.15895 | 0.15507 | 0.44741 | 0.58345 | 0.46931 | 0.5431 | 0.52784 | 0.91687 | 0.4706 | 0.66308 | 0.46188 | 0.93229 | 0.41811 | 0.32162 | 0.67175 | 0.2326 | 0.19151 | 0.050344 | -0.017344
Chart: magnet ID
| 3 | 4 | 5 | 6 | 7 | 8 | 15 | 16 | 17 | 19 | 20 | 22 | 25 | 26 | 27 | 28 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 41 | 42 | 43 | 44 | 47 | 48 | 51 | 57 | 59 | 61 | 63 | 67 | 68 | 69 | 70 | 72 | 89 | 98 | 100 | 112
CH (CH-CV Series) | -0.76015 | -0.59737 | -0.63149 | -0.21111 | -0.52327 | -0.34419 | -0.50365 | -0.4756 | -0.45045 | -0.96409 | -0.77912 | -0.95621 | -0.41797 | -0.38858 | -0.75349 | -0.65476 | -0.668 | -0.70778 | -0.31594 | -0.3287 | -0.7299 | -0.459 | -0.73798 | -0.39316 | -0.78069 | -0.99645 | -0.43609 | -0.97 | -0.70577 | -0.86419 | -1.3063 | -1.3194 | -0.37039 | -0.82154 | -0.37753 | -1.087 | -0.65947 | -0.6922 | -0.65761 | -0.70585 | -0.79552 | -0.42291 | -0.47695 | -0.59154 | -0.15913 | -1.0903
Roll angles between +/-1 mrad (few higher)
sextupole ~200 units
Harmonics, CH

## Slide 17: Results 112 CH(S)/CV with RC: exemplary CH/CV
Chart: harmonic number
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Av b in u | -28.9896 | -196.7313 | 0.20598 | -4.5431 | 0.092975 | -0.31684 | 0.3629 | 0.30655 | 0.38222
Av a in u | -136.5153 | -8.4353 | 1.8324 | -0.23229 | -0.12242 | -0.065657 | 0.91651 | -0.045623 | 0.46234
Chart: harmonic number
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Av b in u | 56.546 | 9.9542 | -2.5135 | -0.64989 | -0.15962 | 0.16024 | 0.43716 | -0.33921 | -0.46627
Av a in u | -102.7633 | -196.2024 | -0.73403 | 5.4772 | -0.54037 | -0.087636 | 0.53741 | -0.41743 | -0.38121
17
Harmonics, CV
Multipoles as expected
Chart: magnet ID
| 20 | 39 | 43 | 63 | 41 | 6 | 3 | 37 | 8 | 59 | 4 | 68 | 19 | 42 | 31 | 5 | 47 | 70 | 17 | 112 | 89 | 51 | 69 | 7 | 98 | 72 | 27 | 48 | 57 | 33 | 25 | 28 | 16 | 67 | 15 | 35 | 38 | 30 | 26 | 100 | 34 | 44 | 22 | 32 | 61 | 36
CV (CH-CV series) | 0.37421 | 0.58163 | 0.6105 | 0.17885 | 0.59884 | 0.64953 | -0.0070511 | 0.3298 | 0.67099 | 0.65852 | 0.60461 | 0.56671 | 0.82254 | 0.55409 | 0.72304 | 0.65933 | 0.33735 | 0.52129 | 0.84985 | 0.65132 | 0.50101 | 0.3394 | 0.6211 | 0.61765 | 0.95634 | 0.42109 | 0.56274 | 0.15895 | 0.15507 | 0.44741 | 0.58345 | 0.46931 | 0.5431 | 0.52784 | 0.91687 | 0.4706 | 0.66308 | 0.46188 | 0.93229 | 0.41811 | 0.32162 | 0.67175 | 0.2326 | 0.19151 | 0.050344 | -0.017344
Chart: magnet ID
| 3 | 4 | 5 | 6 | 7 | 8 | 15 | 16 | 17 | 19 | 20 | 22 | 25 | 26 | 27 | 28 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 41 | 42 | 43 | 44 | 47 | 48 | 51 | 57 | 59 | 61 | 63 | 67 | 68 | 69 | 70 | 72 | 89 | 98 | 100 | 112
CH (CH-CV Series) | -0.76015 | -0.59737 | -0.63149 | -0.21111 | -0.52327 | -0.34419 | -0.50365 | -0.4756 | -0.45045 | -0.96409 | -0.77912 | -0.95621 | -0.41797 | -0.38858 | -0.75349 | -0.65476 | -0.668 | -0.70778 | -0.31594 | -0.3287 | -0.7299 | -0.459 | -0.73798 | -0.39316 | -0.78069 | -0.99645 | -0.43609 | -0.97 | -0.70577 | -0.86419 | -1.3063 | -1.3194 | -0.37039 | -0.82154 | -0.37753 | -1.087 | -0.65947 | -0.6922 | -0.65761 | -0.70585 | -0.79552 | -0.42291 | -0.47695 | -0.59154 | -0.15913 | -1.0903
Roll angles between +/-1 mrad (few higher)
sextupole ~200 units
Harmonics, CH
Good quality of magnets delivered

## Slide 18: Outline
Context
Rotating coils measurement system
Exemplary results electromagnets
Exemplary results permanent magnets
Conclusion
18
SLS2 magnets installed in the tunnel

## Slide 19: Specs permanent magnets (PM)
Name | AN (QS2D) | ANM (QS2C) | VE (QS2K)
Subtypes | 10 | 2 | 2
Length / mm | 140 | 150 | 240
Field / T | +0.26947 | +0.27246 | -0.65495
Gradient/ T/m | -77.6562 | -82.8733 | +45.7648
Amount | 120 (10x12) | 24 (12+12) | 24 (12+12)
Drawing |  |  | 
19

## Slide 20: Measurement program PM
Pre-warming of magnets for 3 days in building, 1 night in hutch
Mechanical preparation of magnets
20

## Slide 21: Measurement program PM
RC measurement with moderator plates at 0-position
RC measurement with shims
21
Insertion of shims
Moderator plates at 0-position

## Slide 22: Measurement program PM
Tuning of magnet (closing moderator plates) to target value +/- 3 u (10 types)
RC measurement of harmonics, magnetic axis and roll angle in reference position
22
Magnet Type (AN label) | B2_Nominal (T) | Shim (mm)
ANO1 | -11.43486087 | NO
ANI2 | -11.26424458 | 4.5
ANO3 | -11.41488081 | NO
ANI4 | -11.33068781 | 2.5
ANO5 | -11.4197839 | NO
ANI6 | -11.35074981 | 2
ANO7 | -11.40144712 | NO
ANI8 | -11.348197 | 2
ANO9 | -11.36359016 | 2
ANI10 | -11.31130482 | 2.5

## Slide 23: Measurement program PM
Measurement of magnet position on bench with AT500 laser tracker
  Level laser w.r.t. gravity
  Adjust measurement template in Spatial Analyzer
  Align instrument -> Measure the fiducial of the bench -> check RMS < 10 um compared to reference magnet measurement
  Measure magnet fiducials
  Measure base plate fiducials -> check AVG Mag < 10 um and Max Mag < 15 um compared to reference magnet measurement
23
Laser tracker
Moderator plates in tuned position

## Slide 24: Measurement program PM
RC Measurement of roll angle, flip position
Perform axis transfer compared to moving wire measurement
Export fiducialization file
Upload information on inventory database
24

## Slide 25: Results PM, exemplary for AN
Chart: an and bn in 10-4 of main field [units]
| b3 | a3 | b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8 | b9 | a9 | b10 | a10
 | 4.7393 | -3.1282 | -3.1156 | -0.20192 | 0.26396 | 0.49853 | 0.63412 | 0.57494 | 0.012392 | -0.075546 | 0.50132 | 0.12052 | -0.041445 | -0.10495 | -0.018836 | -0.064414
Labels | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15 | -15
Chart: Magnet ID
Average | -11.6765 | -11.6765
25
B2/RRef, before tuning
Harmonics
Successful tuning for each spec to below +/- 3 u
Field strength getting lower with time due to adjustment of PM block assembly plan (10 charges) as expected
Low multipole values <10 units,
small spread
Roll angles below 0.5 mrad

## Slide 26: Conclusion
Rotating coils have proved to be the «working horse» for the SLS2 magnetic measurements
Successful series measurement with this RC system of
  Electromagnets:
    116 Sextupoles (8 types)
    82 combined-function Octupoles (with Normal Quad and Skew Quad) (4 types)
    112 steerers (i.e. 112 CH(S)+112 CV)
    55 QP+53 QPH magnets (presented during last IMMW)
  Permanent magnets:
    120 AN (10 types)
    24 ANM (2 types)
    24 VE (2 types)
26

## Slide 27: Thank you for your interest
We would like to thank:
PSI line managers for their support during this massive undertaking
PSI technicians for their highly valued contributions in manufacturing parts, assembly, crane operation, …
Logistics team for making in-time deliveries and pre-warming possible
27
C. Zoller, M. Duda, T. Ernst, G. Montenero, R. Riccioli, V. van de Vijfeijken
IMMW23, Bad Zurzach, 08/10/2024

## Slide 28: Results 116 SX/SXQ with RC: harmonics
28
5 types

## Slide 29: Transfer function with 3 σ
Chart: CHS (CHS-CV series)
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
TF CHS (pos I) | 1.5299 | 1.5498 | 1.5442 | 1.5147 | 1.4225 | 1.5454 | 1.5867 | 1.6108 | 1.6461
TF CHS (neg I) | 1.5297 | 1.5496 | 1.5441 | 1.5148 | 1.4226 | 1.5455 | 1.5867 | 1.6108 | 1.646
Chart: CV (CHS-CV series)
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
TF CV (pos I) | -1.0453 | -1.0695 | -1.0763 | -1.0772 | -1.0749 | -1.0956 | -1.1076 | -1.1197 | -1.1478
TF CV (neg I) | -1.0461 | -1.0695 | -1.076 | -1.0768 | -1.0747 | -1.0955 | -1.1077 | -1.1203 | -1.1494
Chart: CH (CH-CV series)
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
TF CH (pos I) | 1.5953 | 1.6162 | 1.6184 | 1.6112 | 1.5919 | 1.6403 | 1.6608 | 1.6794 | 1.7131
TF CH (neg I) | 1.5896 | 1.6155 | 1.6183 | 1.6115 | 1.5922 | 1.6408 | 1.6611 | 1.6798 | 1.7139
Chart: CV (CH-CV series)
| 1 | 2 | 3 | 4 | 5 | 4 | 3 | 2 | 1
TF CV (pos I) | -1.055 | -1.0756 | -1.0812 | -1.0817 | -1.0795 | -1.1005 | -1.1129 | -1.1255 | -1.1543
TF CV (neg I) | -1.0503 | -1.0744 | -1.0811 | -1.0819 | -1.0798 | -1.1009 | -1.1133 | -1.1261 | -1.1553
29

## Slide 30: Average harmonics at with min and max
Chart: CH (CH-CV series)
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Av b in u | -28.9896 | -196.7313 | 0.20598 | -4.5431 | 0.092975 | -0.31684 | 0.3629 | 0.30655 | 0.38222
Av a in u | -136.5153 | -8.4353 | 1.8324 | -0.23229 | -0.12242 | -0.065657 | 0.91651 | -0.045623 | 0.46234
Chart: CV (CH-CV series)
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Av b in u | 56.546 | 9.9542 | -2.5135 | -0.64989 | -0.15962 | 0.16024 | 0.43716 | -0.33921 | -0.46627
Av a in u | -102.7633 | -196.2024 | -0.73403 | 5.4772 | -0.54037 | -0.087636 | 0.53741 | -0.41743 | -0.38121
Chart: CHS (CHS-CV series)
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Av b in u | 50.5413 | -220.947 | 2.3115 | -5.8014 | 0.41433 | -0.028619 | 0.36428 | 0.18628 | 0.25682
Av a in u | -132.0281 | -8.6602 | 1.3513 | -0.11004 | 0.65987 | -0.22123 | 0.86813 | -0.016052 | 0.2131
Chart: CV (CHS-CV series)
| 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Av b in u | 56.0604 | 12.0875 | -2.4277 | -0.5454 | -0.165 | 0.20267 | 0.38944 | -0.36659 | -0.45879
Av a in u | -105.8212 | -191.7932 | -0.31812 | 5.5723 | -0.48265 | -0.074843 | 0.54608 | -0.40605 | -0.40734
30

## Slide 31: Roll angle at
Chart: CHS (CHS-CV Series)
Chart: CV (CHS-CV Series)
Chart: CH (CH-CV Series)
| 20 | 39 | 43 | 63 | 41 | 6 | 3 | 37 | 8 | 59 | 4 | 68 | 19 | 42 | 31 | 5 | 47 | 70 | 17 | 112 | 89 | 51 | 69 | 7 | 98 | 72 | 27 | 48 | 57 | 33 | 25 | 28 | 16 | 67 | 15 | 35 | 38 | 30 | 26 | 100 | 34 | 44 | 22 | 32 | 61 | 36
CV (CH-CV series) | 0.37421 | 0.58163 | 0.6105 | 0.17885 | 0.59884 | 0.64953 | -0.0070511 | 0.3298 | 0.67099 | 0.65852 | 0.60461 | 0.56671 | 0.82254 | 0.55409 | 0.72304 | 0.65933 | 0.33735 | 0.52129 | 0.84985 | 0.65132 | 0.50101 | 0.3394 | 0.6211 | 0.61765 | 0.95634 | 0.42109 | 0.56274 | 0.15895 | 0.15507 | 0.44741 | 0.58345 | 0.46931 | 0.5431 | 0.52784 | 0.91687 | 0.4706 | 0.66308 | 0.46188 | 0.93229 | 0.41811 | 0.32162 | 0.67175 | 0.2326 | 0.19151 | 0.050344 | -0.017344
Chart: CH (CH-CV Series)
| 3 | 4 | 5 | 6 | 7 | 8 | 15 | 16 | 17 | 19 | 20 | 22 | 25 | 26 | 27 | 28 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 41 | 42 | 43 | 44 | 47 | 48 | 51 | 57 | 59 | 61 | 63 | 67 | 68 | 69 | 70 | 72 | 89 | 98 | 100 | 112
CH (CH-CV Series) | -0.76015 | -0.59737 | -0.63149 | -0.21111 | -0.52327 | -0.34419 | -0.50365 | -0.4756 | -0.45045 | -0.96409 | -0.77912 | -0.95621 | -0.41797 | -0.38858 | -0.75349 | -0.65476 | -0.668 | -0.70778 | -0.31594 | -0.3287 | -0.7299 | -0.459 | -0.73798 | -0.39316 | -0.78069 | -0.99645 | -0.43609 | -0.97 | -0.70577 | -0.86419 | -1.3063 | -1.3194 | -0.37039 | -0.82154 | -0.37753 | -1.087 | -0.65947 | -0.6922 | -0.65761 | -0.70585 | -0.79552 | -0.42291 | -0.47695 | -0.59154 | -0.15913 | -1.0903
31

## Slide 32: Measurement system: Rotating Coils (RC)
PCB with 5 radial coils (1 spare), each 120 turns (in collaboration with Elettra Synchrotron Trieste)
Reference radius: 18 mm
Active coil length: 500 mm
Digital bucking of dipole and quadrupole field components
Shaft with hexagonal cross section
x
y
Beam entrance
CW winding
Start (Bk)
Connections
Maxon motor
FF