## Slide 1: Hall mapper for magnet sorting
P. Vagin, Deutsches Elektronen Synchrotron
08.10.2024, IMMW23

## Slide 2: Direct measurement of magnetic errors
Poster M. Tischer “Magnetic Measurements and Tuning of an APPLE-III Undulator for FLASH at DESY”

## Slide 3: Magnet characterization by stretched wire
Poster M. Gehlot “PM & Fe Material Characterization for PETRA IV DLQ Prototype Magnets”
Optimze magnet model parameters to fit measured data

## Slide 4: Model of magnet errors
Hall probe field map measurements
Nonuinform magnetization by individual M of each subblock optimized to match measured and model fields
Measured
Model
Initial
Optimized

## Slide 5: Magnetic moment of magnet model
Magnetic moment of magnet model with errors vs Helmholtz measurements
Absolute values require proper susceptibility and calibration of distance to magnet
Helmholtz
Mapper

## Slide 6: Magnetic field integrals of magnet model
„Virtual“ measurements of transverse dependence of field integrals of magnet model vs stretched wire measurements. Square magnet, 4 sides.

## Slide 7: Sorting results, phase shifter
+/-0.25Tmm * = 0.7Tmm errors
Additional mechanical mounting errors
Transverse dependence of field integral (Tmm)
0.1
-0.1

## Slide 8: Sorting results, phase shifter
~0.1Tmm by sorting, with further shimming (dashed) < 0.03Tmm
Poster K. Götze “Set-up, characterization and mitigation of cross-talk between PMbased and ferrite-enforced appliances for FLASH 2020”

## Slide 9: Hybrid magnetic structure. Modulator
Length = 2.5m
Period = 84mm
Min. gap = 9mm
Bmax = 1.8T
K = 12.9

## Slide 10: Modulator
Short undulator model with error magnet to get signatures
8 sets: top/bottom, pos/neg, flipped/nonflipped

## Slide 11: Sorting results, modulator, before tuning
Within the specs without any poletuning
Additional girder curvature spoiled phase error
K
Phase
Trajectory horizontal
Trajectory vertical
K & Phase error gap dependence

## Slide 12: Modulator, after tuning
Sorting of magnets reduces amount of poletuning
0.5deg RMS phase error tuned at minimum gap
Girder shape strikes back at intermediate gaps due to different gap dep.
K
Phase
X, m
X, mm
Gap, mm
Trajectory
Phase error
K & Phase error gap dependence

## Slide 13: Hall mapper
Sensor | TMAG5273
Range | ±130/260mT
Sensor resolution | 8uT / 16 bit; ADC 12bit / 20kHz + oversampling
Noise | Bx/By:23uT, Bz:17uT RMS @ 100 frames/s Bx/By:2.3uT, Bz:1.8uT RMS @ 1 frame/s
Linearity | Calibrated with NMR
Sensor array | 24 x 24 = 576
Sensor pitch | 3.2mm
Sensitive area | 73.6 x 73.6mm
Readout | ~10ms, up to 100frames/sec 2.5ms sampling + 7ms readout
PC interface | USB 2.0 HS, bus-powered.

## Slide 14: TMAG5273
3D magnetic field sensor, 3x3mm SOT23-6
±40/80 or ±130/260mT range
I2C serial interface

## Slide 15: I2C
I2C allows addressing and bus sharing, but only 7bit <127 devices
Not much pins in SOT23-6 to set individual addresses at power-up

## Slide 16: Row/column
Separate SCL/SDA in rows/columns
2N pins required for NxN array
Simplifies PCB layout

## Slide 17: Shift register
Daisy-chained shift registers 74xx595 / 74xx165
SPI interface to rule them all
7ms to readout of 24x24=576 “pixel” frame
FT232H USB->SPI

## Slide 18: 1.5mm pitch with TMAG3001 sensors
DSBGA-6 0.8mm×1.3mm
Field range of 260mT limits distance to magnet to 5-10mm

## Slide 19: Hall mapper
Fast measurements
Build model of magnet error distrbution
Virtual measurements derived from magnet model
Improves the sorting
Less magnetic shimming

## Slide 20: Thank you

## Slide 21: Pulsed wire

## Slide 22: Inverse pulsed wire
Propagation speed
sampling rate resolution
step sensitivity of field
speed sensitivity of field integral
acceleration sensitivity of second field integral
Noise floor spectal noise density rms voltage noise @ 1MHz BW

## Slide 23: ADAQ4003
ADC 18bit x 2Msps, RMS noise
Low noise preamplifier ADA4898 , 65MHz GBW
Gain 50 makes ADC input reffered noise below preamp & 1MHz bandwidth

## Slide 25: Inverse pulsed wire
Propagation speed
sampling rate resolution
step sensitivity of field
speed sensitivity of field integral
acceleration sensitivity of second field integral
Noise floor spectal noise density rms voltage noise @ 1MHz BW