## Slide 1: Towards the magnetic characterization of a meter-long bulk high-temperature superconducting undulator
Alexandre Arsenault :: Center for Photon Science :: Paul Scherrer Institute
Magnetic measurement workshop #23
October 11, 2024, Bad Zurzach
SLS2.0

## Slide 2: Overview
The HTS (REBCO) bulk Staggered Array undulator
Results on short samples
Status of the meter long HTS Undulator prototype
Conclusions

## Slide 3: Introduction
undulator
undulator
Brightness

## Slide 4: The new µ-Tomography beamline of SLS2.0
SmCo @300K
Nb3Sn @ 4.2K
NbTi @ 4.2K
PrFeB @77K
magnetic gap = 4mm

## Slide 5: Permanent Magnet Undulator with Fe poles
By
Permanent magnets
Fe poles
Undulator period
gap
Electrons

## Slide 6: Superconducting Staggered Array Undulator
time
T. Kii, et al.: Proc. FEL2006 (2006) p. 653.
Example of field cooling magnetisation
Time

## Slide 7: Example of Field Cooling (FC)

## Slide 8: Superconducting Staggered Array

## Slide 9: Superconducting Staggered Array

## Slide 10: Superconducting Staggered Array
e-
λu

## Slide 11: Overview
The HTS (REBCO) bulk Staggered Array undulator
Results on short samples
Status of the meter long HTS Undulator prototype
Conclusions

## Slide 12: Samples Overview
1st Bulk Sample
6mm gap
Bulk Industrial Sample
4mm gap
Bulk Simplified Sample
2nd Bulk Sample
4mm gap
2019
2023
The “Good” Sample
4mm gap
4mm gap
2021

## Slide 13: Hall sensor array
the solenoid
13
Calibrated 12 Hall sensors in a PPMS from 4-20 K and from 0-3 T
Difference of <0.8 % between sensors

## Slide 14: Hall sensor array
5 Hall sensors embedded in 3D printed holder
3 offset sensors to measure the undulator field
2 others to measure the perpendicular fields

## Slide 15
±12T
the solenoid
15

## Slide 16
±12T
the solenoid
16

## Slide 17: Planar Hybrid: CAN-SUPERCONDUCTOR

## Slide 18: Planar Hybrid: CAN-SUPERCONDUCTOR

## Slide 19: Overview
The HTS (REBCO) bulk Staggered Array undulator
Results on short samples
Status of the meter long HTS Undulator prototype
Conclusions

## Slide 20
Active length : 1.0 m
Total length : < 2m
period length : 10.5 mm
magnetic gap : 4.5 mm
B0 ∼ 1.8 T
Cryocoolers
HTS Mag-temp 10K
LTS temp 4.0K
20
THE METER LONG PROTOTYPE

## Slide 22: Cooling scheme

## Slide 23: Horizontal measurement bench

## Slide 24: Horizontal measurement bench

## Slide 25: Horizontal measurement bench
Tested the sealing of the vacuum insert with an O-ring
Vacuum remains stable, but the cryogenics are also a concern
Motor
Vacuum chamber
Linear table
Connection to pump
Sealing O-Ring

## Slide 26: Conclusions & outlooks
We demonstrated high magnetic field in a short sample staggered array undulator made of GdBCO bulks high temperature superconductors.
With 5 Hall probes, we were able to measure the undulator field vertically in the short sample
We are now working on the measurement bench for the meter-long undulator, expected to arrive in early 2025

## Slide 27: Acknowledgements
PSI : M. Calvi, K.Zhang, X.Liang, S.Hellmann, Th.Schmidt, L.Huber, S.Reiche, M.Bartkowiak, C.Calzolaio, Prof. M. Stampanoni, Prof L.Patthey, F. Marone & G.Lovric
CHART : Prof. H.R.Ott & Prof. L.Rivkin
Uni Cambridge : J.Durrell, A.Dennis, Y. Shi
King's College London: M.Ainslie
ESRF : G. Le Bec
Spring8 : T.Ishikawa, M.Yabashi, H.Tanaka
UniKyoto : R.Kinjo, T.Kii, H.Ohgaki
Uni Malta : N.Sammut, A.Sammut, J.Cassar
SENIS : Prof.R.Popovic, S.Spasic, S.Dimitrijevic
KIT : Prof. M.Noe
Fermilab: C.Boffo, M.Turenne, F.McConologue, V.Martinez, J.Hayman

## Slide 28: Planar Hybrid: Nippon Steel
B0-µ ∝ lnt
∝ 1-exp[-t/𝜏]
𝜏=2.2days
µ≃1