## Slide 1
Soren Prestemon
US Magnet Development Program
Lawrence Berkeley National Laboratory
On behalf of the US MDP Collaboration
US MD Program - Road Map & Test Infrastructures

## Slide 2: Outline
The US Magnet Development Program – status of updated roadmap following P5
The MDP Nb3Sn magnet program
The MDP HTS program
  Bi2212 magnet developments
  REBCO magnet developments
Test facility needs
Infrastructure investments underway

## Slide 3: Our program has been reviewed and revised to align with P5 recommendations
Improve integration for hybrid magnets
Investigate HEP-motivated solenoid designs
Strengthen linkage between technologies and magnets
Align with, and support, collider design efforts
Central focus: develop and test high field magnets for HEP
Support magnets with critical materials, expertise & dev. of new enabling technologies
Forward looking – what is enabled by our advances, and what is achievable for colliders
Further build collaborations, leverage synergies with fusion and with the NHMFL

## Slide 4: A key early MDP result was the 14.5T “MDPCT1” dipole
FNAL 14.5T “MDPCT1”
Bottura, Prestemon, Rossi, & Zlobin, Front. Phys., 12 October 2022
I
II
III
MDP Perspective:
[I]: Highest priority issue: degradation mechanisms; design mitigation
[II]: Second priority: Initial quench current and memory after thermal cycle
[III]: Third priority: Training rate

## Slide 5: A priority now is to build the Nb3Sn outserts
Canted Cosine theta:
  4 layers
    Bore field of ~12 T / 13 T for standalone operation
    Bore diameter: 120 mm
Stress-managed Cosine Theta:
  2 layers
    Bore field of ~12 T
    Bore diameter: 120mm
30+ % current margin at target fields of 12 T, 4.2 K and 13 T, 1.9 K
SMCT
CCT
These are two variants on stress-management
CCT is a “limiting case” of maximal SM
SMCT is a more efficient design

## Slide 6: Assembly steps for the SMCT mirror test
Sasha Zlobin => Igor Novitski

## Slide 7: Stress managed cos-theta development is progressing
First mirror test performed
Zlobin et al., IPAC’24

## Slide 8: SMCT mirror test demonstrated concept Next: SMCTD1 - fabrication of coils and impregnation with Telene
Trained to >90% ISS in 2-layer SMCT mode
Training limited by inner (CT) coils in 4-layer mode
No degradation apparent from test, but poor memory
Plan:
  New SMCT coils, impreg with Telene
  Test envisioned mid 2026

## Slide 9: Subscale magnets are used to evaluate impregnation materials – the return of Paraffin Wax!
    Daly et al 2022 ,SUST 35 055014
    D. Arbelaez, IEEE TAS, Vol. 32, No. 6, Sep. 2022, 4003207.
    D Arbelaez et al., SUST, 37 065015, 2024
    E. Barzi et al 2024 SUST. 37 045008
Very promising – is it a lasting breakthrough?
Diego Arbelaez
Subscale CCT’s built with Paraffin wax (sub-6), then filled-wax (sub-7)
Subscale with Telene is being fabricated

## Slide 10: Need to demonstrate technology at relevant stress levels
Practice winding of CCT6
✔️
✔️
Under fabrication at LBNL; test planned at FNAL in late April
“Flagship” ~14T large bore dipole construction beginning; highly relevant to muon collider storage ring and FCC-hh
Stress on Turn from Lorentz Force
CCT5w coils completed

## Slide 11: Recent progress on Bi2212 focused on conductor development, effects of cabling, and insulation
Series produced 2-kg billets yield regressed performance.
Scaled up 10-kg billets have lower performance than 2-kg billets.
Lack of understanding why and how.
Dedicated project:
“Enhancing Domestic Production of High Temperature Superconducting Bi2Sr2CaCu2Ox/Ag wires for High Field Magnets“
Tengming Shen
Champion
Now
(Data by Jianyi Jiang, NHMFL)

## Slide 12: Effects of Rutherford cabling under investigation

## Slide 13: Insulation of Bi2212 cables being tackled on multiple fronts
Dedicated pure alumina braid insulation system (ASC)
Al2O3 slurry process
CCT ARDAP coil BIN5E:
  Inner and outer layer coils wound. No electrical shorts.
  NEW: Use Al2O3 slurry to “repair, reinforce and lubricate” alumina fibers. (courtesy of Dr. Jun Lu, NHMFL)

## Slide 14: C3 is a 6-layer CCT magnet using CORC conductor
Xiaorong Wang
145 m of CORC® wires in six pieces, maximum piece length 35 m
Specified the minimum tape Ic for HM tapes

## Slide 15: C3 achieved 5.2T => major goal of the 2020 MDP roadmap
First test successfully completed – decision to limit to 10 micro-volt/layer
Second test campaign in coming months
  Will include magnetic measurements
  Push to higher field (higher voltage)
Strain measured via distributed optical fiber – fibers in each layer, all worked well throughout test (Linqing Luo, LBNL)

## Slide 16: COMB concept yielding results
COMB-STAR-1 magnet (2023-24) Achieved 1.5 T bore field @ 3.3 kA in LHe
  Degradation in one coil explored vi micro-CT scan
Vadim Kashikhin

## Slide 17: Designs for the next STAR and CORC COMB magnets are progressing
STAR™ allows for smaller bend radius => 60mm bore, 6 layers, may consider grading
CORC™ allows higher current but limited bending => ~97mm bore, 2 layers
STAR wire: 12 layers of AMPEER tape, 1 tape/layer; wire OD 2.6mm
CORC: 24 Superpower HM tapes, 2 tapes/layer; wire OD 3.8mm
4.8T bore field with 120mm OD

## Slide 18: Major push now is to integrate HTS and LTS in hybrid magnets
Paolo Ferracin
Tentative – dates still being revised

## Slide 19: Test facility needs for MDP Roadmap
Large-bore Nb3Sn dipoles will utilize large diameter “Utility Structure”
  Need test cryostats with ~1m diameter
  Large stored energy => requisite dump resistors
  Accommodate CLIQ, heaters, other protection methodologies
Hybrid magnets will require independent power and energy extraction systems
  Preferably use IGBTs for fast switching
  Ample current for each (preferably >16kA)
  Energy extractions should accommodate different dump resistor values
  Want both 4.5K and 1.9K capability within MDP
For development magnets (e.g. subscale)
  Need high current
  Need to accommodate very low inductance (low stored energy)
  Need fast energy extraction (high Jcu)
Planned: 860mm OD compatible with LBNL cryostat and future FNAL HFMTF

## Slide 20: Magnet R&D testing must accommodate new instrumentation
Continued diagnostics & instrumentation developments challenge test facilities
  Many issues unique to magnet R&D:
    New diagnostics require adapting wiring / ports
    New protections schemes require integration and commissioning
    Magnet test plans are challenged to leverage diagnostics feedback
  Example: power cryo-electronics offer new opportunities, but may pose difficulties:
    Integration into existing systems
    Validation, fault scenario evaluations, safety reviews, etc
E. Ravaioli, CERN MSC Seminar

## Slide 21: Facilities within MDP, and upgrade paths
BNL:
  Already demonstrated hybrid magnet testing capabilities (1.9K)
    10T common coil + independent powering of insert coils
    Independent IGBT switching and energy extraction
    Recently upgraded to >10kA + 20kA (?) for insert and outsert powering
LBNL:
  Hybrid capability recently developed (4.2K)
    First test using insert cable in a ~8.5T “outsert” dipole completed
    Independent IGBT switching and energy extraction
    Insert currently limited to ~7.2kA; further upgrade planned
FNAL:
  Hybrid capability being developed as part of joint HEP-FES Cable Test Facility project
  Will have independent IGBT switching and energy extraction
  Current >20kA for both insert and outsert
  Large bore cryostat (~1.2m) with 1.9K capability
George Velev

## Slide 22: LBNL Test Facility Advances
IGBT temp & flow monitoring and interlock
IGBT bus bars
cRIO PS control, quench detection, DAQ
Reed Teyber

## Slide 23: BNL facility advances
Mithlesh Kumar

## Slide 24: Thank you!

## Slide 25: The US MDP currently pursues research addressing a– critical – subset of the magnet needs for a future FCC hadron collider
Current MDP is highly relevant
xx T

## Slide 26: A muon collider will require critical advances in magnet technology – ripe for synergies with other applications
Radiation is a major consideration:
  Study tradeoff in aperture/bore+shielding vs magnet radiation hardness
  Further advance understanding of radiation hardness of superconductors and magnet materials
Rapid acceleration is critical:
  Study fixed-field booster options where applicable
  Further investigate high dB/dt magnet concepts
  Evaluate acceleration (particularly low-energy) schemes in an integrated approach
Large thermal loads suggest higher-temperature operation
  Explore all-HTS option
  Explore facility and operational cost models
Leverage strong synergies with fusion and High-Field magnets (e.g. condensed matter):
  Fastest development path for very challenging target and cooling magnets
New P5-aligned MDP roadmap focuses on these areas

## Slide 27: Central themes of MDP magnet R&D
Understanding the disturbance spectrum and its control
  Study training, operating margin, and means to mitigate/reduce
Develop stress-management concepts to enable high-field accelerator magnets with strain-sensitive materials (Nb3Sn, HTS)
Develop and demonstrate REBCO and Bi2212 magnet technologies
Explore the viability of hybrid HTS/LTS magnets for efficient high-field accelerator magnets
Work with industry to advance superconductors tailored to HEP needs
Use fast turn-around platforms (subscale magnets, mirror magnets, etc)
Develop and apply advanced diagnostics, modeling
Explore “Quench Current-boosting”, high-Cp concepts, etc.
Focus on developing conductor / cable / coil / magnet processes, identifying key issues
Leverage elements above to design optimized high-field configurations
Longstanding nexus between Labs, Universities, and industry in the US
  Example: Annual Low Temperature Superconductor Workshop >40+ years!

## Slide 28: Managing mechanical stresses is key to higher fields – exploring stress-managed structures
HTS insert
Nb3Sn outsert
MDP stress-managed hybrid magnets are under development
Critical for strain sensitive Nb3Sn & HTS conductors
Characterized by significant interfaces
“Traditional” Cos-theta
- Midplane stress due to azimuthal force accumulation
“Stress-managed” Cos-theta
- Groups of turns, azimuthal forces intercepted by support
Serves as good candidate for muon collider ring dipole
These “stress-managed” structures may enable combined function high-field accelerator magnets, which are subject to complex force distributions

## Slide 29: Strong synergies with Fusion REBCO research are leveraged
A two layer Cable Model Coil to test for cyclic degradation
No sign of degradation seen in high field & low-cycle fatigue testing - IC>80% sum of tapes
Demonstrate feasibility of direct dry wound (non-VPI) coil design
DOE Offices of HEP & FES jointly funding a large-bore cable test facility
Will provide 15T dipole field over 750mm good-field, 1.9-50K on-sample
Cryostat will enable testing of high-field hybrid magnets
Being located at FNAL

## Slide 30: Bi2212 shows strong promise – being readied for hybrids
CCT6-Bi-CCT1
ID 40mm
OD 95mm
SSL 5T
17-strand
0.8mm diameter
3 coils at FSU, ready for reaction
CCT6-Bi-CCT2
ID 40mm
OD 115mm
SSL 6.8T
23-strand
1.0mm diameter
Renegade furnace

## Slide 31: New paradigms: quench-free HTS magnet designs?
Traditional superconducting magnet design ensures magnet can survive quenches
  Motivation:
    spontaneous quenches => lack of reliable precursor, not controllable
    Training => potential for improved performance after quenching
Design to eliminate run-away quenching !?
Can we contemplate a new paradigm for HTS?
Higher MQE => not (?) susceptible to spontaneous quenches => no “random” behavior
So far no indication that HTS magnets exhibit training => no performance enhancement
T. Shen et al., PHYS. REV. ACCEL. BEAMS 25, 122401 (2022)
“Typical” Nb3Sn CCT magnet training
Sub 2/3 thermal cycle
“Rapid” training to ~75% short-sample, then rate changes
“Fair” memory after thermal cycle

## Slide 32: New paradigms: Liquid hydrogen cooled collider?
Hydrogen has critical advantages:
  Plentiful => not supply limited
  Carnot + liquefaction efficiency => dramatic improvement in ”wall-plug efficiency”
  Strong investments from other societal uses => cost, storage/shipping evolving rapidly
But there are concerns/issues:
  Safety => highly combustible in presence of oxygen
  Materials compatibility => some restrictions due to embrittlement/corrosion
  Limits superconductor option => only REBCO maintains significant transport current at 20K
Sustainability will be a driving consideration in any future international physics experiment - our community needs to make a strong, dedicated effort to explore liquid hydrogen for future colliders

## Slide 33: DOE-OHEP has an excellent record of developing advanced technology
Long term investments in general accelerator R&D set the stage for dedicated readiness programs, which in turn enable successful delivery of advanced technology for colliders
The programs strive to coordinate efforts to more rapidly advance technology development
The US DOE approach balances long-range R&D and project preparation
(ex: US MDP)
(ex: LARP)
(ex: HL-LHC AUP)
General R&D - programmatic
Directed R&D
(Technology readiness)
Project
Directed R&D
(Technology readiness)
Project

## Slide 34: Nb3Sn accelerator magnet technology is - for the 1st time - being installed in a collider
S. Prestemon, Workshop on Advanced Superconducting Materials and Magnets, KEK January 22 2019
S. Prestemon, Workshop on Advanced Superconducting Materials and Magnets, KEK January 22 2019
HiLumi magnet production is arguably “boutique production”
First implementation of Nb3Sn superconductor in a collider
What are the risks and benefits of full-scale industrial production of Nb3Sn magnets?
What elements of the design are “robust”, and what elements generate risk/performance limitations?
There is significant value-engineering that can be performed