## Slide 1: JORDI, a test stand for high-current conductors and coil windings
SMTF Workshop
02/04/2025
Nikolay Bykovskiy

## Slide 2: Who is JORDI?
The KA-III cryoplant at EPFL SPC can supply supercritical helium at 10 bar, 4.5 K, 10 g/s
It has 4 ports to serve different ‘experiments’:

## Slide 3: JORDI for JOint Resistance DIstribution
Original study on the inter-strand resistance in cable-in-conduit conductors:
10 kA power supply, pair of actively cooled copper current leads
Helium bath cooling with automated refill
Thermal shield cooled separately by 80 K outlet of the cryoplant
https://doi.org/10.1109/TASC.2004.830653

## Slide 4: HTS currents leads
WEKA
CRPP
https://doi.org/10.1109/TASC.2013.2281121
Connections to cryoplant and recovery line
New sample holder providing closed-loop helium circulation
Thermal shield cooled in parallel by 4 K circuit (80 K circuit no longer available)
Current leads and sample cooled by low pressure helium (i.e. placed after JT valves)

## Slide 5: Quench study
https://doi.org/10.1016/j.cryogenics.2015.07.003

## Slide 6: Current status
JORDI offers large test volume for variety of high-current samples by:
Single cooling circuit (~6 K helium inlet at 10 bar)
10 kA / 2 V power supply
Two sample holders – helium bath and closed-loop circulation
Next samples:
Superconducting switches for quench protection (Nb-Ti, MgB2)
Transformer and flux-pump (Nb3Sn)
Sub-size coils for VNS (ReBCO)
…
Each one calling for certain upgrades…

## Slide 7: Superconducting switches
Need for mass flow measurements and keeping helium at high pressure, thus:
Orifice flow meter installed
JT valve placed near the exit
+ active cooling of HTS section of the leads
Connections to cryoplant and recovery line
Helium flow
Thermally activated switch by non-inductive 12-wire Nb-Ti winding

## Slide 8: Superconducting switches
Rough agreement (within ~10%) between calibration used in SULTAN (function of dp, P and T) and calorimetric assessment of mass flow (ratio between heating power and enthalpy change)
However, Tmin ~5.7 K only by reducing pressure to 5 bar
So far, only ~2.5 kA operation achieved. Operation in LHe bath should increase Iop by a factor 2-3.
Current discharge of the 10 kA PS is relatively slow, but it was nearly instantaneous due to fast switching of the sample to the normal state.
MgB2 switch aimed at 10 kA nominal operation and ~0.3 Ohm at 40 K off-state to be tested.

## Slide 9: Transformer and flux-pump
SC transformer using Nb3Sn wires:
Possible operation at elevated temperatures due to high jc, which is only ~10% lower at 6 K than at 4.5 K for Nb3Sn at 5 T (compared to ~60% for Nb-Ti)
Design and construction of the demonstrator rated at ~100 kA is on-going…
To be equipped with a set of switches to enable rectifier operation (e.g. fluxpump)
 Need for AC current source and quench protection of the primary coil

## Slide 10: Transformer and flux-pump
Control system to be implemented for:
1 kA circuit breaker and dump resistor
AC power supply (±500 A / ±20 V):

## Slide 11: Sub-size coils for VNS tokamak
Feasibility study on using HTS for the ‘in-situ’ wound TF coils of VNS planned to be carried out in JORDI
Indirectly cooled HTS conductor
Co-wound steel strip with embedded quench detection
TF winding pack (in-situ winding)

## Slide 12: Sub-size coils for VNS: step 1
Double pancake HTS coil:
~70 m long LASSO cable using varying number of tapes along the length (18 to 14)
Pancake transition by a splice made of copper strip soldered to cable terminals
Cooling pipe placed between the pancakes
Quench detection by a co-wound instrumentation strip containing SQD wires, thermocouple arrays and optical fibers
Laminated stacked-tape soldered conductor (LASSO)
Co-wound strip for quench detection and turn insulation

## Slide 13: Sub-size coils for VNS: step 2
Quench protection by external energy dump using 10 kA circuit breaker (procured from Secheron) and dump resistor to be implemented in JORDI
Protection by SC switches as an alternative?
Sample design parameters:
400 mm bore, 400 mm tall, 100 mm thick winding
Operation ~10 kA, current density ~190 A/mm2
Central field ~15 T, energy ~10 MJ, L ~0.2 H
LASSO conductor ~1.3 km long in 16 single pancakes
Total length of 4 mm tape ~23 km

## Slide 14: Conclusion
The JORDI test stand is being upgraded to meet various demands for high-current testing of superconducting cables, switches, transformers and coils.
Cooling by helium bath (~1 bar) or helium forced flow (~10 bar).
Thank you for your attention and let us know if you are interested to test in JORDI!