## Slide 1: HTS quench detection using optical fibers, SQD wires and thermocouple arrays
IDSM Workshop
03/04/2025
Nikolay Bykovskiy

## Slide 2
https://doi.org/10.1051/jphyscol:19841130

## Slide 3: Introduction
QD methods studied at EPFL-SPC in the context of fusion magnets:
Superconducting quench detection (SQD) wires
Thermocouple chain (TC)
Optical fibers
 Aiming at temperature-based response immune to:
electromagnetic noise (challenging for SQD and TC)
mechanical strain (challenging for optical fibers)

## Slide 4: SQD
Thermal coupling
V
SQD twisted pair
Coil winding
I2
 measuring resistance of insulated thermally-coupled SC wire:
Distributed spatial sensing
Sensitivity controlled by I2 and wire off-state resistance
Twisted-pair SQD allows eliminating inductive noise and necessity of electrical contact with the main winding (no HV penetration!).
SQD practically immune to mechanical strain
of SQD wire conductor Tq Tq of LTS conductors ~ Tc (i.e. ~10 K) Tq of HTS conductors?

## Slide 5: SQD: quench temperature of HTS conductors?
Tq determines balance between cooling and Joule heating
SULTAN QE samples

## Slide 6: SQD: testing on sub-size fusion conductors

## Slide 7: Thermocouple chain
 measuring voltage over series connected thermocouple wires:
Continuous response on T gradient among joints
Immune to EM noise by using shielding sleeve
Varying sensitivity due to discrete sensing
Conventional thermocouple: response on ΔT only at the ends
Array of thermocouple wires connected in series: response on ΔT along the length
sense point
ref point
V

## Slide 8: Optical fibers
 measuring spectral shift of light reflected by each FBG:
Continuous temperature monitoring at each FBG location
Decoupled mechanically by Teflon tubing
Brittle; high spatial resolution over long length is cumbersome
FBG studied by Hugo Bajas at SPC till mid-2024
SPC samples in 2025 will include bare fibers for Distributed Fiber Optic Sensing (DFOS) using:
Rayleigh OFDR by ENEA: Spatial resolution ~5 mm, Rate ~100 Hz, Range ~0.1 km
Sensitivity decreasing at low temperature
https://doi.org/10.1109/ TASC.2025.3532931
Brillouin OFDA by University of Campania: Spatial resolution ~10 mm, Rate ~10 Hz, Range ~0.3 km
Closed-loop sensing
Sensitivity increasing at low temperature (!)
https://doi.org/10.1109/ SAS60918.2024.10636574

## Slide 9: Test sample – LASSO coil
20-turn flat racetrack
Fiberglass turn insulation
Impregnated and indirectly cooled
~13% DMSO (common cryoprotective agent)
Steel casing (2 welded U-shapes, 4 mm thick)
142 mm
92 mm
Inlet cooling (supercritical helium)
Laminated stacked-tape soldered conductor (LASSO)
Twisted-pair Nb3Sn 0.2 mm, acrylate insulation
Type K 0.2 mm, ~60 joints, wrapped copper shield
48 FBGs in 0.6 mm Teflon tubing in 4 paths:
(1)
(2)
(3)

## Slide 10: Detection response
~70 K
6 kA
SQD
FBG
TC
~15 K
Quench by embedded heater
Quench by overcurrent
~85 K
8 kA
SQD
FBG
TC
~20 K
Limited quench testing due to steel casing cracked by EM load ~1200 kN/m (at 8.3 kA, 7.2 T) during DC testing…
New sample needed to address numerous test issues: fracture of steel structure, arcing to ground, SULTAN false-positive quench triggers, damage of the coil terminal and optical feedthroughs…

## Slide 11: Nb3Sn coil: recycle of the instrumentation plate
Flat racetrack coil using MQXF conductor (thanks D. Araujo for the coil winding!)
Protection by high-current diodes (~10 V discharge)
Laser-welded steel structure
~50 K
10 kA
SQD
TC
FBG
4 V
~8 K
QD response delayed by a fraction of second
Current cannot be maintained by PS due to coil becoming resistive too fast…

## Slide 12: New tooling for QD sensors
Twisted-pair with back-twist pay-off (SQD)
Small braiding machine for insulation (SQD and TC) and shielding (TC)
Optical fiber reinforced by copper braid
data by H. Bajas

## Slide 13: Future plans
Co-wound strip for quench detection and turn insulation:
Co-wound strip can also provide mechanical reinforcement:
Reel-to-reel epoxy filling
 SQD, TC and optical fibers will be embedded in the two new samples as a co-wound strip:
LASSO double pancake
LASSO racetrack

## Slide 14: Conclusion
SQD wires, thermocouple chain and optical fibers offer promising ways for the temperature-based quench detection uncoupled from EM noise and mechanical strain.
Practical way of their integration is being developed, next attempt is focused on a co-wound strip.
The remaining issues are:
SQD: industrial availability of specific layouts
TC: long-length manufacturing, varying sensitivity
Optical fibers: optimal sensing method? increasing complexity for large magnets?
THANK YOU FOR YOU ATTENTION!