## Slide 1: Status of the EDIPO2 Test Facility
X. Sarasola,
P. Bruzzone,
N. Bykovskiy,
J. Greenwood, M. Jenni,
C. Müller, T. Nes, K. Sedlak
April 2nd, 2025

## Slide 2: Where do we come from?
SULTAN test facility:
  Bmax = 10.9 T in test well
  Homogeneity (2%) along ~400 mm
SULTAN has been pivotal in qualifying forced-flow conductors in the last three decades
  ITER
  DTT
  EU-DEMO
  JT60-SA
Nov 2024
  SPARC
  BEST
  CFETR
  …
ITER CS
ITER TF
DEMO TF
JT60-SA CS and EF

## Slide 3: Where do we come from?
The EDIPO test facility was built to complement and upgrade SULTAN
In May 2016, the magnet of EDIPO was damaged by the malicious manipulation of the quench detection software
Unfortunately, the magnet cannot be repaired
The rest of the test facility remains available
JT60-SA CS and EF

## Slide 4: Where do we go?
 | SULTAN (SPC) | EDIPO (SPC) | FRESCA2 (CERN) | EDIPO 2 | Units
Bcenter aperture | 10.9 | 12.35 | 13 (14.6) | 15 | T
Aperture size | 94×144 | 90×141 | Ø100 | 144×144 | mm
Homogeneous field length (1%) | 320 | 680 | 650 | 900 | mm
Sample current | ≤100 | ≤100 | ≤ 32 (50) | >100 | kA
Sample operating temperature | 4.5 to 50 | 4.5 to 50 | 1.9 & 4.2 | 4.5 to 50 | K
Rising demand towards:
  High current conductors (beyond 100 kA)
  Conductors for high field magnets (partly driven by the development of HTS)
EDIPO 2 will enhance the background B field and the aperture size while keeping attractive features from SULTAN and EDIPO
Since January 2025, a SNF Infrastructures grant funds the construction of EDIPO 2 (as part of the Swiss Fusion Hub)

## Slide 5: Conceptual design of the EDIPO 2 magnet
Dipole based on two pairs of planar racetrack coils:
  Bath cooled (4.2 K), high jeng winding pack (as opposed to SULTAN and EDIPO1)
  Operating current ≤ 18 kA (limited by existing power supply)
    It requires a large cross-section of superconductor
  There is no 3D transition in the coil ends:
    No hardway bending → Presumably no performance limitation in the ends region
    Simplifies manufacturing
    Simplifies management of mechanical stress

## Slide 6: EDIPO2 strand and cable design
Nb3Sn high-jc strand:
  jc,nc ≥ 2600 A/mm2 at 12 T and 4.2 K, 0.7 mm diam, Cu:nCu = 1.0
  ~110 kg delivered in Dec 2023 for prototype cabling
  1.6 tons of strand required for the production of the magnet:
    Adjudication of this call will be published in the coming days
Cable based on a flat two-stage design: 24×(6+1), 0.7 mm
  Cabling R&D activities in 2024 (copper dummy):
    Two industrial partners + CERN have been qualified to produce this cable
  Production of 150 m of Nb3Sn prototype cable + 500 m of insulated copper dummy:
    Contract signed in 2024
    Production expected by summer 2025

## Slide 7: Conceptual design of the EDIPO 2 magnet
Field generated by two sets of flat racetrack coils:
  Vertical coils: one pair of coils each made of 4 pancakes: 46 turns/pancake
  Side coils: one pair of coils each made of 6 pancakes: 16 turns/pancake

## Slide 8: Magnetostatic 3D analysis
 | Iop = 0.85×Iss | Iop = Imax | 
Cable layout | 24×(6+1), 0.7 mm diam |  | 
Number of turns | Side coils: 2×6×16 Vertical coils: 2×4×46 |  | 
Total number of turns, ntotal | 560 |  | 
Total area of insulated conductor | 52886 |  | mm2
Operating current, Iop | 17.40 (85%×Iss) | 18.00 (88.1%×Iss) | kA
B field in the center of the aperture, B0 | 15.00 | 15.46 | T
Peak B field in the coils, Bpeak | 15.04 | 15.51 | T
Total ampere-turns, Itotal | 9.74 | 10.08 | MAt
Total magnet stored energy, Etotal | 20.7 | 22.1 | MJ
Magnet self-inductance, L | 136.6 |  | mH
Engineering current density, jeng | 184.3 | 190.6 | A/mm2
Copper current density, jCu | 522.2 | 540.1 | A/mm2
B field in the magnet
B field in the winding pack
Iop = 0.85×Iss
https://doi.org/10.1109/TASC.2025.3526109

## Slide 9: Magnetostatic 3D analysis: field quality
Field quality is not a crucial design target
Uniformity along x and y axis: ±1%
Uniformity around a circumference of Rref = 40 mm: ±1%
Homogeneity along the z axis:
  1% drop of the field at z = ±0.450 m
  2% drop of the field at z = ±0.526 m
Uniformity along x and y axis
Uniformity around Rref = 40 mm

## Slide 10: 3D quench analysis
[W/m3]
t_detect
t_detect+t_d
1.8 kV
260 K
50 V
18 kA
Vmax = ±0.9 kV (assuming symmetric grounding)
Tmax = 260 K for the operation at 18 kA and Vth = 0.1 V detection threshold
Higher values of Vth highly undesirable, increasing Tmax above 300 K at 0.5 V
~98% of stored energy released in the dump resistor
Terminal-to-terminal voltage, kV
 56’000 nodes to evaluate heat propagation in 3-D (560 turns x 100 nodes per turn)
Protection scheme based exclusively on energy extraction:
  Assumed delay time: 100 ms

## Slide 11: Mechanical 3D analysis
Coils assembled in a steel casing
Lorentz forces reacted by the casing and a 30-mm-thick steel shell
ateral and axial pre-load on the vertical coils
The test well is stress-free during operation

## Slide 12: Mechanical 3D analysis
Coils assembled in a steel casing
Lorentz forces reacted by the casing and a 30-mm-thick steel shell
Lateral and axial pre-load on the vertical coils
The test well is stress-free during operation
Deformation during operation

## Slide 13: Mechanical 3D analysis
Stress is moderate after cool-down
Remains below allowable limits during operation:
  Side coils:
    σeq ≤ 82 MPa
    εL ranging from -0.06 and +0.06%.
  Vertical coils:
    σeq ≤ 155 MPa (at low field regions, B ≤ 6 T)
    εL ranging from -0.2 and +0.29%
Vertical coils at B = 15 T
Stress in the coils at B = 15 T
Side coils at B = 15 T
https://doi.org/10.1109/TASC.2025.3526109

## Slide 14: Magnet R&D activities
Magnet R&D activities to de-risk technologies associated with the EDIPO2 coil design:
  Contract will be signed with a qualified industry in the coming weeks
Cable and subscale coil tests planned in SULTAN in 2025-2026:
  Nb3Sn cable and joints
  Subscale coils (pancake transitions and detachable poles)

## Slide 15: Cooling / Cryogenics
EDIPO 1 was based on a CICC design (cooled by a forced-flow of supercritical He)
The EDIPO 2 magnet will be bath-cooled at 4.2 K
  Volume: ~50 l
New helium vessel. Three main parts:
  Bottom base (interface with the existing facility)
  Cylindrical body
  Lid (not final design)
Main parameters:
  Operating pressure: 1 bar
  Accident pressure: 3 bar
  Leak rate < 10-8 mbar·l/ s
https://doi.org/10.1016/j.cryogenics.2023.103648

## Slide 16: Cooling / Cryogenics
EDIPO 1 was based on a CICC design (cooled by a forced-flow of supercritical He)
The EDIPO 2 magnet will be bath-cooled at 4.2 K
  Volume: ~50 l
New helium vessel. Three main parts:
  Bottom base (interface with the existing facility)
  Cylindrical body
  Lid (not final design)
Main parameters:
  Operating pressure: 1 bar
  Accident pressure: 3 bar
  Leak rate < 10-8 mbar·l/ s
In case of quench or loss of vacuum, the evaporated He volume captured in a balloon
https://doi.org/10.1016/j.cryogenics.2023.103648

## Slide 17: Cooling / Cryogenics
Estimated thermal heat load
  Conduction: 2.4 W
  Radiation: 1.1 W
Joule heating from joints
  Assumed
    R=3 nΩ
    I=18 kA
    n=10
  P = 9.7 W
Total heat load at max current: ~13 W
https://doi.org/10.1016/j.cryogenics.2023.103648

## Slide 18: Modified cryogenic circuit (preliminary)

## Slide 19: Sample environment
EDIPO 2 keeps attractive features from SULTAN and EDIPO:
  Separate cryogenic environment for magnet and sample (quick sample change)
  Sample cooling by supercritical He at 10 bar
  Sample operating range:
    Current up to 120 kA (new superconducting trafo)
    Variable temperature between 4.5 to 50 K
    Mass flow up to 10 g/s at 4.5 K

## Slide 20: Conclusions and Outlook
EDIPO 2 will generate a background field of 15 T in a large aperture (144×144 mm2)
Use of a Nb3Sn two-stage cable design for high operating current
Dipole purely based on the use of planar racetrack coils:
  No hardway bending
  Simplification of the coil manufacturing
Cooling/cryogenics shall be modified (bath cooled at 4.2 K)
Outlook for 2025:
  Production of 150 m of Nb3Sn prototype cable (contract signed)
  New contracts with the industry:
    Procurement of 1.6 tons of Nb3Sn strand required for the magnet
    Technological coil R&D activities (including production of a prototype coil and test in SULTAN)
    Magnet manufacturing design

## Slide 21: We are hiring
EDIPO2 Postdoc
https://www.psi.ch/en/hr/job-opportunities/68766-postdoctoral-fellow-mechanical-engineer-superconducting-magnets-epfl
Join our team!

## Slide 22
Thanks for your attention!