## Slide 1: Introduction and Welcome EPFL-SPC
April 2, 2025
Kamil Sedlak

## Slide 2: SPC – the Largest Laboratory of EPFL in Lausanne

## Slide 3: Swiss Plasma Center was known as CRPP
1961
1968
Plasma Physics Laboratory (PPL) is created by Federal Council
PPL becomes “Centre de recherches en physique des plasmas” (CRPP)
1973
CRPP joins EPFL
1978
Agreement with Euratom
1989
Industrial
Plasma
Group
1992
TCV tokamak is built
2015
2002
CRPP is Center of the School of Basic Science
CRPP becomes SPC

## Slide 4: SPC Now Counts 200 Staff Members
Majority of SPC (180 people) works on plasma research in Lausanne.
20 people working on applied superconductivity is based at premises of PSI in Villigen.

## Slide 5: Research Lines of SPC
Tokamak Physics - TCV
Plasma Heating
  FALCON: testing of ITER Gyrotron components
  T-Rex: experiment to understand electron cloud formation
Theory
  Studies of core and boundary turbulences in plasma
  Plasma control
  Advanced modelling on powerful computing clusters
Low Temperature Plasma and Application
Applied Superconductivity
Chart: 
| Swiss | Italian | French | Belgian | British | German | Spanish | Russian | Chinese | American | Others
 | 75 | 40 | 21 | 7 | 7 | 7 | 6 | 5 | 4 | 3 | 30

## Slide 6: TCV: the Most Flexible Tokamak Worldwide
R=0.88 m
a=0.25 m
graphite walls
Rmajor = 0.9 m
Rminor = 0.25 m
Ip < 1 MA
BT < 1.54 T
2.3 MW NBI heating
3.75 MW ECRH
Independently powered
16 shaping coils
2 OH coils
1 internal vertical control coil
k < 3, -0.6 < d < 0.9
Graphite tiles
Internal divertor baffles
More than 40 international institutions participate in the TCV program

## Slide 7: Built-in Flexibility and Versatility of TCV Tokamak
Fasoli et al., Nucl. Fusion 2020

## Slide 8: Applied Superconductivity Group
Testing of superconductors for fusion magnets:
  Sample assembly (conductors and joints)
  Sample testing
Maintenance and upgrades of existing test facilities SULTAN, EDIPO and the smaller one JORDI.
R&D on fusion-size superconductors within EUROfusion programs:
  DEMO, VNS, stellarator
  Quench behaviour in HTS, fusion-relevant samples
  Quench detection based on non-voltage methods (optical fibers; co-wound superconducting strands; thermocouples)
Other collaborations, e.g. with Bruker Biospin and CERN

## Slide 9: Test Facilities

## Slide 10: SULTAN Test Facility – DC Field up to 10.9 T

## Slide 11: AC Loss Measurements in SULTAN
AC sinusoidal field:
  Frequency 0.2 – 10 Hz
  Max. field amplitude 0.4 T
Pulse mode:
  Pulse duration: 40 ms – 130 ms
  Amplitude: up to 4 T (130 ms) or up to 1.3 T (40 ms)
  Sinusoidal, trapezoidal, triangular
Effective field length: 390 mm
Re-cooling time after a test: a few minutes

## Slide 12: Tests in SULTAN
Possible use of the SULTAN/EDIPO test facilities:
Test of superconducting cables for fusion magnets (ITER, EU DEMO, CFS, BEST, CFETR, DTT, …) up to 85 kA.
Test of joints (fusion and accelerator cables).
Quench experiments (only up to 15 kA).
Test of sub-size accelerator coils (e.g. Feather HTS magnets for CERN).
 | SULTAN | EDIPO II
status | in operation | to be upgraded after accident
Matnetic field | 11 T | 15 T
Sample space | 94x144 mm2 | 144x144 mm2
Temperature | 4.5-50 K | 4.5-50 K

## Slide 13: Tests with Superconducting Transformer
Currents up to ~85 kA.
With a small resistance (a few nΩ) in the sample (due to the joints), the test duration can be up to an hour – very precise measurement of IC or TCS.
When the resistance is larger than a few nΩ, the test duration can get severely limited  also the measurement precision is reduced.
In case of quench  “high” resistance in the sample leads to an immediate current switch off.
  Measurements can be done until quench, and the quench evolution cannot be studied.
Typical tests: IC, TCS, effect of electromagnetic and thermal cycles on the sample performance, AC loss, MQE.

## Slide 14: Tests of HTS Samples Using the Transformer
Currents theoretically up to ~85 kA, in practice usually less due to higher overall resistance of the sample.
An HTS Adaptor must be inserted as an interface between the HTS sample and the superconducting transformer (made of NbTi). The adaptor made of HTS tapes can carry current up to 100 kA, but has a low heat conductivity  it allows us to keep the temperature of the terminals attached to the transformer low (<8 K), while the sample temperature can reach up to 50 K.
In addition, a recuperating heat exchanger preheats the cold helium (4.5 K) coming from the cryoplant to a higher temperature (up to 50 K), and at the same time pre-cools the warm helium coming from the sample to lower temperature manageable by the cryoplant.
Left – NTNT
Right – ASTRA
HTS adaptor
Field center
2555
790

## Slide 15: HTS Adaptor

## Slide 16: Tests with a Power Supply – Quench Studies
A sample holder replaces the transformer.
The current is provided by a direct power supply. It is limited to 15 kA.
The current can be maintained also in the resistive sample. Maximum voltage over the sample is a few V.
In the Quench experiments, temperature over 200 K could be reached, allowing us to study the quench evolution in HTS samples.
Cryogenic circuit
Sample holder with and without the thermal shield

## Slide 17: Variable Temperature Cryostat
Most of fusion conductors are forced-flow cooled, surrounded by vacuum in the SULTAN test well.
Occasionally, we test accelerator-type conductors (e.g. Rutherford cables or joints) or sub-scale coils (e.g. Feather M0.4 and M0.5, CERN), which need He coolant surrounding the sample.
 We use Variable Temperature Cryostat, with He gas inside.
Feather M0.4, M0.5

## Slide 18: R&D for Fusion Magnets

## Slide 19: React & Wind Nb3Sn Conductor for DEMO
1 mm
Post-ITER LTS conductor development
Cable assembled at room temperature from heat-treated Nb3Sn cable. Steel jacket laser welded from two symmetric half-profiles.
Measured effective strain:
  εeff = -0.28%
  (ITER TF: εeff ≈ -0.7%)
 DEMO RW conductor reaches ITER TF cable performance with only 50% of Nb3Sn.
Additional saving due to grading of Nb3Sn and steel in the layer-wound winding pack.
Very small AC loss (cable might be used also in the CS coil).
In 2025-2026: We work on an industrial demonstration of 100m long conductor manufacture.

## Slide 20: RW Diffusion-Bonded Joint
Diffusion-bonding (DB) of two overlapping RW conductors. The bonding is done after the Nb3Sn heat treatment.
In operating conditions :
R at 8 T, 63.3 kA = 0.54 nΩ
(Target: 1.0 nΩ)

## Slide 21: R&D on HTS Conductors
  NTNT – Non-Twisted Non-Transposed conductor, 2024
  SPC: 60 kA, B^12.5 T, 7.8 K, 2016
  The SPC conductor is transposed, scalable to 50-100 kA, designed for B^ > 12 T, AC tolerant, force flow.
  (Nikolay Bykovskiy)
Three stacks in the Cu profiles
He
  (Davide Uglietti)
Notes: Other conductor designs, e.g. Röbel based cables and CORC are still far from the threshold of 50kA / 12T

## Slide 22: ASTRA prototype construction & testing
3.3 mm tapes 21 tapes in a stack 8 x 4 mm copper profile
50 mm
26 mm
  Nikolay Bykovskiy, SPC, 2023
Designed for 60 kA at 18 T
Impregnation with dimethyl sulfoxide (DMSO) – water solution

## Slide 23: ASTRA full-size conductor 2023
Impregnated by DMSO 12%
Performance degradation of the ASTRA conductor, likely due to voids in the solder in between the tapes.
Overall observation for HTS samples tested in SULTAN from all the world:
Conductors are usually very stable against quench (as expected).
Making the terminations (joints) with low resistance is challenging.
Almost always there is a performance degradation with electromagnetic cycling. So far only Viper cable from CFS showed only negligible degradation. Other conductors degraded significantly.

## Slide 24: SPC Quench Samples
Full-scale layout:
Round soldered strands in copper-cored Rutherford layout
Aligned stacks transposed in Roebel arrangement (ASTRA)
Sub-size samples:
Features:
twisted stacks & strands
straight stacks & strands, perp. field
twisted stacks & strands, solder filled
twisted stacks & strands
straight stack & strand,
parr. field, indirect cooling
Ref
No-twist
Filled
BISCCO
ASTRA
ASTRA2
D36 mm
22 mm
30 mm
35 mm
24 mm
D36 mm
D36 mm
We reached Thot-spot around 200 K (sometimes leading to the conductor degradation)
Quench Propagation Velocity (QPV) in HTS samples is 10-100 mm/s (it confirms QPVHTS<< QPVLTS ~500-1000 mm/s)
Enhancing the thermal coupling between the cable and steel jacket is found to be important to avoid overheating, even though it decreases the QPV.

## Slide 25: Final Comments
SULTAN and EDIPO test facilities are key elements of applied superconductivity group of SPC.
We try to keep them up-to-date with maintenance, small updates and large upgrades.
  EDIPO upgrade to 15 T: 2025-2028
  Cryoplant upgrade to reduce electricity consumption: 5 months, starting towards the end of 2025.
The second largest activity is R&D on conductors & joints for fusion-size magnets, and related technologies (quench detection using optical fibers and SQD, superconducting switches, …)

## Slide 26: Guided Tour PSI & SPC

## Slide 27: Guided Tour Through PSI & SPC Labs
We will visit 4 stations at PSI:
SULTAN with Jack Greenwood and Mattia Ortino
Test stand WNLA/010 with Michal Duda and Quentin Gorit
Magnetic Measurement (MM) lab with Giuseppe Montenero and Rebecca Riccioli
CHART lab with Douglas Araujo Martins and Jaap Kosse
For the visit, we will split into 4 groups. Every group will visit every station.
Please inform your guides, if you have a heart implant. In this case you are not allowed to enter MM lab.
Notes: Nicht aktualisiert

## Slide 28: The Guides
Every group has a guide. The colour of your workshop badge will tell you to which group you belong.
Joep Leon
Van den Eijnden
Notes: Nicht aktualisiert

## Slide 29: Time Schedule of the Tours
14:20-14:45 Coffee Break in foyer Auditorium: Pick up your entrance badge and your headset in the foyer and check that it is working.
14:45 Go to your group guide
14:50 Walk to the first station
15:05-15:35 Station 1
15:45-16:15 Station 2
16:20-16:30 Break Water and Toilets
16:35-17:05 Station 3
17:15-17:45 Station 4
17:55 Bus stop PSI West return PSI Badge_Headset_Dosimeter to your guide
18:00 Bus transfer to Gala Dinner in Eglisau