## Slide 1: Low-energy mSR (LEM) applications
Thomas Prokscha
Muon Spectroscopy School 2026, Jan 14 – 21, Rigi-Kaltbad

## Slide 2: Outline
Low-energy (keV) muons (m+) basics
  The low-energy muon facility (apparatus & mSR spectrometer, LEM) at PSI
  Special features of low-energy mSR (LE-mSR) compared to standard mSR
  Implantation of low-energy m+ in matter – stopping Profiles
Applications of LE-mSR: thin films and interfaces
  Superconducting and magnetic properties at surfaces and interfaces
    Meissner screening, volume fractions, proximity effects
Summary
Appendix: Depth profiling of defect regions with nm resolution at technologically relevant semiconductor interfaces (Metal-Oxide-Semiconductor, solar cells)

## Slide 3: Generation of polarized epithermal (~eV) m+
~100 mm Ag
Using a proper moderator:
motivated by experiments for positron moderation, a solid film of a rare-gas should work!
Energy spectrum after a degrader
Solid line: muon energy spectrum
Solid circles: energy spectrum of muonium
T. Prokscha et al., Phys. Rev. A58, 3739 (1998).
„Surface“ Muons
~ 4 MeV
~ 100% polarized
muonium

## Slide 4: Generation of polarized epithermal (~eV) m+
~100 mm Ag
~500 nm
s-Ne, Ar,
s-N2
6 K
„Surface“ Muons
~ 4 MeV
~ 100% polarized
T. Prokscha et al., Appl. Surf. Sci. 172, 235 (2001).
T. Prokscha et al., Phys. Rev. A58, 3739 (1998).
E. Morenzoni et al., J. Appl. Phys. 81, 3340 (1997).
D. Harshmann et al., Phys. Rev. B36, 8850 (1987).

## Slide 5: Characteristics of epithermal (~eV) m+
 suppression of electronic energy loss for E > Eg, large band gap Eg (10-20 eV) „soft, perfect“ insulators
 large escape depth L (10-100 nm), no loss of polarization during moderation (~10 ps)
 moderation efficiency is low (requires highest intensities m+ beams, > 108 m+/s, i.e. MW proton beam):
DW: probability to escape into vacuum (~50% for isotropic angular distribution)
FMu: muonium formation probability, DR ~ 100 mm width of muon stopping distribution in moderator
+ = Nepith/N4MeV ≈ DW (1-FMu ) L/DR ≈ 0.25 L/DR ≈ 10-4 – 10-5
E. Morenzoni, F. Kottmann, D. Maden, B. Matthias, M. Meyberg, T. Prokscha, T. Wutzke, U. Zimmermann, PRL 72, 2793 (1994).
E. Morenzoni, T. Prokscha, A. Suter, H. Luetkens, R. Khasanov, J.Phys.: Cond. Matt. 16, S4583 (2004).
AP(t)
P(0) 1
L

## Slide 6: Low-energy m+ facility at PSI at the mE4 surface m+ beamline
- UHV system, 10-10 mbar
- some parts LN2 cooled
Polarized low-energy m+ Beam Energy: 1 - 30 keV DE, Dt: 400 eV, 5 ns Mean Depth: 5 – 200 nm Polarization ~90 % (surface m+) Beam Spot: 12 mm (FWHM)
~ 16’000 (24’000) LE-m+/s, s-Ar (s-Ne); accelerate up to 20 keV
~2.7 • 108 +/s
at sample: up to ~ 6’400 (9’600) m+/s, s-Ar (s-Ne)
Beam spot at sample
Spin-rotator (E x B)
Conical lens
Start detector
(10 nm C-foil)
Sample cryostat
e+ detectors
electrostatic mirror
Einzel lens
(LN2 cooled)
moderator
Einzel lens
(LN2 cooled)
mE4 “surface” m+ beam, ~4 MeV, ~90% polarization
Spin
Rates at 2.2 mA proton beam current (2025)

## Slide 7
At 2.2 mA proton current
~6.2 • 108 m+/s total, Dp/p = 9.5% (FWHM) ~2.7 • 108 m+/s on LEM moderator ~1.6/2.4 • 104 m+/s moderated (solid Ar/solid Ne)
T. Prokscha, E. Morenzoni, K. Deiters, F. Foroughi, D. George, R. Kobler, A. Suter and V. Vrankovic, Nucl. Instr. Meth. A595, 317 (2008).
Low-energy m+ facility at PSI at the mE4 surface m+ beamline
Notes: 7

## Slide 8: Low-energy μ+ beam and setup for LE-μSR
Muon Spin
Muon Momentum
Moderator low-energy μ+
source
Why re-accelerate slow µ+?
for E ≈ 10eV
No µ+ left

## Slide 9: Low-energy μ+ beam and setup for LE-μSR
Muon Spin
Muon Momentum
Mirror
energy filter
Un-moderated fast µ+
Moderated slow (keV) µ+

## Slide 10: Low-energy μ+ beam and setup for LE-μSR
Muon Spin
Muon Momentum
Spin-Rotator / Separator
E-Field
B-Field

## Slide 11: Low-energy μ+ beam and setup for LE-μSR
Muon Spin
Muon Momentum
Trigger
implantation time
Carbon foil:
≈ 1.5 - 2.5 µg/cm2
≈ 10 nm
K.S. Khaw et al., JINST 10, P10025 (2015)
G. Janka et al., Phys. Rev. AB 27, 054501 (2024)
1.7 mg/cm2

## Slide 12: Low-energy μ+ beam and setup for LE-μSR
Muon Spin
Muon Momentum
Trigger
implantation time
Carbon foil:
≈ 1.5 - 2.5 µg/cm2
≈ 10 nm
1.7 mg/cm2
2.6 mg/cm2
1.7 mg/cm2
G. Janka et al., Phys. Rev. AB 27, 054501 (2024)

## Slide 13: Low-energy μ+ beam and setup for LE-μSR
Muon Spin
Muon Momentum
Trigger
implantation time
Carbon foil:
≈ 1.5 - 2.5 µg/cm2
≈ 10 nm
1.7 mg/cm2
1.7 mg/cm2
2.6 mg/cm2
G. Janka et al., Phys. Rev. AB 27, 054501 (2024)

## Slide 14: Low-energy μ+ beam and setup for LE-μSR
Muon Spin
Muon Momentum
Carbon foil:
≈ 1.5 - 2.5 µg/cm2
≈ 10 nm
15 keV µ+
This energy loss distribution (= time-of-flight
distribution with width Dt) is limiting the
frequency resolution of LEM to ≤ 50 MHz
K.S. Khaw et al., JINST 10, P10025 (2015)
G. Janka et al., Phys. Rev. AB 27, 054501 (2024)
Trigger
implantation time
Trigger
implantation time
Dt

## Slide 15: Low-energy μ+ beam and setup for LE-μSR
Muon Spin
Muon Momentum
0.6m

## Slide 16: Low-energy μ+ beam and setup for LE-μSR, WEW magnet
0.6m

## Slide 17: LEM experiment geometries
Bperp - WEW
Bpar - AEW
µ+ beam
Side Half View
µ+ Spin In/Out-of-Plane WEW/AEW (TF/ZF)
Bperp
µ+ direction view
µ+ Spin anti-/parallel WEW (LF)
Upstream detectors
Downstream detectors

## Slide 18: LEM experiment geometries, rates, asymmetries
Bperp - WEW
Bpar - AEW
µ+ beam
Side Half View
Upstream detectors
Downstream detectors
LE-mSR parameter:
LEM rates (@ 2.2 mA proton current)
  WEW, ZF, TF: up to 2’600/sec, 9M/h (depending on beam transport energy)
  WEW, LF: up to 2’000/sec – 2’400/sec,7 – 8.6 M/h (depending on beam transport energy and spin direction: parallel/anti-parallel beam momentum)
  AEW, TF: up to 1’500/sec, 5.4 M/h)
Max. asymmetry:
  WEW/AEW ZF, TF: 0.24
  WEW/LF: 0.11
µ+ Spin In/Out-of-Plane WEW/AEW (TF/ZF)
µ+ Spin anti-/parallel WEW (LF)

## Slide 19
Special features of low-energy mSR (LE-mSR) compared to standard mSR

## Slide 20: t0 at a quasi continuous muon source – LEM
Where is the prompt peak, and hence the t0 TDC channel?
?
?
Positron Detector Assembly
Trigger or M-Counter

## Slide 21: t0 at a quasi continuous muon source – LEM
Where is the prompt peak, and hence the t0 TDC channel?
Positron Detector Assembly
Trigger or M-Counter
Positrons at about the speed of light
e+

## Slide 22: t0 at a Quasi Continuous Muon Source – LEM
Where is the prompt peak, and hence the t0 TDC channel?
Positron Detector Assembly
Trigger or M-Counter
e+
Mu
Positron
Mu

## Slide 23: t0 at a quasi continuous muon source – LEM
Positron Detector Assembly
Trigger or M-Counter
e+
Mu
Measure TOF with an MCP instead of Cryo

## Slide 24: How does the beam transport affect the LE-mSR spectra?
A. Suter et al., J. Phys.: Conf. Ser. 2462, 012011 (2023)
Observations for different muon transport energies («Tr=7.5,12,15kV»):
The first ~70 ns are severely distorted by the time-of-flight distribution  ignore this time window when fitting LEM data!
The asymmetry at 1 keV is smaller than the asymmetry at 13.6 keV  this is due to backscattering of muons at low implantation energies, where backscattered muons form Mu
The asymmetry at 7.5 keV beam transport energy is reduced due to a higher Mu formation probability at the carbon foil of the trigger detector/M-counter
These effects – absent in standard mSR – must be taken into account when analyzing LEM data, e.g. calculating volume fractions
Ag sample
ZF
TF 10 mT

## Slide 25: How does the beam transport affect the LE-mSR spectra?
A. Suter et al., J. Phys.: Conf. Ser. 2462, 012011 (2023)
Observations for different muon transport energies («Tr=7.5,12,15kV»):
The first ~70 ns are severely distorted by the time-of-flight distribution  ignore this time window when fitting LEM data!
The asymmetry at 1 keV is smaller than the asymmetry at 13.6 keV  this is due to backscattering of muons at low implantation energies, where backscattered muons form Mu
The asymmetry at 7.5 keV beam transport energy is reduced due to a higher Mu formation probability at the carbon foil of the trigger detector/M-counter
These effects – absent in standard mSR – must be taken into account when analyzing LEM data, e.g. calculating volume fractions
Ag sample
ZF
TF 10 mT
Ferromagnetic Ni, ZF

## Slide 26: How does the beam transport affect the LE-mSR spectra?
Observations for different muon transport energies («Tr=7.5,12,15kV»):
The first ~70 ns are severely distorted by the time-of-flight distribution  ignore this time window when fitting LEM data!
The asymmetry at 1 keV is smaller than the asymmetry at 13.6 keV  this is due to backscattering of muons at low implantation energies, where backscattered muons form Mu
The asymmetry at lower beam transport energy is reduced due to a higher Mu formation probability at the carbon foil of the trigger detector/M-counter
Increase of depolarization rate below 2 keV: beam reflection!
Unpublished LEM data, LEM group (2023)
Ag sample

## Slide 27: How does the beam transport affect the LE-mSR spectra?
Muon beam reflection at low implantation energies
Origin is the large, decelarating electric field in front of the sample plate, as also demonstrated by musrSim/Geant 4 simulations
In TF-mSR in a ferromagnetic Ni layer, the asymmetry increases below ~3 keV. This is due to reflected m+ stopping in the non-magnetic radiation shield of the cryostat – and not due to an increase in non-magnetic volume fraction
Magenta: m+
Blue: e+
Suter et al., J. Phys.: Conf. Ser. 2462, 012011 (2023)
musrSim: K. Sedlak et al., Phys. Proc. 30, 61 (2012)
Ferromagnetic Ni, TF 10 mT

## Slide 28: LEM – sample plates and beam spot
7cm
Sample plates:
Ag coated pure aluminum
Ni coated pure aluminum
Muon
Beam Spot
Sample size dependent
Muon fraction
How do we deal with the background?

## Slide 29: LEM – sample plates, mSR parameters
H. Saadaoui et al., Physics Procedia 30, 164 (2012)
E=14keV, T=100K
E=14keV
T=100K

## Slide 30: LEM cryostats – cold finger cryostats («Konti»)
Konti flow cryostats, 4 - 320 K at sample plate
Konti-1: normal operation and for special experiments
(current injection and tests)
Konti-2: normal user operation
Konti-3: normal user operation,
application of electric fields, current injection
Konti-4: normal user operation
Sample change: 2 – 3 h
Sample plate can be biased up to +/-12.5kV to adjust the muon implantation energy.
A sapphire disk is used for electric insulation and providing good thermal conductivity to the cold finger of the cryostat

## Slide 31: LEM cryostats – «LowTemp Cryo» with He phase separator
2.1K
2.8K
2.3K
≈ 200 mW
Sample change: 6 h

## Slide 32: LEM – Oven
Macor
Radiation shield missing in the picture
Boron Nitrate
heater plate
High voltage lead
RT – 400 K with +-10 kV at sample
T > 400 high voltage might get tricky
Tmax ~ 600 K
Sample change: 2 – 3 h

## Slide 33
Implantation of low-energy m+ in matter – stopping profiles

## Slide 34: Different muon energies for different applications
LE-µSR
Bulk µSR
Decay Beam
Surface Beam
Cu
Cosmic Muons
Bulk μSR (MeV muons):
ʻʻnormalʼʼ samples (sub-mm)
bulk samples in pressure cells or containers (e.g. liquids)
MeV muons delivered by the “secondary beam lines” connected to the proton beam (“primary beam line”) target
Low-energy mSR (LE-μSR, keV m+):
depth-dependent investigations (≈ 5 – 300nm)
Cannot be extracted from the proton beam target
Needs an efficient conversion (“moderation”) of MeV muons to keV muons, “tertiary beam line” of keV muons
Strategy: Convert MeV muons to thermal (meV) or epithermal (eV) energies and re-accelerate up to 30 keV

## Slide 35: Particles Stopping in Matter
Energy loss of particles in matter:
Stopping Power
W. Eckstein, “Computer Simulation of Ion-Solid Interactions”, Springer (1991). J.F. Ziegler, J.P. Biersack, M.D. Ziegler, “SRIM - The Stopping and Range of Ions in Matter”, Lulu Press Co.
Bethe-Bloch

## Slide 36: Low-energy µ+ stopping profiles
Calculated by the Monte Carlo code TRIM.SP
TRIM.SP: W. Eckstein “Computer Simulation of Ion-Solid Interactions”, Springer (1991)
0
5
10
15
20
25
30
35
0
50
100
150
200
Range
Variance
Energy [keV]
nm
YBa2Cu3O7
YBa2Cu3O7

## Slide 37: TRIM.SP, SRIM – check Monte Carlo Codes
E. Morenzoni et al., NIM B 192, 254 (2002).
Idea:
Experimental fact: in fused quartz implanted µ+ form almost 100% muonium, Mu, at almost all implantation energies.
Grow sample on SiO2, and do the following:

## Slide 38: TRIM.SP, SRIM – check Monte Carlo Codes
E. Morenzoni et al., NIM B 192, 254 (2002).
TRIM.SP

## Slide 39
Applications of LE-mSR: thin films and interfaces
Superconducting and magnetic properties at surfaces and interfaces:
Meissner screening, proximity effects, volume fractions

## Slide 40
nonlocal
local
z
B(z)
x(T=0) = ħvf/[pD(T=0)]
Direct, absolute measurement of
magnetic penetration depth l
effective mass
density of supercarriers
Determination of the coherence length x („size of Cooper pairs), and magnetic penetration depth l; k=l/x (Ginzburg-Landau parameter)
Local, non-local response: local if k >~ 1.4; if local: field profile is exponential: B(z) = B0 exp(-z/l)
Direct determination of temperature dependence of SC order parameter ns(T) ~ 1/l(T)2
Direct test of theories (London, BCS)
Magnetic field profile in a superconductor
Notes: 40

## Slide 41
July-05 2010
page 41
A superconductor expels a magnetic field from its interior (“Meissner effect”)
First direct study of 1D field profile by LE-mSR
Notes: 41

## Slide 42
samples produced by R. Liang, W. Hardy, D. Bonn, Univ. of British Columbia;
Mosaic of samples glued onto the Ni coated sample plate of the LEM cryostat.
1/l2 ~ ns/m* ≡ rs, superfluid density
T-dependence: symmetry of the SC gap
effective mass
density of super carriers
In-plane anisotropy in detwinned YBa2Cu3O6.92
Notes: 42

## Slide 43
page 43
100 K
8 K
8 K
at low T for a d-wave SC:
la = 126(1.2)nm, lb = 105.5(1.0) nm, la/lb = 1.19(1)
R.F. Kiefl et al, Phys. Rev. B81, 180502(R), (2010)
(r(z): muon stopping profile)
Detwinned YBa2Cu3O6.92, Tc = 94 K, B = 9.47 mT
Notes: 43

## Slide 44
(r(z): muon stopping profile)
i) If parametrization of B(z) is known: Directly fit mSR asymmetry A(t) with the proper function [Eq. (2)].
ii) B(z) can be determined without knowledge of its functional form: Fourier-transform of A(t) to obtain mSR field distribution p(B,E) as a function of implantation energy E. For low-statistics data: use a Maximum-Entropy analysis to determine p(B,E). The following procedure works for monotonous B(z).
n(z,E): muon stopping distribution at implantation
energy E.
A(t)
A. Suter et al., Phys. Rev. B72, 024506 (2005).
R.F. Kiefl et al, Phys.Rev. B81, 180502(R), (2010).
Two methods to determine field profile B(z)
Notes: 44

## Slide 45
A. Suter et al., Physical Review B72, 024506 (2005).
Pb, 5.2 keV, 3.05 K; B(z) determined by using Eq. (13) from previous slide.
Exponential B(z) (local response); data clearly
deviate from exponential → non-local effect!!
1st direct observation of non-local effects in Pb (k~0.6)
Notes: 45

## Slide 46
Non-local: non-exponential
local: exponential
T.J. Jackson et al., Phys. Rev. Lett. 84, 4958 (2000).
A. Suter et al., Phys. Rev. Lett. 92, 087001 (2004).
A. Suter et al., Phys. Rev. B72, 024506 (2005).
k = l0/x0 ~ 0.6
k = l0/x0 ~ 90
1st experimental determination of x0 in a non-local superconductor; confirmation of some predictions of BCS (~50 years after theory!!)
Magnetic field profiles in Pb and YBa2Cu3O7-d
Notes: 46

## Slide 47: LE-mSR study of interface/proximity effects
Measure local magnetic field as function of energy/depth below and above Tc
Meissner screening at T < Tc
Normal metal (Cu) exhibits a Meissner effect when in contact with a superconductor (Nb): results confirmed by theoretical calculations
Using LE-mSR an unexpected effect is found when adding a ferromagnetic (Co) layer: the enhancement of the Meissner effect in the non-magnetic Cu layer separated from the ferromagnetic layer by the 50-nm-thick Nb layer
Observation of Anomalous Meissner Screening in Cu/Nb and Cu/Nb/Co Thin films
M.G. Flokstra et al., Phys. Rev. Lett. 120, 247001 (2018)
S(II): Nb layer with higher purity Nb than S(I)
NS(II): Cu/Nb layer with higher purity Nb
NSF(I): Cu/Nb/Co layer with lower purity Nb
NSF(II): Cu/Nb/Co layer with higher purity Nb

## Slide 48: LE-mSR study of interface/proximity effects
Unexpected results: largest flux expulsion observed when a 2.4 nm FM Co layer is added
The new, «electromagnetic proximity effect» is the origin of the enhanced flux expulsion: screening response of the SC to a vector potential near the SC/FM interface (A.F. Volkov et al., PRB 99, 144506 (2019))
Observed cooperation of SC and FM could be a key ingredient for superconducting spintronics
Manifestation of the electromagnetic proximity effect in superconductor-ferromagnet thin film structures
M.G. Flokstra et al., Appl. Phys. Lett. 115, 072602 (2019)

## Slide 49: LE-mSR study of interface/proximity effects
Field enhancement in TI, «paramagnetic Meissner effect» arising from an odd-frequency SC state in the TI
1st observation of bulk odd-frequency SC in a TI
Paramagnetic Meissner effect in Au/Ho/Nb: A. Di Bernardo et al., PRX 5, 041021 (2015)
Proximity-Induced Odd-Frequency Superconductivity in a Topological Superconductor
J.A. Krieger et al., Phys. Rev. Lett. 125, 026802 (2020)

## Slide 50: LE-mSR study of interface/proximity effects
unique combination of ARPES/DFT (electonic structure at interface) and LE-mSR (local magnetic properties)
comparison between EuS/Bi2Se3 and EuS/Ti on sapphire: observed local magnetic properties independent of topology and the electronic structure at the interface
No need to introduce interplay between topology and FM at the interface
Do topology and ferromagnetism cooperate at the EuS/Bi2Se3 interface?
J.A. Krieger et al., Phys. Rev. B 99, 064423 (2019)

## Slide 51: LE-mSR: AFM order in ultra-thin LaNiO3
Dimensionality Control of Electronic Phase Transitions in Nickel-Oxide Superlattices
A.V. Boris et al., Science 332, 937 (2011)
Transition metal oxides AMO3 with perovskite structure have attracted wide-spread interest:
- Wide range of functionalities originating from interplay between lattice, electronic, and magnetic degrees of freedom
- Rare-earth nickelates RNO3 are a prototypical case with great potential for engineering novel electronic and magnetic states
- LaNiO3 paramagnetic metal down to lowest temperatures; all others show a MI transition, accompanied by a PM-AFM transition
Phase diagram of RNO3, from J. Fowlie et al., PSI proposal 20190133.

## Slide 52: LE-mSR: AFM order in ultra-thin LaNiO3
Dimensionality Control of Electronic Phase Transitions in Nickel-Oxide Superlattices
A.V. Boris et al., Science 332, 937 (2011)
Superlattices (SL) of (LaNiO3)N/(LaAlO3)N with N=2 u.c. and N=4 u.c. were grown by PLD on LSAO and STO substrates (compressive and tensile strain), total SL thickness of 100 nm.
Spectral ellipsometry: dielectric permittivity for N=2 u.c. and N=4 u.c. LaNiO3 on different substrates, showing a MI transition at 160 K (C) and 110 K (D) for N=2 u.c., but not for N=4 u.c. which remains metallic.
Expect a PM-AFM transition for the N=2 u.c. sample. But how to detect AFM order in such a thin SL?
Use LE-m+SR!
TMI
TMI

## Slide 53: LE-mSR: AFM order in ultra-thin LaNiO3
Dimensionality Control of Electronic Phase Transitions in Nickel-Oxide Superlattices
A.V. Boris et al., Science 332, 937 (2011)
Time evolution of zero-field mSR Polarization (A) and transverse field precession amplitude (C ) with LSAO substrate:
Development of static AFM state at T < 50 K for the N=2 u.c. sample.
In agreement with the expectation: MI transition is related to a PM-AFM transition.

## Slide 54: LE-mSR: AFM order in ultra-thin LaNiO3
Dimensionality Control of Electronic Phase Transitions in Nickel-Oxide Superlattices
A.V. Boris et al., Science 332, 937 (2011)
Competition between collective quantum phases in strongly correlated electron systems depends sensitively on dimensionality, which is difficult to control by standard solid-state chemistry
Metal-oxide superlattices allow the control of the dimensionality and collective phase behavior of correlated electron systems
Magnetic volume fraction fm and dielectric permittivity e1* showing the MI and AFM transition temperatures TMI and TN (tensile strain (SrTiO3) and compressive strain (LaSrAlO4)).

## Slide 55
LE-mSR: nanometer-scale magnetic homogeneity
Evidence for the homogeneous FM phase in (Ga,Mn)(Bi,As) epitaxial layers from mSR
K. Levchenko et al., Scientific Reports 9, 3394 (2019)
Spintronics: magneto-resistive devices, based on planar Hall effect (PHE), can be made of DFS (Ga,Mn)As
Adding Bi, (Ga,Mn)(Bi,As), enhances magneto-transport effects due to strong enhancement of spin-orbit coupling
Practical limitations may arise if the system is inhomogeneous:
use LE-m+SR to test magnetic homogeneity
Notes: 55

## Slide 56
LE-mSR: nanometer-scale magnetic homogeneity
Evidence for the homogeneous FM phase in (Ga,Mn)(Bi,As) epitaxial layers from mSR
K. Levchenko et al., Scientific Reports 9, 3394 (2019)
Notes: 56

## Slide 57
LE-mSR: nanometer-scale magnetic homogeneity
Evidence for the homogeneous FM phase in (Ga,Mn)(Bi,As) epitaxial layers from mSR
K. Levchenko et al., Scientific Reports 9, 3394 (2019)
A.J. Drew et al, Nature Materials 8, 109 (2009)
LE-mSR shows:
Long-range FM order develops below TC in full volume fraction
Weak magnetic stray fields in the substrate indicates single domain FM phase with low interface roughness (<~ 2nm)
Notes: 57

## Slide 58
LE-mSR: magnetic transition in multiferroics under strain
Engineering the magnetic order in epitaxially strained Sr1-xBaxMnO3 perovskite thin films
L. Maurel et al., APL Materials 7, 041117 (2019)
FIG. 2. Temperature dependence of the transverse fraction fTTF of the muons normalized to the fraction at 300 K, determined from LE-μSR measurements for 10-nm-thick Sr1-xBaxMnO3 films on (a) LSAT and (b) TSO. The arrows indicate the magnetic order temperature.
Notes: 58

## Slide 59: Summary
The low-energy muon facility with LE-mSR is the most complex experimental setup for mSR studies
Apparatus/experimental effects at low implantation energies makes analysis of mSR data more complicated than «standard» mSR data
  Time-of-flight distribution to the sample distorting the first 70 ns of mSR spectra, energy dependence of asymmetry, contribution of reflected muons below 3 keV
  Muon stopping distribution
Unique experimental capabilities in measuring magnetic field profiles in superconductors and superconductor heterostructures with 2-3 nm depth resolution, proximity effects, homogeneity of magnetic order in thin layers and heterostructures, dimensional effects

## Slide 60: Muon Spin Spectroscopy School 2026, Jan 14 – 21
Jointly organised by PSI, ISIS, KTH
Thank you for your attention!

## Slide 61
Appendix
Depth profiling of defect regions with nm resolution at technologically relevant semiconductor interfaces (MOSFETs, solar cells)

## Slide 62: Why to use m+ to measure defect profiles at SC interfaces?
Defects and structural changes at semiconductor interfaces are of fundamental importance for the performance of semiconductor devices. SiC-based MOSFET fabrication, for example, requires oxidation, ion-implantation and other processes creating defects in the device structure.
Standard characterization methods (DLTS, CV, IV, PL) for the investigation of process-induced defects have limited depth resolution (>100 nm) of the defect profiles close to interfaces. ARPES, TEM and EELS show large spread of data from nm to tens of nm.
Defect profile information on the nm scale is essential to better understand the relation between defects and limitations in device performance.
Low-energy muon spin rotation (LE-m+SR, 1 – 30 keV, mean implantation depths 5 – 200 nm) is a powerful tool to study defect distributions with nm depth resolution.
Here: study the effect of defects in proton-irradiated Si and 4H-SiC on the formation of hydrogen-like muonium states, and apply the technique to SiO2/Si, SiO2/SiC interfaces and solar cell materials (CIGS).

## Slide 63: Muonium complexes in Si and 4H-SiC
R. L. Lichti, et al., Phys. Rev. B 70, 165204 (2004)
M. E. Bathen, et al., J. Appl. Phys. 127, 085701 (2020)
4H-SiC
Si
T
BC
B.D. Patterson, Rev. Mod. Phys. 60, 69 (1988)
in AB to Si(k),
at ABC,
HAL-9500, PSI 2022
R. L. Lichti et al.,
Phys. Rev. B 70, 165204 (2004)
T=30 K E=15.4 keV
0.15 T
Notes: In Si, we will focus on the BC state. MuBC0 ionizes a
In 4H-SiC: Mu0 in AB to Si(k)
Which is also likely to be acceptor.

## Slide 64: LE-µSR study of defects in Si (n ̴5×1011 cm-3)
10-keV proton profiles (circles) and muon stopping profiles.
4H-SiC annealed at 1150oC after irradiation (mainly VC left).
Defects ↑: AD & FD=AD/(AD+AMu)↑
AMuBC & AMuT ↓
Identification of defect regions in Si
J. Woerle, et al., Physical Review B 100, 115202 (2019)
J. Woerle, et al., Physical Review Applied 14, 054053 (2020)
10 keV protons
Notes: Mu- formation
mention SIO2 side: defects

## Slide 65: LE-µSR study of defects in 4H-SiC (n ̴3×1015 cm-3)
Carbon vacancies ↑ , AD ↑
[VC] > 1×1017 cm-3
µ+ trapping in VC followed by double electron capture to form Mu-.
Silicon vacancies ↑ , AD ↓
[VSi] > 3×1014 cm-3
VSi – Mu is energetically more favorable than isolated VSi.
«Muons can distinguish VC and VSi»
J. Woerle, et al., Physical Review B 100, 115202 (2019)
J. Woerle, et al., Physical Review Applied 14, 054053 (2020)
Notes: Mu- formation
mention SIO2 side: defects

## Slide 66: Analysis of SiO2/Si (n ̴5×1016 cm-3) interface
Model of the depth variation of the muon signal in the SiO2/Si system obtained from the measured energy dependence.
The muon signal (diamagnetic fraction and paramagnetic fraction, FD, FMu) is sensitive to the presence of free carriers and defects.
Deposited oxide (PECVD) (300oC) on Si:
Deposition of oxide results in a sharp interface.
Deposited oxide is defect-rich.
Thermal oxidation (1050oC) of Si leads to:
Defect-rich/strained region ( ̴20 nm) on SiO2 side.
5 – 10 nm defective region in Si, or electron accumulation at the interface (Mu- formation).
Dit ̴1012 cm-2 eV-1.
M. Mendes Martins, et al., Adv. Mater. Interfaces 10, 2300209 (2023)
M. Mendes Martins, et al., J. Phys.: Conf. Ser. 2462, 012025 (2023)
A.F.A. Simões, et al., Rev. Sci. Instr. 91, 023906 (2019)
MuBC0
MuBC+
Si-C: Si-B, HF, PECVD

## Slide 67: Analysis of SiO2/4H-SiC interface
4H-SiC Si-face, epi-layer (n ̴8×1015 cm-3)
4H-SiC C-face: (n ̴1019 cm-3)
PECVD of SiO2 and thermal oxidation (1050oC) of 4H-SiC lead to:
SiC-A: Dit ~1×1012 cm-2 eV-1, SiC-B: Dit ~8×1012 cm-2 eV-1.
Si-face: more defects and oxidation induced strain in 20 nm of SiO2, 5 nm defective region in SiC.
Si-face: higher e- concentration from interface traps cause disappearance of FMu in SiC-B.
C-face: defect rich region in 10 nm of SiO2. 30 nm defective region in SiC, formation of C-rich layer during oxidization, which persists after removal of SiO2.
C-face: thermal growth of oxide results in a layer with more structural disorder, not suitable for device applications
M. Mendes Martins, et al., Adv. Mater. Interfaces 10, 2300209 (2023)

## Slide 68: Analysis of SiO2/4H-SiC (n~1019 cm-3) interface, C-face
SiC-D = SiC-C, HF, PECVD
C-face: defect rich region in 10 nm of SiO2. 30 nm defective region in SiC, formation of C-rich layer during oxidization, which persists after removal of SiO2.
C-face: thermal growth of oxide results in a layer with more structural disorder, not suitable for device applications
M. Mendes Martins, et al., Adv. Mater. Interfaces 10, 2300209 (2023)
Muon implantation energy (keV)
Depth (nm)
Depth (nm)
Muon implantation energy (keV)
Diamagnetic Fraction
Diamagnetic Fraction
Deposited

## Slide 69: LE-µSR study of annealing effects at the SiO2/4H-SiC interface
Defects created in SiO2 increase AD
In SiC:
AD ↑ due to Mu- formation, n ≳ 1×1016 cm-3 and passivation of Vsi
AD ↓ due to presence of Vsi (Ar1300)
Annealing in NO at 1300℃ introduces N which acts as donor, and which passivates VSi: AD ↑
P. Kumar, et al., Phys. Rev. Applied 19, 054025 (2023)
4H-SiC n ̴3×1015 cm-3
Notes: Mu- formation
mention SIO2 side: defects

## Slide 70: Interfacial defect layers in CIGS solar cells
Near interface, lattice distortions appear in a ~50-nm wide region due to long-range strain fields caused by defects
Defects increase barrier height  FD ↓
Passivation of defects by buffer layers is crucial for device performance/efficiency
LE-mSR measurements allow quantification of defect passivation effect of various buffer layers
H.V. Alberto, et al., Adv. Mater. Interfaces 9, 2200374 (2022)
Notes: Mu- formation
mention SIO2 side: defects