## Slide 1
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program, http://chart.ch.
MagDev2 Overview
B. Auchmann for the MagDev Teams
SMACC1 Conceptual Design Review, Jan 13-14, 2025.
HFM
High Field Magnets
Programme

## Slide 2
CHART 2016-2019

## Slide 3: Canted Dipole 1 Built at PSI
Magnet design, lab refurbishment, equipment, and commissioning, as well as magnet construction from 02.2017 to 10.2019.
[G. Montenero et al., Coil Manufacturing Process of the First 1-m-Long Canted-Cosine-Theta (CCT) Model Magnet at PSI, IEEE Trans. on App. SC., Vol 29(5), 2019. G. Montenero et al., Mechanical Structure for the PSI Canted-Cosine-Theta (CCT) Magnet Program, IEEE Trans. on Appl. SC., Vol 28(3), 2018.]

## Slide 4: CD1 Lessons on Robustness and Performance
Courtesy F. Mangiarotti (CERN) and M. Daly (PSI).
Magnet test in January 2023:
The magnet trained A LOT.
But, it reached 100% of maximum field at 4.5 K.
These were the first Nb3Sn training coils at PSI:
  No conductor degradation occurred from handling, assembly, powering, or thermal cycling.
Stress-management works, CD1 is a robust magnet.

## Slide 5: CHART1 Collaborations
CERN: co-financed MagDev0 and MagRes0; tested CD1.
ETHZ D-MAT Soft Materials Group: Characterize commonly used epoxies for fracture toughness and other properties in cryogenic conditions.
LBNL: transferred Nb3Sn CCT technology
PSI Magnet Section: directly involved in laboratory refurbishment, magnet technical design, and magnet construction.

## Slide 6
CHART 2020-2024

## Slide 7: MagDev Laboratory at PSI
31.11.2019
30.6.2020
The lab is an extension to WLHA building, which houses normal-conducting magnet development, field quality measurements, and undulator development.
It provides 400 m2, organized roughly along the lines of CERN’s 927 laboratory.

## Slide 8: MagDev Laboratory
Douglas Araujo
Engineer LTS
Henrique Rodrigues
Process Engineer ReBCO
Dmitry Sotnikovs Design Engineer ReBCO
André Brem
Material Scientist
Thomas Michlmayr
CAD, Technical Design
Colin Müller Mechanic LTS
Jaap Kosse
Engineer ReBCO
Anna Stampfli
Technician Processes
Jürgen Schmidt
Technician HTS
Joep Van den Eijnden
PhD Student
Christina Lindner
Technician HTS
Matteo Crescenti
PhD Student
+ 2 more arrivals in 2025
Kirtana Puthran
Engineer ReBCO

## Slide 9: Fast-Turnaround Stress-Management R&D
HFM R&D has suffered from slow turnaround and late feedback on technology.
Minimum viable products have enabled a breakthrough in stress-managed Nb3Sn technology.
Goal: Build industrializable Nb3Sn high-field magnets that “just work”.
Materials and Composite Samples (not powered)
Powered Samples and Mechanical Models
Sub-scale Magnets (5 T)
Short Magnets Ultimate Field (14…16T)
Long Magnets Ultimate Field Magnets (14…16 T)
2019
2020
2024
First deliverable
100s
10
2-3
0.5-1
#Deliverables / year
Long-magnet infrastructure available only at CERN.
2025/26
Courtesy D. Araujo
Courtesy M. Daly
Courtesy D. Araujo
2x
1x
5x
1x
produced in Q2/24 ...

## Slide 10: 10-Stack
ETHZ: 10-stack measurements with image analysis (particle-tracking method).
  Epoxy vs. paraffin, vs. filled epoxy and paraffin.
Extraction of homogenized material description for ANSYS (or other) pending.
ETHZ D-ITET PhD thesis work on multi-scale modeling in its first year.
[X. Kong, T. Tervoort, et al., CHART annual meeting, indico link, Oct. 2023.]

## Slide 11: BOX
alumina-filled paraffin wax
Courtesy, A. Brem, M. Daly, S. Otten, S. Sidorov
BOX (BOnding eXperiment) program with uTwente has shown a wide variety of results, from complete conductor degradation (no impregnation) to substantial training (epoxy) to no-training (wax, Stycast, filled wax), with 21 BOX samples successfully and tested to date.
Notes: LBNL is preparing a wax impregnated subscale CCT magnet

## Slide 12: Compression BOX
Courtesy M. Daly
Successful systems are characterized in U Twente’s transverse-compression setup.
CTD 101-K measurements reproduce previous resultsof Twente U-shaped samples.
Paraffin wax’s lower modulus and yield increase degradation. Filled wax bumps wax up to CTD 101-K support.
Courtesy, A. Brem, M. Daly, S. Otten, S. Sidorov

## Slide 13: subSMCC1 Performance
[Test data courtesy of G. Willering, CERN]

## Slide 14
PSI/BNL BigBOX: a 13-turn SM racetrack.
No training with 12.3 T coil field, 170 MPa coil stress at BNL’s DCC17.
LBNL wax impregnated sub-scale (5 T) CCT.
First Nb3Sn CCT without training.
Alumina-filled wax subCCT with a single training quench.
Wigner Inst./CERN SuShi septum for FCC
Wax impregnated Nb-Ti CCT, no training to nominal current.
CERN FCC-ee final focus quad demo
Nb-Ti CCT to short-sample without training.
PSI subSMCC1 2-in1 dipole (5T)
Nb3Sn common coil R&D magnet without training at 4.5 K. Support from LBNL/CERN.
Courtesy D. Barna et al., Wigner Institute
Courtesy J.L. Rudeiros Fernandez, LBNL
Courtesy M. Koratzinos et al., CERN/PSI
D. Barna et al., Training-free performance of the wax-impregnated SuShi septum magnet, SUST 37, 2024.
D. Arbelaez et al., Training-free demonstration of a 5.4 T Nb3Sn Canted–Cosine–Theta accelerator dipole impregnated with paraffin wax, SUST 37(6), 2024.
Six stress-managed R&D magnets with (almost) no Training
Courtesy D. Araujo et al
Courtesy D. Araujo et al

## Slide 15: High-Temperature Superconductor: 4-Stack Technology Solenoid
inside

## Slide 16
15 T in 72 mm warm bore
15 K conduction-cooling
Solid-state (Pb) thermal buffer
5 coils from 12 mm ReBCO, 110 mm ID 21 T peak field
target
HTS no-insulation positron-capture solenoid, to demonstrate positron source with 10x increased yield wrt. state of the art. Manufacturing/commissioning in 2024/25. Experiment at PSI’s SwissFEL 2025/26
FCCee Injector Study: P3 experiment (PSI Positron Production)
Coil technology licensed from

## Slide 17: HTS ReBCO Accelerator Magnets for FCC-hh
ReBCO promises more sustainable operation, higher physics reach, and a more credible cost prospect.
Higher magnet temperature (20 K) improves power consumption for static and beam-induced losses.
  Higher fields and collision energies could be envisaged but main cryo load for FCC-hh becomes synchrotron radiation (SR) on the beam screen.
  Increased ramp losses may (at least) in part cancel the improved cryogenic efficiency at 20 K.
    Initial estimates indicate a >2x increase in ramp losses wrt. Nb3Sn state of the art.
Screening-current and -loss calculation Courtesy D. Sotnikov, PSI
Screening current density [A/m2]
Power density [W/m, integrated over cable x-sec]

## Slide 18: ReBCO FCC-hh Dipole Scaling Exercise
As expected, AC losses grow non-linearly with field due to larger field sweep and growth in coil-size.
In this study (for which all previous caveats and assumptions apply) AC losses increase 4-fold from 14 to 20 T.
Initial results indicate that losses decrease mildly towards lower temperatures.

## Slide 19: ReBCO FCC-hh Dipole Scaling Exercise
In this study, a strong screening effect is observed. Multiple cycles are needed to reach reproducible conditions.
Experimental validation is of the essence.
Local correction schemes will be required.
How much can be achieved with beam-based feedback and possibly AI models?

## Slide 20: HTS subscale preliminary work
Goals:
Re-use subSMCC design and structure for 6-8 T ReBCO magnet (6-8 tapes).
Dry or soldered ReBCO insulated tapes-stack cable.
SMCC magnet with apertures for field quality measurements.
Experimental and numerical protection studies.
Reproducibility study.

## Slide 21: CHART2 Collaborations
BNL: BigBOX testing, common coil design for US-MDP 20-T design study (DA extra hours)
CEA: Rutherford cable geometrical models and meshes
CERN TE-MPE: protection simulations,
CERN TE-MSC: LTS conductor procurement and characterization, assistance in coil reaction, magnet testing, cold magnetic measurements, BOX program, etc.
CERN TE-CRG: FCC-hh@20 K sustainability study
EPFL SPC: ASC on campus, material characterization, coil winding, pre-tinning, forced-flow cooling
ETHZ D-MAT SMG: resin development, LTS coil composite characterization and const. modeling
ETHZ D-MAVT pd|z: AM for structural coil parts in Nb3Sn magnets
ETHZ D-ITET EE: Model-Based Systems Engineering
ETHZ D-ITET PES: Cryogenic power converters
FNAL: materials exchange
LBNL: subscale cables, exchanges on materials R&D
PSI Magnet section: Laboratory construction and services, cryogen-free test station, HTS4 FQ measurement, manufacturing aid in times of need.
PSI Spectroscopy of Quantum Materials: manipulator head for ACCESS2.0 beam line
PSI Neutron Scattering: split solenoid cryostat
UniGE: Metal-Insulator Switching Materials
uTwente: BOX program, HTS coils AC measurements

## Slide 22
CHART 2025-2028

## Slide 23: CHART MagDev3
Main goals:
Demonstrate LTS baseline technology for FCC-hh as soon as possible.
Develop HTS accelerator-magnet technology as if our future depended on it.

## Slide 24: CHART MagDev3
Discussions with CERN- hosted HFM Programme and CHART started.