## Slide 1: PSI SMACC1 quench protection
Emmanuele Ravaioli (CERN)
D. Araujo (PSI), B. Auchmann (PSI), A. Verweij (CERN), M. Wozniak (CERN)
PSI SMACC1 Design Review
2025.01.13

## Slide 2
SMACC magnet by Douglas Araujo at PSI
First demonstrator will be built at PSI
12 T bore field with >20% margin at T=1.9 K
Circular bore with 50 mm diameter
250 mm intra-beam distance
Utilizing two already-existing Nb3Sn cables
Inom= 12.9 kA  12.0 T
14.1 kA  13.0 T
15.3 kA  14.0 T
ISS= 16.8 kA  15.2 T
No flexibility in the choice of conductor grading
Quench protection is much more challenging
(one conductor heats up twice more quickly!)

## Slide 3
Hot-spot temperature Thot<350 K
Peak voltage to ground Ug<1 kV
Quench protection targets and constraints
If CLIQ is used,
CLIQ unit current IC<5 kA

## Slide 4
ACTIVELY
EXTRACT ENERGY
Energy extraction system
ACTIVELY
SPREAD ENERGY
Active heating system
Energy extraction with constant resistor
Energy extraction with varistor
CLIQ
(Coupling-Loss Induced Quench system)
Energy Extraction + CLIQ
Analyzed quench protection options

## Slide 5
Quench detection based on differential voltage monitoring
Resistive voltage build-up simulated
for different quench locations
LEDET
Detection threshold of 100 mV is reached in 4.3 ms after quench in a high-field turn
(that is the worst case for protection here)
4.3 ms

## Slide 6
Total reaction time tR
Total reaction time
tR
Quench detection time
Validation time
Triggering time
+
+
=
4.3 ms
for a quench in the worst-case turn
5 ms
assumption based on experience with similar magnets
3.2 ms
for energy extraction mechanical switch
0.2 ms
for CLIQ unit
12.5 ms
for energy extraction
9.5 ms
for CLIQ
≈
Of course these values are not general, but they are valid for the test facility where the tests will be performed

## Slide 7
Quench protection options
CLIQ
(Coupling-Loss Induced Quench system)
EE
(Energy extraction)

## Slide 8
Quench protection with 1 kV energy extraction with constant resistor
The presence of quench-back influences significantly the transient
Reduction of differential inductance
Quench-back (coil resistance increase due to transient losses)
LEDET
hot-spot (highest field location in the outer layers)

## Slide 9
Hot-spot temperature as a function of total reaction time
LEDET
Varistor (EEV) improves quench protection (30-50 K temperature reduction)
Quench protection possible (Thot<350 K)
if tR<20 ms (for EER) or tR<25 ms (for EEV)
Estimated total reaction time tR=12.5 ms, which leaves a good margin at Inom

## Slide 10
Quench protection summary at Inom – EER and EEV
LEDET
Quench protection | T_hot [K] | Peak U_ground [V] | Peak I_CLIQ [kA]
1000 V EER | 288 | 1000 | 0.0
1000 V EEV | 257 | 966 | 0.0

## Slide 11: Electrical connections of CLIQ configurations
CLIQ-C1
CLIQ-C2
CLIQ-C3

## Slide 12
CLIQ optimization
CLIQ PERFORMANCE CAN BE GREATLY ENHANCED BY SELECTING THE OPTIMUM CONFIGURATION
CLIQ-C1
CLIQ-C2
CLIQ-C3

## Slide 13
Quench protection with 50 mF, 300 V CLIQ-C3 system
LEDET
Very fast quench
(most turns quenched in <5 ms)
Hot-spot temperature ~280 K
Peak voltage to ground ~150 V
hot-spot (highest field location in the outer layers)

## Slide 14
Quench protection summary at Inom – CLIQ
LEDET
Quench protection | T_hot [K] | Peak U_ground [V] | Peak I_CLIQ [kA]
1000 V EER | 288 | 1000 | 0.0
1000 V EEV | 257 | 966 | 0.0
500 V CLIQ C-1 | 293 | 250 | 4.7
400 V CLIQ C-2 | 277 | 195 | 4.4
300 V CLIQ C-3 | 279 | 151 | 4.5

## Slide 15
Energy extraction + CLIQ optimization
EE + CLIQ-C1
EE + CLIQ-C2
EE + CLIQ-C3
LEDET
Parametric study to identify the combinations of CLIQ configuration, CLIQ charging voltage, and EE voltage rating that satisfy all requirements in terms of hot-spot temperature
(Thot<350 K), peak voltage to ground (Ug,m<1000 V), and peak CLIQ current (IC,m<5 kA)
Recommandation: CLIQ “Configuration 1”, 300 V CLIQ + 1 kV EE
Low hot-spot temperature. Redundancy. Wider, more flexible parameter space.

## Slide 16
Quench protection summary at Inom – EER+CLIQ and EEV+CLIQ
LEDET
Quench protection | T_hot [K] | Peak U_ground [V] | Peak I_CLIQ [kA]
1000 V EER | 288 | 1000 | 0.0
1000 V EEV | 257 | 966 | 0.0
500 V CLIQ C-1 | 293 | 250 | 4.7
400 V CLIQ C-2 | 277 | 195 | 4.4
300 V CLIQ C-3 | 279 | 151 | 4.5
1000 V EER + 300 V CLIQ C-1 | 227 | 1000 | 4.8
900 V EER + 100 V CLIQ C-2 | 232 | 958 | 4.6
600 V EER + 100 V CLIQ C-3 | 256 | 614 | 4.7
1000 V EEV + 200 V CLIQ C-1 | 206 | 1000 | 4.1
900 V EEV + 100 V CLIQ C-2 | 216 | 959 | 5.0
600 V EEV + 100 V CLIQ C-3 | 244 | 607 | 4.9
There is some flexibility since several options can protect the magnet

## Slide 17
Currents versus time for the different quench protection options
LEDET
All options can protect the magnet if the total reaction time is <24 ms
CLIQ charged to low-medium voltage achieves sufficiently low temperature
with 4-5 times lower voltage to ground
Energy extraction plus CLIQ achieves the lowest hot-spot temperature overall
There is some flexibility since several options can protect the magnet

## Slide 18
Hot-spot temperature as a function of total reaction time
All options can protect the magnet if the total reaction time is <24 ms
LEDET
CLIQ charged to low-medium voltage achieves sufficiently low temperature
with 4-5 times lower voltage to ground
Energy extraction plus CLIQ achieves the lowest hot-spot temperature overall
Recommandation: CLIQ “Configuration 1”, 300 V CLIQ + 1 kV EE

## Slide 19
Selection of the quench protection strategy
LEDET
 | EER | EEV | CLIQ | EER+CLIQ | EEV+CLIQ
Lower T_hot |  |  |  |  | 
Lower U_ground |  |  |  |  | 
Simpler |  |  |  |  | 
More redundant |  |  |  |  | 
Protection at 12 T |  |  |  |  | 
Protection at short sample |  |  |  |  | 
Protection equipment available |  |  |  |  | 
Green=Good. Yellow=Fair. Red=Bad. |  |  |  |  | 
Recommandation: CLIQ “Configuration 1”, 300 V CLIQ + 1 kV EE

## Slide 20
Quench detection at higher currents
Resistive voltage build-up simulated
after quench in a high-field turn
LEDET
Detection threshold of 100 mV is reached in 4.3 ms at 12.9 kA (12 T)
in 2.5 ms at 14.1 kA (13 T)
in 1.2 ms at 15.3 kA (14 T)
4.3 ms  1.2 ms

## Slide 21
Hot-spot temperature as a function of initial current, EER+CLIQ-C1
Up to nominal current (12.75 kA, i.e. 12 T), with REE=78 m, i.e. UEE=1 kV at nominal,
the quench protection is comfortable.
LEDET
At higher currents, REE needs to be reduced to maintain UEE≤1 kV
12 T
13 T
14 T
SS

## Slide 22
Hot-spot temperature as a function of initial current, EER+CLIQ-C1
Up to nominal current (12.75 kA, i.e. 12 T), with REE=78 m, i.e. UEE=1 kV at nominal,
the quench protection is comfortable.
LEDET
At higher currents, with lower REE=59 m,
i.e. UEE=1 kV at short-sample (ISS=16.85 kA),
the quench protection is at the limit.
12 T
13 T
14 T
SS

## Slide 23
Hot-spot temperature as a function of initial current, EER+CLIQ-C1
Up to nominal current (12.75 kA, i.e. 12 T), with REE=78 m, i.e. UEE=1 kV at nominal,
the quench protection is comfortable.
LEDET
In the previous simulations, EER and CLIQ are triggered simultaneously.
In reality, CLIQ is triggered in 0.1 ms while EER is triggered in 3.2 ms.
Quench protection is possible up to ISS
At higher currents, with lower REE=59 m,
i.e. UEE=1 kV at short-sample (ISS=16.85 kA),
the quench protection is at the limit.
12 T
13 T
14 T
SS

## Slide 24
Conclusion
Quench protection of 12 T common-coil SMACC magnet (PSI)
Five quench protection strategies are analyzed and compared
Energy extraction with constant resistor Energy extraction with constant resistor + CLIQ
Energy extraction with varistor Energy extraction with varistor + CLIQ
CLIQ
Optimized CLIQ connection configuration, CLIQ voltage, EE voltage rating
Recommandation: CLIQ “Configuration 1”, 300 V CLIQ + 1 kV EE
Low hot-spot temperature. Redundancy. Readily available equipment.

## Slide 25
For a general introduction on STEAM:
https://indico.cern.ch/event/1161448/
All simulations presented today were performed with LEDET,
a program that is part of the STEAM framework developed at CERN
All STEAM programs are available free of charge for the community
Interested? Visit us → https://espace.cern.ch/steam or Contact us → steam-team@cern.ch
LEDET

## Slide 26: Annex

## Slide 27
New common-coil concept by Douglas Araujo at PSI
with acknowledgment to a similar design proposed in LBNL, which did not focus on field quality [S. Gurlay et al., 1995]
Common-Coil
SMACC Common-Coil

## Slide 28
Magnet cross-section
4 cm thick Al shell
Pressured bladders and load keys for preload
623 mm yoke OD
3D end layout
Top-bottom coil asymmetry
Asymmetric common-coil by GL. Sabbi and E. Ravaioli (LBNL)
From FCC Week 2017

## Slide 29
No racetrack coils around the pole
Large bending radius for all turns
SMACC magnet by Douglas Araujo at PSI
SMACC
Stress-Managed
Asymmetric
Common-Coil
Congratulations to Douglas!
This is a major development
for the common-coil technology!

## Slide 30: Energy extraction system (EE)
Advantages
Straightforward design and implementation
Extracts energy from the cryostat
Disadvantages
Can be large and expensive for high current magnets
Impractically high voltage needed for high current density magnets
Can’t be applied to a chain of high-field magnets
Note: EE of LHC main dipole circuits doesn’t protect magnets

## Slide 31: Coupling-Loss Induced Quench (CLIQ)
Advantages
Fast and effective heat deposition
Heat deposited simultaneously in most of the coil volume
Electrically robust system
Disadvantages
Direct electrical connection to the magnet circuit
Challenging to make it redundant
Additional asymmetric forces on the magnet coils
Current change
Transient losses
Temperature increase
Coil SC→resistive
Magnet energy discharged
Reduced hot-spot temperature
Field change

## Slide 32: Interaction between CLIQ and energy extraction (EE) system
EE
Discussion
Is it possible/recommended to test and EE system together?
positive polarity → Superposition of voltage across CLIQ and across EE causes higher voltage to ground
negative polarity → Subtraction of voltage across CLIQ and across EE reduces CLIQ performance

## Slide 33
Hot-spot temperature as a function of total reaction time, EER+CLIQ-C1
At nominal current, the quench protection has significant margin even for REE=59 m, i.e. UEE=1 kV at short-sample current
LEDET
At short-sample current (16.85 kA),
Thot<350 K for tR<9 ms,
which is quite tight but not out of reach:
0.5 ms detection time +
5.0 ms validation time +
3.2 ms triggering time =
8.7 ms total reaction time

## Slide 34
Hot-spot temperature as a function of initial current, EER+CLIQ-C1
Up to nominal current (12.75 kA, i.e. 12 T), with REE=78 m, i.e. UEE=1 kV at nominal,
the quench protection is comfortable.
LEDET
At higher currents, with lower REE=59 m,
i.e. UEE=1 kV at short-sample (ISS=16.85 kA),
the quench protection is at the limit.
12 T
13 T
14 T
SS

## Slide 35
Quench protection with 1 kV energy extraction with constant resistor
The presence of quench-back influences significantly the transient
Reduction of differential inductance
Quench-back (coil resistance increase due to transient losses)
LEDET
hot-spot (lowest field location in the outer layers)