## Slide 1: Cryogenic pulsating heat pipes for efficient cryocooler-based HTS magnets
Speakers: Quentin Gorit1,2, Cees Maris1,2 and Carolin Zoller1
Co-authors: André Brem1, Michal Duda1, Henrique Garcia Rodrigues1, Jaap Kosse1, Rebecca Riccioli1, Stéphane Sanfilippo1, and Yannik Studer1
PSI CAS Seminar, Villigen, 26 June 2025
1) Department of Accelerator Technology, Paul Scherrer Institut, 5232 Villigen PSI, Switzerland
2) VDL ETG Technology & Development B.V., De Schakel 22, 5651 GH, Eindhoven, The Netherlands

## Slide 2: Outline
2
26.06.2025
PSI CAS Seminar
Context and motivation
Pulsating heat pipes
Experimental set-up
Characterization
Model and visualization
Application
Conclusion and outlook
Cryocooler-based test facility for superconducting magnets and advanced cryogenics

## Slide 3
High energy demand of PSI Large Research Facilities
Strong contribution from resistive magnets to power consumption (HIPA 2.6 MW, 26 %)
Aim: magnet performance ↑ energy demand ↓
Example SLS SLS2:
  Higher performance
  Magnet energy consumption reduced by ~60% using permanent magnets
Context: PSI Large Research Facilities

## Slide 4
High energy demand of PSI Large Research Facilities
Strong contribution from resistive magnets to power consumption (HIPA 2.6 MW, 26 %)
Aim: magnet performance ↑ energy demand ↓
Example HIPA (IMPACT=HiMB+TATTOOS):
  Higher performance
  HiMB energy consumption increased by factor 6
    70 % of the power comes from special radiation-hard cables
    Permanent magnets not possible due to radiation
    Important to find other solutions in high radiation environment
    Idea to use high temperature superconducting (HTS) magnets
MgO
Cu
Context: PSI Large Research Facilities

## Slide 5: Context: High temperature superconducting (HTS) magnets
Typically made of rare-earth barium copper oxide (ReBCO)
No ohmic losses in superconducting state saving energy consumption during operation
Operating temperature depending on field strength and current density, typically 10…50 K
Challenges:
  Radiation damage to superconductor and insulation
  Fast change of magnetic field (AC losses)
  Cooling
  SMILE initiative
Liquid bath Forced flow Cryocooler
Cryocooler
Superconducting coil
Copper bars and braids
Courtesy B. Baudouy
5
26.06.2025

## Slide 6: Context: SMILE initiative
Aim of PSI SMILE (Superconducting Magnets to Improve Large Research Facility Efficiency):
  Improve the performance of superconducting AC and DC magnets with/without radiation
  Develop smart cryogenic systems integrated with highly efficient cryocoolers
6
26.06.2025
PSI CAS Seminar
For Pulsating Heat Pipe (PHP) project, established collaborations with:
  VDL ETG (since 2023): Design and manufacturing, characterization, application
  VDL ETG, PSI NES and IUSTI/Aix-Marseille University (since 2024): Visualization and modelling

## Slide 7: VDL ETG at Park Innovaare
7
26.06.2025
PSI CAS Seminar
VDL Enabling Technologies Group:
A global development and manufacturing company, in the field of high-tech systems and modules which designs, develops, manufactures, and produces complex components and systems.
Semiconductor Capital Equipment
Medical Equipment
Space
Analytical Equipment
Science & Industry

## Slide 8: VDL ETG at Park Innovaare
8
26.06.2025
PSI CAS Seminar
R&D in advanced cryogenics:
Development of pulsating heat pipes (PHP) for an efficient, lightweight, passive, autonomous thermal link and switch operating in no-gravity, high-magnetic-field and high-radiation environments.
R&D in magnetic measurements:
Development of magnetic field measurement methods, for precise and industrial magnetic lens validations
Contact our people at PiA for your project Engineering, Modeling and Manufacturing!

## Slide 9: Motivation
Trend: Cryocoolers increasingly favored over traditional immersion bath cooling for superconducting (SC) components
Challenge: Transport heat efficiently, with possibility of thermal switch, from SC coil or current leads to cryocooler
State of the art: Copper links (heavy, bulky)
?
Copper braids
Copper blocks
Cryocooler
SC coil
9
26.06.2025

## Slide 10: Motivation
Trend: Cryocoolers increasingly favored over traditional immersion bath cooling for superconducting (SC) components
Challenge: Transport heat efficiently, with possibility of thermal switch, from SC coil or current leads to cryocooler
State of the art: Copper links (heavy, bulky)
PHP
Cryocooler
SC coil
Proposed solution:
  Use pulsating heat pipes (PHP) filled with neon (for HTS) or helium (for LTS)
  Principle:
  Transfer heat from “warm” evaporator to cold condenser using two-phase flow
latent heat (enthalpy of phase change) +
sensible heat (advection and convection)
10
26.06.2025

## Slide 11: Outline
11
26.06.2025
PSI CAS Seminar
Context and motivation
Pulsating heat pipes
Experimental set-up
Characterization
Model and visualization
Application
Conclusion and outlook
Cryocooler-based test facility for superconducting magnets and advanced cryogenics

## Slide 12: Literature on cryogenic PHPs
12
PHPs are experimentally studied under cryogenic conditions since 2007: ~50 papers and 2 PhD manuscripts from 8 different working groups (USA, China, Japan, France, India, Switzerland).
Maximum effective thermal conductivity of different PHPs from literature and comparison to copper thermal conductivity against temperature
Several orders of magnitude can be gained on the thermal conductivity of a thermal link by replacing solid copper by PHPs.
Neon is a promising working fluid for cooling HTS since it provides a good balance between PHP and superconductor performances.
Q. Gorit, J.C. Maris and C. Zoller, 2025, Experimental characterization of neon pulsating heat pipes for cryocooler-based HTS magnets. Cryogenics.
5th Superconducting Magnets Test Facility Workshop (SMTF 5)
26.06.2025

## Slide 13: PHP design features
Pipes:
Material: 316 L steel
Diameters:
for neon or for helium
Adiabatic length:
Number of turns: 10 or 20
Evaporator and condenser:
Material: High purity copper
Thickness:
Width:
Contact to tubes: Apiezon N grease
Evaporator cross-section
20-turn PHP
Condenser
Evaporator (lower half)
Pipes
Brazed connection
Pipe cross-section, courtesy of A. Brem, PSI
13
26.06.2025
PSI CAS Seminar

## Slide 14: Outline
14
26.06.2025
PSI CAS Seminar
Context and motivation
Pulsating heat pipes
Experimental set-up
Characterization
Model and visualization
Application
Conclusion and outlook
Cryocooler-based test facility for superconducting magnets and advanced cryogenics

## Slide 15: Experimental set-up for PHP characterization
15
DAQ
Cryostat
Gas supply rack
Mini gas rack
Cryocooler RDK-415D
wire feed-
throughs
26.06.2025
PSI CAS Seminar

## Slide 16: Parametric study on neon PHP
16
26.06.2025
PSI CAS Seminar
Three configurations:
10-turn PHP alone
20-turn PHP alone
2 x 10-turn PHP in parallel
Parametric study:
Heat load: 2.0 to 22.8 W
Filling ratio: 15 to 90 %
Condenser temperature: 27 and 30 K
Number of turns: 10 and 20
10- turn
20- turn
2 x 10- turn
Notes: Temperature and pressure evolution during 20-tube PHP operation with condenser temperature at 27 K and 55 % of liquid filling ratio

## Slide 17: Outline
17
26.06.2025
PSI CAS Seminar
Context and motivation
Pulsating heat pipes
Experimental set-up
Characterization
Model and visualization
Application
Conclusion and outlook
Cryocooler-based test facility for superconducting magnets and advanced cryogenics

## Slide 18: Exemplary cooldown
Condenser
PHP tubes
(adiabatic part)
Evaporator
18
26.06.2025
PSI CAS Seminar
Notes: Temperature and pressure evolution during cooldown with condenser temperature at 27 K and 16 % of liquid filling ratio

## Slide 19: Exemplary characterization
19
Condenser
PHP tubes
(adiabatic part)
Evaporator
26.06.2025
PSI CAS Seminar
Notes: Temperature and pressure evolution during 20-tube PHP operation with condenser temperature at 27 K and 55 % of liquid filling ratio

## Slide 20: Parametric study results
20
26.06.2025
PSI CAS Seminar
Thermal resistances
Optimum parameters
Thermal resistance in function of the heat load at different condenser temperatures and filling ratios for; (a) the 5-turn PHP, (b) the 10-turn PHP and (c) the two 5-turn PHPs in parallel.
2x10-turn in parallel, filling ratio of 35 % and condenser temperature of 27 K
These conditions lead to the lowest evaporator temperatures with thermal resistances ranging from 0.15 to 0.29 K.W-1, while no dry-out phenomena occur in the input heat load range tested
Dry-out
Notes: Temperature and pressure evolution during 20-tube PHP operation with condenser temperature at 27 K and 55 % of liquid filling ratio

## Slide 21
21
26.06.2025
Parametric study results
Frequency analysis
Aim: Determine the dominant frequency of oscillation motion using the pressure signal obtained at each pseudo-steady state.
Method: Calculate the continuous wavelet transform and the wavelet power spectrum of the sample period using Matlab software.
Main result: High dominant frequencies and low thermal resistances measured at 35 and 55 % of filling ratios support the assumption of enhanced sensible heat transfer due to greater fluid movement in these conditions.
Dominant frequency of pressure signal in function of the heat load at different condenser temperatures and filling ratios for; (a) the 10-turn PHP and (b) the two 5-turn PHPs in parallel.
Notes: Temperature and pressure evolution during 20-tube PHP operation with condenser temperature at 27 K and 55 % of liquid filling ratio

## Slide 22
22
26.06.2025
PSI CAS Seminar
Parametric study results
Comparison between the power-law correlation results and those of the experiments.
An empirical correlation for the heat transfer is determined using the appropriate dimensionless numbers and 139 experimental data points obtained from the individual characterizations of the 10-and 20-turn PHPs.
The average standard deviation of and about 10.5 % where 93.5 % of deviations are within 30 %. It seems that the correlation can reasonably predict the input heat flux for the different condenser temperatures, filling ratios and turn numbers.
where
The Kutateladze number can be expressed following an exponential relationship:
where
Correlation
Notes: Temperature and pressure evolution during 20-tube PHP operation with condenser temperature at 27 K and 55 % of liquid filling ratio

## Slide 23: Outline
23
26.06.2025
PSI CAS Seminar
Context and motivation
Pulsating heat pipes
Experimental set-up
Characterization
Model and visualization
Application
Conclusion and outlook
Cryocooler-based test facility for superconducting magnets and advanced cryogenics

## Slide 24: Neon PHP modelling
24
26.06.2025
PSI CAS Seminar
Collaboration with experts from CNRS/IUSTI on two-phase flow CFD modelling
CryoPHP numerically studied since 2017:
only 12 papers and 1 PhD manuscript on the subject but no publication on neon PHP modelling
No analytical framework allows to analyze the PHP physics
at cryogenic temperatures
PHPs designs are generally based on empirical correlation techniques
Unreliable
Solution for the prediction of their behavior: use numerical models
The Volume Of Control (VOF) numerical scheme and the Lee model are used for simulation of the 2D two-phase flow in Ansys Fluent:
The next step is the model validation by comparing thermal resistances obtained with models and experiments.
Liquid volume fraction in a single turn neon PHP at Tcond=27 K, FR=55 %,=5 W.

## Slide 25: Neon PHP visualization
25
26.06.2025
PSI CAS Seminar
Collaboration with experts on two-phase flow visualization from PSI/NES
No publication on visualization of the two-phase flow in transparent neon PHP
Experimental visualization of the two-phase flow in transparent PHP is an important step for improving and validating models.
Obtain the flow characteristics captured using a high-speed camera and a code for image processing to study the:
Evolution of flow patterns (bubbly, slug, churn, annular and mist flows)
Vapor and liquid interfaces (filling ratio)
Liquid film thickness
Fluid motion (velocities, dominant frequencies of oscillation motions)
Relationship between flow and heat transfer
Y. Shi, Visualized investigation of a nitrogen pulsating heat pipe, 2024.
Transparent 10-turn neon PHP

## Slide 26: Outline
26
26.06.2025
PSI CAS Seminar
Context and motivation
Pulsating heat pipes
Experimental set-up
Characterization
Model and visualization
Application
Conclusion and outlook
Cryocooler-based test facility for superconducting magnets and advanced cryogenics

## Slide 27: Experimental set-up for PHP application to non-insulated HTS coil
27
DAQ
Cryostat
Gas supply rack
Mini gas rack
Cryocooler
RDK-418D
Cryocooler
RDK-500B
Water cooled copper leads
Power supply
wires feedthroughs
26.06.2025
PSI CAS Seminar

## Slide 28: Exemplary application to non-Insulated HTS coil
28
HTS coil: ReBCO non insulated pancake
Current ramps of 1 A/s : I= 0 to 100 A and 100 to 120 A
Current, temperature and thermal resistance measurements:
keff= 156.5 kW.m-1.K-1
= 12.1 W
= 18.2 W
Status: Cooling and operating an NI HTS coil using two neon PHP in parallel has been performed.
kCu,RRR=100= 2.3 kW.m-1.K-1
Condensers
Evaporators
Coil
26.06.2025
PSI CAS Seminar
Results:
1st test: Heat loads too high
(PHPs operated well, high resistance of aluminum supports, changed for pure copper)
2nd test: Heat loads too low
(PHPs cold but not started-up, no possibility to increase current for safety reasons)
Neon PHPs: condenser at 27 K and filling ratio at 35%

## Slide 29: Experimental set-up for PHP application to insulated HTS coil
29
26.06.2025
PSI CAS Seminar
DAQ
Cryostat
Gas supply rack
Mini gas rack
Cryocooler
RDK-418D
Cryocooler
RDK-500B
Water cooled copper leads
Power supply
wires feedthroughs
Main differences with insulated coil application:
The coil itself
Powering in AC and not DC mode
Stycast for electrical insulation located between the coil and the cryocooler instead of between the coil and the PHP
PHPs in parallel are operated individually instead of connected to the same external reservoir

## Slide 30: Exemplary application to insulated HTS coil
30
HTS coil: ReBCO insulated pancake
Status: first test of cooling and operating an insulated HTS coil using two neon PHP in parallel has been performed.
Condensers
Evaporators
Coil
26.06.2025
PSI CAS Seminar
Cooldown: After charging neon, it takes less than 2 hours to cool the coil from 100 to 27 K
Neon PHPs: condenser at 27 K and filling ratio at 35%

## Slide 31: Exemplary application to insulated HTS coil
31
HTS coil: ReBCO insulated pancake
Current ramps of 350 A/s : I= 0 to 500 A during 500 cycles
Condensers
Evaporators
Coil
26.06.2025
PSI CAS Seminar
Neon PHPs: condenser at 27 K and filling ratio at 35%

## Slide 32
32
26.06.2025
PSI CAS Seminar
Current and magnetic field measurements:
Voltages measurements and differentiation:
AC losses post-processing:
Exemplary application to insulated HTS coil
Inductance: measured using slow ramps
Voltage:
Instantaneous dissipated Power:
Total dissipated energy:
Dissipated power per cycle:
Dissipated energy per cycle:
W

## Slide 33: Simplified model for comparison with copper braid
33
26.06.2025
PSI CAS Seminar
Results comparison:
Model description:
Energy equation:
Boundary conditions:
Initial conditions:
Numerical solution:
Explicit Euler method
Proof of concept:
Heat loads in the range of PHP operation (starting-up to dry-out)
Thermal conductivity of the link increased by a factor 54 compared to a copper braid of the same dimensions
Coil temperature margin increased of 4.5 K compared to a copper braid of the same dimensions
Tcond | FR | Imax | dI/dt
27 | 35 | 500 | 200
27 | 35 | 500 | 350
27 | 55 | 500 | 200
27 | 55 | 500 | 350
30 | 35 | 500 | 200
30 | 35 | 500 | 350
30 | 55 | 500 | 200
30 | 55 | 500 | 350
Experiments in post-processing:
Repeat the tests replacing PHPs by copper braids of the same dimensions for experimental validation
Next experiments:
keff= 123.8 kW.m-1.K-1
kCu,RRR=100= 2.3 kW.m-1.K-1

## Slide 34: PHP foreseen applications to accelerator magnets
34
26.06.2025
PSI CAS Seminar
High field
High radiation environment
Fast ramping
Current leads
High reliability
Influence of magnetic field on evaporation and potential cryocooler damage
Nuclear load and potential cryocooler damage
Cryocooler redundancy
High AC losses
Bulky and heavy
Require reliable thermal switches
Require long length thermal link
Require efficient thermal link
Require compact thermal link
Require thermal link working without gravity
Main advantages: Passive, efficient, possibility to operate without gravity and to be used as thermal switch.
These can be used to gain on weight, bulk, reliability and electricity consumption.
Pulsating heat pipe
Applications
Application
Problematics
Solutions

## Slide 35: Outline
35
26.06.2025
PSI CAS Seminar
Context and motivation
Pulsating heat pipes
Experimental set-up
Characterization
Application
Model and visualization
Conclusion and outlook
Cryocooler-based test facility for superconducting magnets and advanced cryogenics

## Slide 36: Conclusion
36
Neon and helium PHPs designed and manufactured
Experimental setup dedicated to PHP characterizations and applications built at PSI
Characterization of 3 configurations of neon PHP, leading to optimal parameters definition and correlations to predict their performances
First ever application of neon PHP to cool down and operate non-insulated and insulated HTS coils, leading to a proof of concept for replacing conventional copper braids
First ever CFD model of neon PHP in development for improvement of performance predictions
First ever neon PHP visualization in development for accurate validation of the CFD model
PSI CAS Seminar
26.06.2025
Neon PHP is a very promising candidate for optimizing the cooling of cryocooler-based HTS magnets

## Slide 37: Outlook for 2025-2027
37
26.06.2025
PSI CAS Seminar
Characterization:
Parametric study on the effect of internal diameter (helium, neon)
Investigate different orientation and shapes: horizontal orientation, coil shape, L-shape…
Model:
Validate the models of 10 and 20-turn Ne PHP with the characterization and visualization results
Extend the model from 2D to 3D
Model the HTS coil with neon PHP and validate with the application results
Model a HTS magnet with embedded PHP in operation and quench
Visualization:
Characterize transparent neon PHP without visualization
Modify test facility for visualization
Perform the visualization campaign
Post-process images
Application:
Improve actual design by displacing the electrical insulations of the coil
Use PHP as thermal switches with 2 cryocoolers for redundancy and improved reliability
Cool and operate CORC coil with neon PHP
Cool and operate NbTi coil with helium PHP
Use embedded neon PHP in a high field or high radiation environment superconducting magnet

## Slide 38: Thank you for your interest
Q. Gorit1,2, C. Zoller1, J.C. Maris1,2
PSI CAS Seminar, Villigen, 26 May 2025
We would like to thank:
PSI CAS and VDL ETG for their ongoing commitment
PSI magnet section and CHART team for support
PSI technicians for support in manufacturing, assembly and, vacuum-, volume- and pressure tests
38