## Slide 1
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program, http://chart.ch.
MagDev
D. Araujo, B. Auchmann, A. Brem, M. Crescenti, M. Duda, N. Kehl, J. Kosse, C. Lindner, T. Michlmayr, C. Müller, I. S. P. Peixoto, K. Puthran, H. Rodrigues, J. Schmidt, D. Sotnikov, A. Stampfli, J. Van den Eijnden
CHART Workshop 2025, 12 November, 2025
HFM
High Field Magnets
Programme

## Slide 2
MagDev LTS Status and Plans

## Slide 3: MagDev Laboratory
Inês S. P. Peixoto
Magnet Engineer
Alejandro Carlòn Zurita
Technician HTS, CAD
Douglas Araujo
Engineer LTS
Henrique Rodrigues
Process Engineer ReBCO
Dmitry Sotnikovs Design Engineer ReBCO
André Brem
Material Scientist
Thomas Michlmayr
CAD, Technical Design
Colin Müller Mechanic LTS
Jaap Kosse
Engineer ReBCO
Anna Stampfli
Technician Processes
Jürgen Schmidt
Technician HTS
Joep Van den Eijnden
PhD Student
Christina Lindner
Technician HTS
Matteo Crescenti
PhD Student
Kirtana Puthran
Engineer ReBCO
Nicolas Kehl
Technician LTS

## Slide 4: Fast-Turnaround Stress-Management R&D
Materials and Composite Samples (not powered)
Powered Samples and Mechanical Models
Sub-scale Magnets (5 T)
Short Magnets Ultimate Field (14…16T)
Long Magnets Ultimate Field Magnets (14…16 T)
2019
2020
2024
First deliverable
100s
10
2-3
0.5-1
#Deliverables / year
Long-magnet infrastructure available only at CERN.
2025/26
Goal: Build industrializable Nb3Sn high-field magnets that “just work”.

## Slide 5: BOX Program
BOX (BOnding eXperiment) program with uTwente has shown a wide variety of results, from complete conductor degradation (no impregnation) to substantial training (epoxy) to no-training (wax, Stycast, filled wax), with 20 BOX samples successfully and tested to date.
Courtesy, A. Brem, S. Otten
Pictures by M. Daly, S. Sidorov, S. Otten
11-T solenoid
SC Transformer

## Slide 6: Compression BOX
Courtesy S. Ott et al.
Courtesy M. Daly
Four tests with filled wax and three different cables.
cBOX6 performance equivalent to epoxy.
High-field cable of PSI high-field magnet demonstrator performs very well!
Courtesy, A. Brem, S. Otten

## Slide 7: Magnets Using Filled-Wax
11 T
10 T
9 T
8 T
7 T
CCT5w in LBNL (D. Arbaleaz, at HFM forum)
PSI/BNL BigBOX: a 13-turn SM racetrack.
No training at 12.3 T, 170 MPa with wax Filled-wax BigBOX2 awaiting test at BNL’s DCC17 test station.
LBNL sub-scale CCT (5 T) .
First Nb3Sn CCT without training. Alumina-filled wax subCCT with a single training quench.
PSI subSMCC1 and 2 2-in1 dipole (5T)
Nb3Sn common coil R&D magnet without training at 4.5 K. Support from LBNL/CERN.
LBNL CCT5w, re-build of CCT5, replacing epoxy by filled wax.
Magnet reached short sample current at 4.5 K and 1.9 K.
Next up: LBNL CCT6 and PSI’s SMACC1

## Slide 8: Wax Irradiation Tests at CERN
Irradiation study in atmosphere for paraffin wax, filled paraffin wax, and filled high-melting-temperature High-Tm waxes.
High-Tm waxes show very encouraging performance up to 10 MGy (max. tested to date).
Study by Christian Scheuerlein (CERN) and André Brem (PSI), presented at HFM Forum, 06.11.2025, https://indico.cern.ch/event/1599118/

## Slide 9: MagNum
Modeling
Measurements performed at EHTZ by X. Kong and T. Tervoort
Characterization
Workflow

## Slide 10
Measurements
Measurements performed at Univeristy of Twente, S. Olten.
MagNum
Experimental Validation

## Slide 11: subSMCC1/2a
Subscale (5-T) Stress-Managed Common-Coil (subSMCC) magnet for process validation.
subSMCC2 has ESC protection coils

## Slide 12: SMACC1 Design
SMACC1 is nominally a 12-T demonstrator for the HFM Programme.
Coil stress at 13 T reaches 125 MPa in simulations.
The record field for a single-aperture accelerator magnets is 14.5 T (92% of SMACC1 short sample field).
cBOX results indicate that filled-wax + stress management may get us there.
BUT, this is the first time we test our technologies at the high-field frontier!

## Slide 13: SMACC1 Construction
Two high-field coils have been wound.
Yoke stacking completed – awaiting re-machining.
Procurement of all components started.

## Slide 14: subSMACC1
D. M. Araujo, I. S. P. Peixoto, et al. Combined System for Cryogenics and Protection of High-Field Superconducting Magnets, submitted to IEEE TAS, Oct. 2025.
I. S. P. Peixoto, D. M. Araujo, et al. Subscale Stress-Managed Asymmetric Common Coil Design, submitted to IEEE TAS, Oct. 2025.

## Slide 15: SMACC2
Hybrid Nb3Sn / Nb-Ti 14 T SMACC.
State-of-the art Nb-Ti wire from B-OST.
Mechanical structure and protection to be decided.
Testing foreseen for 2028.

## Slide 16: Exchange of Ideas within HFM Programme
MagDev ideas in HFM
CERN joining BOX program
CERN building filled-wax SMC
CIEMAT aims for an asymmetric common coil
CERN proposed building a long SMACC mirror magnet to the HFM Steering Board
Heat-resistant coating introduced at CERN
Interest in novel “bullet gauges” to supervise end supports
Recent HFM ideas in MagDev
CIEMAT’s hybrid Nb3Sn/Nb-Ti design adopted at CERN and PSI for SMACC2
CIEMAT’s horizontal-split structure considered for SMACC2
CERN’s ESC protection scheme tested on subSMCC2
In addition to the above, MagDev builds upon decades of CERN and US-LARP R&D in Nb3Sn magnets.

## Slide 17
MagDev HTS Status and Plans

## Slide 18: UFOs in the FCC-hh?
UFOs in the LHC are dust particles in the beam pipe that
  get ionized
  get pulled into the beam via electric field
  cause particle showers and get ionized to opposing charge before being ejected from the beam.
The particle showers deposit energy in the magnet coils and can quench magnets.
R~10 µm

## Slide 19: UFOs in the FCC-hh?
For FCC-hh beam energy, we expect >30x higher energy deposition in the coil for a given UFO particle.
At the same time, due to the absence of superfluid helium inside the coil, the enthalpy margin drops ~2x.
As a result, smaller UFOs can cause a quench.
The prevalence of UFOs in the beamscreen has been found to scale 1/V2. and FCC-hh has ~4x longer arcs.
If we need 70 to 100x higher enthalpy margins  do we have to operate at 20 K?
LHC MQED with HeII: 15-20 mJ/cm3

## Slide 20: Main Challenges with ReBCO
Ramp losses and field quality
  LTS wires have filament sizes of few microns (Nb-Ti) to 50 µm (Nb3Sn).
  ReBCO tapes are 2-12 mm wide. Screening currents and associated ramp losses are substantially increased.
  Tape orientation matters!
High-current, low-loss cables with windability
  Do we need full transposition (every tape in a cable ”sees” the same field, inductive loops are shortened)?
  Can we pre-fabricate a cable, or do we need to assemble and insulate it “on the fly” during winding?
  Can the cable withstand pressure of 400+ MPa?
[J. v. Nugteren, High Temperature Superconductor Accelerator Magnets. PhD thesis, UTwente, 2016.]
[Courtesy G. Kirby, J. v. Nugteren, J. S. Murtomäki, et al.]

## Slide 21: HTS technology for HEP is at the level of 1970s LTS technology
[J. v. Nugteren, High Temperature Superconductor Accelerator Magnets. PhD thesis, UTwente, 2016.]
[M. Wilson, Pulsed Superconducting Magnets' CERN Academic Training May 2006]
Early options of cables for main dipoles in Isabelle accelerator at BNL:
Braided cable failed in series manufacturing.
Rutherford-cable development arrived too late, but underpinned Nb-Ti accelerators:
Tevatron (1983), Hera (1991), RHIC (2000), (SSC), LHC (2008)

## Slide 22: Dynamic Effects
HFM-PUB-RPT-0267 v.1 "Deliverables KE5943 / PSI-D2.1”, EDMS 3028682
Intense macroscopic screening current distribution.
The wide variability in tape properties and contact resistances, adds on the challenge related to field reproducibility as well as stability.
Notes: For LHC field sweep at injection energy

## Slide 23: Field stability
For comparison: An LHC dipole magnet has 2 10-4 in main field distortion due to persistent current magnetization. The REBCO dipole has 200 10-4 in field missing, with a drift by 50 10-4 units over a 1000 s plateau.
Every variation in tape/manufacturing parameters is, accordingly, amplified see Prof. Carmine earlier presentation (https://indico.cern.ch/event/1455509/contributions/6586182/).
HFM-PUB-RPT-0267 v.1 "Deliverables KE5943 / PSI-D2.1”, EDMS 3028682
Ironless

## Slide 24: REBCO Block-Coil Dipole Scaling Exercise
As expected, AC losses grow non-linearly with field due to larger field sweep and growth in coil-size.
In this exercise AC losses increase 4-fold from 14 to 20 T.
HFM-PUB-RPT-0267 v.1 "Deliverables KE5943 / PSI-D2.1”, EDMS 3028682

## Slide 25: REBCO FCC-hh Dipole Scaling Exercise
Analogue study for scaling with temperature (5-30 K) for constant 14 T bore field indicates weak scaling of AC losses, notable cost increase.
HFM-PUB-RPT-0267 v.1 "Deliverables KE5943 / PSI-D2.1”, EDMS 3028682

## Slide 26: AC Losses in Context
Presentation by A. Verweij (CERN) at HiTAT2, 23-24 Oct., 2025, https://indico.cern.ch/event/1455509/
Break-even with basline Nb3Sn, 14 T in 1.9 K at ~17 T.

## Slide 27: After all, the price of REBCO is bound to keep falling ..
    [A. Molodyk, https://indico.cern.ch/event/1347361/ (2025)]
    [B. Song, et al., https://indico.cern.ch/event/1347361/ (2025)]

## Slide 28: ReBCO Subscale 1 (RS1) - Cable
Insulated cable illustration 5 turns - block
RS1 magnetic simulations performed by D. Sotnikov
Param | Current | Bpeak | Bbore | Inductance | Emag | % of Ic
Value | 7.0 | 4.8 | 3.9 | 388 | 30.6 | 85
Unit | kA | T | T | uH | kJ/m | -
Protection studies performed @ PSI and CERN (M. Wozniak et al.)

## Slide 29: RS1 - Cable and Coil Manufacturing
Insulating and
winding tools
Tape supply
Set-up developed by C. Linder and colleagues
Co-winding copper tape reel
Pusher roller and Insulating tool
Coli former
HTS-cable
Applying soldering paste and flux
Pocket for voltage taps
Soldering with thick plate, pre-heated with oven. Tcoil = 194 °C.
Process developed by A. Stampfli and colleagues

## Slide 30: RS1 – Impregnation, splicing and assembly
Impregnation set-up: heaters for the box
Cooling plate
Temperature sensors for box, former and cooling circuit
The coil dries overnight
The wax is injected under vacuum when the mold is at 80 to 90 °C
After 3 cycles (vacuum to atmospheric pressure), the cooling circuit is activated
View of inner splicing process: heater and cable
12 mm-based tapes and copper sheet used as shunt between the layers
Support frame
Connection leads for powering
Connection leads for powering
Cooling copper plates inner splice
Connection outer splice
Cooling copper plates inner splice
Clamping device of the coil pack

## Slide 31: LN2 Test Results: Magnetic field
First measurements on a pair of coils in LN2 indicate the presence of strong screening currents.
RS1 magnet test at CERN expected for Q1 2026.
2 cycles: 400 A x 5 and 410 A + 400 A x 5
Normalized to max field

## Slide 32: Next step: REBCO Subscale 2 - RS2
Field-angle optimized coil geometry
High-field coils wound cos-theta style between the apertures, where each block of windings in the high field follows a path like a midplane block in a cos-theta dipole, but with elliptical ends
Low-field turns wound common-coil style
Two winding positions (0° and 90°); intermediate positions are being implemented to improve field alignment.

## Slide 33: REBCO Subscale 3 - RS3
Explore a REBCO SMACC (re-use parts of Nb3Sn SMACC1) with twisted striated cables.
N. Amemiya et al., “Effective reduction of magnetisation losses in copper-plated multifilament coated conductors using spiral geometry,” doi: 10.1088/1361-6668/ac3f9c.
RS2 Could be wound with tape-stack cable or Roebel
https://indico.cern.ch/event/489475/contributions/1166833/attachments/1263291/1868932/
Courtesy of A. Kario et al..

## Slide 34: REBCO Subscale 3 - RS3
Explore a REBCO SMACC (re-use parts of Nb3Sn SMACC1) with twisted striated cables.
Drawing of A. Carlón Zurita
Modeling of REBCO twisted striated – based cables
Modeling: Inês S. P. Peixoto
Notes: Add link to Amemiya, twente

## Slide 35
Synergies

## Slide 36: MagMu – Materials for a 40 T Muon Collider Solenoid
Study tunable partial insulation and metal-insulator switching materials:
Combine the advantages of insulated coils with the stability and protectability of no-insulation coils.
Pedot:Pss
measured @ PSI & Unige with R. Babouche
Courtesy Matteo Crescenti

## Slide 37: SINQ and SLS2.0
High field solenoids for high-magnetic-field user facilities and increased physics reach in experiments.
3.6 cm
Compact solenoid for 6-T on target in the manipulator head for Resonant inelastic X-ray scattering (RIXS) in ACCESS2.0 beamline of the Swiss Light Source.
10 mm
18-T split solenoid for SINQ (Swiss Spalliation Neutron Source)

## Slide 38: Small HTS Magnets for Quantum Material Research
Equip commercial AttoDry systems at ZHAW and ETHZ with NI coils and cryogenic power converters.
Increase the experimental field from currently 0.6 T to 1-3 T.
Additional interest for HTS magnets at D-PHYS: Penning-trap quantum computing and energy-saving accelerator-mass-spectroscopy at LIP.
Courtesy J. Huber, D. Zang

## Slide 39: Proxima Fusion Collaboration
HEP success story attracts Munich startup to perform conceptual design and process development directly on the PSI campus.
Framework agreement, covering conceptual design, signed in June 2024.
Three project agreements signed.
  Collaboration startup in MagDev laboratory 2024/25
  400 m2 laboratory on campus 2025/26,
  1100 m2 laboratory in Kleindöttingen 2026/27,
  to date 20 Proxima employees in Argovia.

## Slide 40: In summary, we need to
Demonstrate 14 T LTS magnets with an emphasis on cost and manufacturability.
Develop technology towards accelerator-quality REBCO magnets.
Realize the important synergies with PSI and Swiss academia.