## Slide 1: Progress of a meter-long bulk high-temperature superconducting undulator
Alexandre Arsenault
November 12, 2025

## Slide 2
Introduction
By
Permanent magnets
Fe poles
Undulator period
gap
Electrons
Synchrotron radiation is achieved with the use of oscillating electrons, typically produced by undulators

## Slide 3
Introduction
By
HTS bulks
Ho poles
Undulator period
gap
Electrons

## Slide 4
Introduction
By
HTS bulks
Ho poles
gap
Electrons
Solenoid

## Slide 5
Introduction
Managed to get good experimental results on a 10 cm prototype
Next step, 200 bulks!

## Slide 6
Introduction
Managed to get good experimental results on a 10 cm prototype
Next step, 200 bulks!

## Slide 7: Outline
HTS undulator
Nb3Sn solenoid
HTS bulks insert
HTS bulks sorting
Conclusion

## Slide 8: Outline
HTS undulator
Nb3Sn solenoid
HTS bulks insert
HTS bulks sorting
Conclusion

## Slide 9: HTS undulator
Preliminary design of the full undulator

## Slide 10: HTS undulator
HTS insert

## Slide 11: HTS undulator
HTS insert cooling

## Slide 12: HTS undulator
Solenoid cooling

## Slide 13: HTS undulator
Aluminium thermal shields cooled by 1st stage cryocoolers

## Slide 14: Cryostat

## Slide 15: Outline
HTS undulator
Nb3Sn solenoid
HTS bulks insert
HTS bulks sorting
Conclusion

## Slide 16: Nb3Sn coil fabrication
Winding of glass fiber insulated Nb3Sn wire

## Slide 17: Nb3Sn coil fabrication
Assembly of copper sleeve

## Slide 18: Nb3Sn coil fabrication
Assembly of stainless steel outer shell

## Slide 19: Nb3Sn coil fabrication
Installation of copper sleeve and stainless-steel shell

## Slide 20: Nb3Sn coil fabrication
Installation of upper flange and anchorage for internal connections

## Slide 21: Nb3Sn coil fabrication
In-vacuum oven for thermal treatment

## Slide 22: Nb3Sn coil fabrication
Fabrication of internal and external joints

## Slide 23: Nb3Sn coil fabrication
Thermal treatment and in-vacuum epoxy impregnation

## Slide 24: Outline
HTS undulator
Nb3Sn solenoid
HTS bulks insert
HTS bulks sorting
Conclusion

## Slide 25: HTS bulks insert

## Slide 26: Strain measurement
Previously used aluminium outer shell to compress the disks
Need to measure the compression of copper shells on disks in liquid nitrogen

## Slide 27: Strain measurement
Previously used aluminium outer shell to compress the disks
Need to measure the compression of copper shells on disks in liquid nitrogen
Strain gauges

## Slide 28: Single direction melt growth
Grown 130 bulks using Single Direction Melt Growth (SDMG)
Cut each bulk in half and shrink-fit into copper sleeves, yielding 260 pieces
Produced 250 holmium poles
Coated in 300 nm silver
Antončík F, et al. J Am Ceram Soc. 2024; 107: 2668–2678. https://doi.org/10.1111/jace.19566

## Slide 29: HTS bulks insert
Grown 130 bulks using Single Direction Melt Growth (SDMG)
Cut each bulk in half and shrink-fit into copper sleeves, yielding 260 pieces
Produced 250 holmium poles
Coated in 300 nm silver

## Slide 30: HTS bulks insert
Field maps measured on seeded and non-seeded surfaces at 1 T and 77 K
6 out of 260 half-moon bulks had visible defects
(a)
1
1
2
2
3
3
4
4
5
5
6
6

## Slide 31: Outline
HTS undulator
Nb3Sn solenoid
HTS bulks insert
HTS bulks sorting
Conclusion

## Slide 32: HTS bulks sorting
Sorting the bulks experimentally leads to an error reduction of a factor of 3.2

## Slide 33: HTS bulks sorting
Sorting done by fitting experimental data to FEM simulation
For 200 bulks, one FEM simulation takes ~6 hours
Bulk HTS properties
FEM simulation
Local field integral (k)

## Slide 34: HTS bulks sorting
Made a machine learning model that takes ~200 ms to get the same FEM result
Machine learning model
Bulk HTS properties
Local field integral (k)

## Slide 35: HTS bulks sorting
Made a machine learning model that takes ~200 ms to get the same FEM result
Machine learning model
Bulk HTS properties
Local field integral (k)

## Slide 36: Outline
HTS undulator
Nb3Sn solenoid
HTS bulks insert
HTS bulks sorting
Conclusion

## Slide 37: Conclusion
Full design of HTS undulator complete
The solenoid is still under discussion
200+ GdBCO bulks have been made and embedded into copper
Produced a machine learning model to help with the magnetic field optimization

## Slide 38: Acknowledgements
PSI : M. Calvi, X.Liang, S.Hellmann, L.Huber, S.Reiche, M.Bartkowiak, C.Calzolaio, Prof. M. Stampanoni, Prof L.Patthey, F. Marone & G.Lovric
CAN: Tomas Hlasek, Filip Antoncik & Jan Plechacek
EUXFEL: T. Schmidt
CHART : Prof. H.R.Ott & Prof. L.Rivkin
Uni Cambridge : J.Durrell, A.Dennis, Y. Shi
King's College London: M.Ainslie
Spring8 : T.Ishikawa, M.Yabashi, H.Tanaka
UniKyoto : R.Kinjo, T.Kii, H.Ohgaki
Uni Malta : N.Sammut, A.Sammut, J.Cassar
SENIS : Prof.R.Popovic, S.Spasic, S.Dimitrijevic
KIT : Prof. M.Noe
Fermilab: C.Boffo, M.Turenne, F.McConologue, V.Martinez, J.Hayman
Zhangjiang lab: K. Zhang, D. Wei

## Slide 39: Magnetic field simulations
Split the solenoid into 4 coils
Calculated field uniformity of 1.12% within a radius of 15 mm
Field near 12 T with a nominal current of 235 A
z

## Slide 40: Mechanical analysis
FEM simulations show that a support is needed to reduce strain
SS304 outer shell was the best candidate found
Inconel 308 mandrel reduced strain further, but requires pre-load at room temperature
Reference “zero” strain after cool-down
No support, cooling
No support, powering
SS304 shell, powering
SS304 shell and Inconel 308 mandrel, powering

## Slide 41: Mechanical analysis
FEM simulations show that a support is needed to reduce strain
SS304 outer shell was the best candidate found
Inconel 308 mandrel reduced strain further, but requires pre-load at room temperature
Reference “zero” strain after cool-down
No support, cooling
No support, powering
SS304 shell, powering
SS304 shell and Inconel 308 mandrel, powering

## Slide 42: Mechanical analysis
FEM simulations show that a support is needed to reduce strain
SS304 outer shell was the best candidate found
Inconel 308 mandrel reduced strain further, but requires pre-load at room temperature
Reference “zero” strain after cool-down
No support, cooling
No support, powering
SS304 shell, powering
SS304 shell and Inconel 308 mandrel, powering

## Slide 43: Mechanical analysis
FEM simulations show that a support is needed to reduce strain
SS304 outer shell was the best candidate found
Inconel 308 mandrel reduced strain further, but requires pre-load at room temperature
Reference “zero” strain after cool-down
No support, cooling
No support, powering
SS304 shell, powering
SS304 shell and Inconel 308 mandrel, powering

## Slide 44
Introduction
HTSU field cool magnetized at 10K in a field of 10T

## Slide 45
Introduction
To increase the flux and energy of synchrotron radiation, higher magnetic fields and lower undulator period
SmCo @300K
Nb3Sn @ 4.2K
NbTi @ 4.2K
PrFeB @77K
magnetic gap = 4mm
HTS