## Slide 1: “Renaissance wax”: Recent results of alumina-filled paraffin wax system
Organisationseinheit verbal optional auf 2 Zeilen
Xiang Kong1, Joep Van den Eijnden1,2, André Brem2, Douglas Martin Araujo2, Bernhard Auchmann2,3 , Theo A. Tervoort1
Department of Materials, ETH Zürich, Switzerland
Paul Scherrer Institution (PSI), Villigen, Switzerland
CERN, Geneva, Switzerland
November 12, 2025
CHART Workshop 2025 for the 10-year anniversary of CHART

## Slide 2: Introduction
Extreme operating conditions:
Cryogenic temperatures
High stresses due to large Lorenz forces
High radiation exposure
CERN website
Insulation material
Rutherford cables
20 mm
15 mm
15 mm
Transverse
Radial
Axial
Daly et al. 2018
10-stack cable
Ferracin et al. 2015
Common coil
Future circular collision (FCC) project

## Slide 3: MagRes: epoxy materials with high toughness at cryogenic temperatures
Epoxy resin system development
Low viscosity (good impregnation)
Long “pot life” (slow curing reaction)
Moderate stiffness at RT (Tg > RT)
Tg slightly above room temperature to reduce built-up of thermal stresses (RT < Tg < 100°C)
High fracture toughness at LN2
Studer et al. 2024, Cryogenics 143-103923.
Studer P. 2025, ETH doctoral thesis: Design of Epoxy Resin Insulation Materials for Cryogenic Applications.

## Slide 4: New insulation materials
Daly et al. 2021, Supcon. Sci. Tech. vol 34.
Daly et al. 2022, Supcon. Sci. Tech. vol 34.
Araujo et al. 2024, IEEE Trans. Appl. Superconductivity, vol 34.
Araujo et al. 2025, IEEE Trans. Appl. Superconductivity, vol 35.
Daly et al. 2022
Daly et al. 2021
Magnet training
  Quench reasons:
  Frictional sliding  decrease surface adhesion
  Micro-cracking  increase Kic but this needs plastic deformation behind the crack tip, which increases training
Aims:
Tailored design of insulation materials for superconductor cables
Cryogenic testing to assess anisotropic mechanical response of Rutherford cables
Constitutive model development to support computational design of next-generation superconductors
  Stress-management common coil (SMACC) design
Notes: Impregnation requirement: 1) 2) 3)
  Friction  surface adhesion
  Fracture dissipation  higher K1c
BOX sample no training with wax system!
Stress-management common coil (SMCC) design

## Slide 5: Content
Materials: rigid epoxy vs. “soft” wax
Results: thermal, rheological and cryo-mechanical characterization
Conclusion & outlook

## Slide 6: MagComp: Alumina-filled wax system
Brem et al. 2024, IEEE Trans. Appl. Superconductivity, vol 34-5.
5% Carnauba wax  particles better dispersed in the matrix
Filled wax system
Chart: 
| Alumina | Parrafin wax | Carnauba wax
vol.% | 45 | 50 | 5
Chart: 
| Alumina | Parrafin wax | Carnauba wax
vol.% | 78.1 | 19.7 | 2.2
volume
Al2O3 particle
Highly filled system (45%)
Mixed wax system
Chart: 
| Parrafin wax | Carnauba wax
vol.% | 50 | 5
volume
POLARIT
Notes: Paraffin wax + carnauba wax + 45% alumina
SEM

## Slide 7: Thermal & rheological results
DSC: Tmelt & Tc
CTE measurement
Immersed at LN2
Continuous cooling 2K/min from RT to 193K
Rheology: low viscosity
“shear thinning”
Melt viscosity < 1 Pa⋅s
Notes: Impregnation:
  processibility  Tm and low viscosity
  CTE match  avoid thermal strain/stress
DSC
TGA
CTE (!) relevant
Rheology

## Slide 8: SEM observation
Inter-strand impregnated insulation
Sub-micrometer Al2O3 particles
Low melt viscosity  filled wax system well dispersed in magnets

## Slide 9: Cryo-mechanical results
20.2 GPa
7.6 GPa
E77K
3-point bending test
Uniaxial compressive test
σy = -0.338T + 110.7
Large scatter!
Epoxy resin (CTD101K)
Filled wax
Mixed wax
Fracture toughness test
Brem et al. 2021, Cryogenics 115-103260.
Studer et al. 2024, Cryogenics 143-103923.
Filled wax has larger stiffness at RT than epoxies due to Al2O3 fillers
Filled wax increases compressive strength and fracture toughness but less than for epoxy systems
Damage due to thermal shrinkage can lower fracture toughness.
Notes: Compression yield stress
Bending  modulus vs. temperature
Fracture toughness (!!!)

## Slide 10: Thermal shock: from RT to LN2
Thermal stresses arise from the CTE mismatch between wax and Al₂O₃, as well as from thermal gradients during cooling.
Due to the latter, a smooth cooling process is advantageous.
Mixed wax
Filled wax
After fast cooling to LN2 temperatures, thermal cracks occur in the mixed unfilled wax due to its high CTE and the large temperature gradient. No visible cracks are observed in the filled wax but a decrease in KIc is measured.
LN2 (77 K)
Mixed wax

## Slide 11: Damage mechanisms under uniaxial compression
Mixed wax at room temperature  Filled wax tested at -55°C (218K)
⌀6 mm
after @218K, 0.1/s
Classic 45° shear-band fracture is found at RT, while the vertical cracks are observed at -55°C (218K)

## Slide 12: Representative volume element simulation
RVE with 22 random particles (Vp=45%)
Plane strain condition
Particle size r/l = 0.085,
Mesh size 1%/l
Step 2: 3% compressive load at 77K
εvm (%)
45
40
35
30
25
20
15
10
5
0
Tensile stress + strain localization  fracture onset
Step 1: thermal contraction 328K  77K
εvm (%)
18
16
14
12
10
8
6
4
2
0
Hydrostatic
σh (MPa)
50
40
30
20
10
0
-10
-20
-30
-40
-50
εglobal ~ 2%
Hydrostatic
σh (MPa)
50
40
30
20
10
0
-10
-20
-30
-40
-50
Ux=0
Uy=0

## Slide 13: 10-stack cables: experiment - simulation (PSI) at 77K
Ceramic plate
Liquid nitrogen
(Tb = –196°C, 77 K)
Finite element modelling
Courtesy of J. Van den Eijnden

## Slide 14: Conclusion
Al₂O₃-filled wax system shows good mechanical and thermal performance at room and cryogenic temperatures, making it a promising insulation material for superconducting magnets.
Alumina fillers significantly enhance compressive strength and modulus and improve CTE matching, while the wax composition maintains a low viscosity.
The effect of thermal-stress is investigated via a simplified RVE model, that elucidates the mechanism of damage and stress evolution during thermal contraction and mechanical loading.
Unpublished data and under preparation for submission soon.

## Slide 15: Acknowledgment
Thank you for your attention!
Jan Vermant, Kirill Feldman, Elena Tervoort, Chris Furrer
MagRes
MagComp

## Slide 16: TGA test

## Slide 17: GPC high temperature: molecular weight distribution
Sample | Mp | Mn | Mw | Mz | Mz+1 | Mv | PDI
Paraffin wax | 553 | 468 | 558 | 642 | 763 | 546 | 1.192
Carnauba wax | 1711 | 1017 | 1587 | 2215 | 3139 | 1506 | 1.560
PC wax | 566 | 486 | 616 | 793 | 1106 | 595 | 1.267

## Slide 18: Representative volume element (RVE) simulation
CTE measurement
3-point bending test

## Slide 19: Multiscale structure
10-stack cable
Cubic level
Nb3Sn filament
Copper matrix
Void
Filament level
~15 mm
~ 1 mm
~700 μm
~50 μm
Ebermann et al. 2018
Epoxy resin
Strand
Insulation
Stainless-steel core
Stack level
Copper matrix
Nb3Sn micro filaments
Strand level
Ebermann et al. 2018, Supercond. Sci. Technol. 31 (2018) 065009
Rutherford cable stack
Vallone, MDP Meeting 2022
20
15
15
Notes:  Mechanical compressive testing