## Slide 1: Electromechanical characterization of Nb3Sn wires
Department of Quantum Matter Physics, University of Geneva, Switzerland
Department of Nuclear and Particle Physics, University of Geneva, Switzerland
Francesco LONARDO, Romain BABOUCHE, and Carmine SENATORE
Simon C. HOPKINS and Thierry BOUTBOUL
CERN, Switzerland

## Slide 2
Outline of the presentation
Motivation of the work
  The updated baseline for the high-field dipoles of the Future Circular Collider
Degradation mechanisms and irreversible reduction of Ic
Catalogue of the Wires
Results: Influence of the wire layout on the transverse stress tolerance
  state-of-the-art PIT Nb3Sn wires
  state-of-the-art RRP Nb3Sn wires
Summary

## Slide 3
High Field Magnets for a FCC-hh 85 TeV
PARAMETER | FCC-hh CDR 2019 | FCC-hh FSR 2025
collision energy (c.m.s.) [TeV] | 100 | 85
dipole field [T] | 16 | 14
Circumference [km] | 97.8 | 90.7
beam current [A] | 0.5 | 0.5
synchr. rad. per ring [kW] | 2400 | 1200
peak luminos. [1034 cm-2s-1] | 30 | 30
events/bunch crossing | 1000 | 1000
stored energy/beam [GJ] | 8.3 | 6.5
integr. luminosity / IP [fb-1] | 20000 | 20000
UPDATED BASELINE
The updated baseline of the FCC study:
91 km-ring
14 T-dipoles based on Nb3Sn
collision energy of 85 TeV
A combination of electromagnetic forces with pre-load and thermomechanical effects exposes the brittle and strain sensitive Nb3Sn to the risk of degradation. The main stress component is in the transverse direction of the Nb3Sn Rutherford cables
Adapted from M. Benedikt, FCC Week 2025

## Slide 4
Two mechanisms govern the irreversible reduction of the critical current:
Degradation mechanisms and irreversible reduction of Ic
155 MPa
190 MPa
Electromechanical tests on Nb3Sn wires impregnated with epoxy
The WASP concept was adapted to transverse loads by
B. Seeber et al., IEEE TAS 17 (2007) 2643, DOI: 10.1109/TASC.2007.897934
The irreversible limit is defined at the force level leading to a 95% recovery of the initial IC after unload
The irreversible stress limit is:
Formation of cracks in the Nb3Sn subelements due, for instance, to the stress concentration at the voids.
Cracks generate a reduction of the current carrying cross section  ICunload/IC0 is independent of the magnetic field.
Plastic deformation of the Cu matrix and residual stress on the Nb3Sn subelements.
Residual stress induces a permanent reduction of BC2 after unload  ICunload/IC0 depends on of the magnetic field.

## Slide 5
Technology |  | # of subelements | Bundle Barrier | Cu/non-Cu | Diameter | Subelement size | HT | Ic(15T, 4.2K) Ti-barrel
PIT |  | 192 | No | 1.22 | 0.85 mm | 43 m | 600°C×120h+ 625°C×200h | 
PIT Bundle Barrier |  | 192 | Yes | 1.2 | 0.85 mm | 43 m | 415°C/48h+ 620°C/48h+ 645°C/50h | 411
RRP |  | 132/169 | No | 1.2 | 1.0 mm | 58 m | 210C/48h+ 400C/48h+ 650C/50h | 780 A
RRP |  | 150/169 | No | 1.1 | 1.0 mm | 58 m | 210C/48h+ 400C/48h+ 650C/50h | 730 A
RRP |  | 162/169 | No | 0.9 | 1.0 mm | 58 m | 210C/48h+ 400C/48h+ 650C/50h | 880 A
MQXFS7
What has been tested – Catalogue of the Wires
FRESCA2
Falcon D
MQXFS7
Study of the effect of design on transverse stress tolerance:
Effect of an Nb barrier surrounding the filament bundle.
Influence of the Cu/non-Cu ratio.

## Slide 6
Outline of the presentation
Motivation of the work
  The updated baseline for the high-field dipoles of the Future Circular Collider
Degradation mechanisms and irreversible reduction of Ic
Catalogue of the Wires
Results: Influence of the wire layout on the transverse stress tolerance
  state-of-the-art PIT Nb3Sn wires
  state-of-the-art RRP Nb3Sn wires
Summary

## Slide 7
Both the wires (PIT and PIT BB) have σirr ̴ 95 Mpa.
The presence of the bundle barrier affects neither the irreversible stress limit, nor the general behaviour of the wire under stress.
The BC2 decrease is similar in the two wires. ΔBC2 (95 MPa ) ~ 0.5 T and ΔBC2 (210 MPa ) ~1.15 T.
95 MPa
Irreversible stress limit of PIT and PIT BB

## Slide 8
Outline of the presentation
Motivation of the work
  The updated baseline for the high-field dipoles of the Future Circular Collider
Degradation mechanisms and irreversible reduction of Ic
Catalogue of the Wires
Results: Influence of the wire layout on the transverse stress tolerance
  state-of-the-art PIT Nb3Sn wires
  state-of-the-art RRP Nb3Sn wires
Summary

## Slide 9
Irreversible stress limit of RRP with different Cu/non-Cu
Cu/non-Cu = 1.2
172 MPa
The lower the Cu/non-Cu ratio, the higher the irreversible stress limit σirr
203 MPa
Cu/non-Cu = 1.1
213 MPa
Cu/non-Cu = 0.9
The ΔBC2 (210 MPa ) after unload is 0.6, 0.45 and 0.65 T.
Notes: .

## Slide 10
RRP 132/169
Subelement Ø = 58 m
HT 650C/50h
RRP 150/169
Subelement Ø = 58 m
HT 650C/50h
RRP 162/169
Subelement Ø = 58 m
HT 650C/50h
The lower the Cu/non-Cu ratio, the higher the irreversible stress limit σirr
Irreversible stress limit of RRP with different Cu/non-Cu

## Slide 11
  Powder in Tube wire (PIT and PIT with bundle barrier):
    The irreversible stress limit σirr is approximately 95 MPa.
    The σirr is not influenced by presence of the bundle barrier.
  Restack Rod Process (RRP) wires:
    The σirr for RRP Nb3Sn wires > 170 MPa, and it can reach 210 MPa for wire as 162/169 used for Falcon D
    A correlation between a lower Cu/non-Cu ratio and a higher irreversible stress limit has been observed
  The permanent degradation of state-of-the-art RRP and PIT wires is primarily driven by residual stresses
    ΔBC2 (210 MPa) is ~ 0.6 T for RRP wires and >1.1 T for PIT wires
Summary and future work

## Slide 12
Thanks for your attention

## Slide 13
Commercial Nb3Sn wires: RRP vs PIT
Section of a Nb3Sn dipole magnet
Segal C. et al.,Supercond. Sci. Technol. 29 (2016) 085003 DOI: 10.1088/0953-2048/29/8/085003
PIT wire: Distorted filaments are partly reacted due to Sn leak, lower Ic
Cabling induce wire distortion
Brown M. et al. Supercond. Sci. Technol. 29 084008 (2016) DOI: 10.1088/0953-2048/29/8/084008
PIT, Ø 1.0 mm
Tested in a 1.15 mm groove
RRP, Ø 0.85 mm
Tested in a 1.15 mm groove
irr  110 MPa
irr  175 MPa
RRP wires have higher transversal stress tolerance. They are mechanically more robust than current PIT wires
Senatore C. et al., Supercond. Sci. Technol., 36 (2023) 075001
DOI: 10.1088/1361-6668/acca50
Rutherford cable
Notes: The first reason is the fact that cabling induce distortion of wire that in the case of the case of PIT cause Sn leak, reducing the Ic and the RRR of stabilizing Cu. The trasversal stress tolerance of RRP is higher. The irreversible stress llimit, that identify the stress that induce a permanent degradation of current of 5%, is higher for RRP.
Let’s move now to the challanges and problems of introducing an OS in the RRP