## Slide 1: NI HTS Solenoid for PSI Positron Production Experiment
B. Auchmann, A. Brem, M. Duda, H. Garcia Rodrigues, J. Haack, J. Kosse, T. Michlmayr, G. Montenero, S. Mueller, R. Riccioli, S. Sanfillipo
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program
CHART Day 12/11/2025

## Slide 2: PSI Positron Production () Experiment
N. Vallis, https://doi.org/10.1103/PhysRevAccelBeams.27.013401
Aims to demonstrate high yield positron source
Part of CHART project FCCee-injector
SwissFEL

## Slide 3: Upscaled version of 18 T PSI NI solenoid
18 T, 50 mm cold bore 15 T, 72 mm warm bore
4 coils
Demonstrator
5 coils
Full scale magnet
Coil manufacturing: H. Garcia Rodrigues

## Slide 4
Non-insulated coils
P3 solenoid design
P3 solenoid assembly and testing

## Slide 5
Non-insulated (NI) high-temperature superconductor (HTS)
100 mm
Single-layer pancake coil wound from bare HTS tape
Solder-impregnated
4x 12 mm wide coil
Coil manufacturing: H. Garcia Rodrigues

## Slide 6: Cryogen-free test stand
18 T by 4 stack at 2 kA, 12 K
stack of 4 NI HTS coils with
connectors
HTS leads
1st cryocooler
4 K coldhead
2nd cryocooler
radiation shield
top plate
Central bore field [T]
Test stand thermals & electrical integration: M. Duda, H. Garcia Rodrigues

## Slide 7
NI coil electrical representation:
Inductor (HTS spiral path)
Resistor (turn-turn contact)
Charging time constant
Large NI magnets (large L) take a long time
Non-insulated (NI) HTS Technology Solenoid
18 T by PSI 4 stack at 2 kA, 12 K

## Slide 8
NI coil electrical representation:
Inductor (HTS spiral path)
Resistor (turn-turn contact)
Charging time constant
Large NI magnets (large L) take a long time
Non-insulated (NI) HTS Technology Solenoid
S. Hahn, D. Park, J. Bascuñán, and Y. Iwasa,
“HTS Pancake Coil without Turn-to-Turn Insulation,” IEEE TAS, 2011.
Thermal conductivity, radiation robustness

## Slide 9: Experiment vs model
Example: 1.8 kA at 15 K in cryogen-free setup
Turn-turn resistance used a fitting parameter
Works reasonably over a 15-77 K range

## Slide 10
Non-insulated coils
P3 solenoid design
P3 solenoid assembly and testing

## Slide 11: Upscaled version of 18 T PSI NI solenoid
18 T, 50 mm cold bore 15 T, 72 mm warm bore
Experimental results of 18 T demonstrator used as input
4 coils
Demonstrator
5 coils
Full scale magnet

## Slide 12
Conduction-cooled system
15 T bore, 21 T conductor @ 1.3 kA, 15-20 K
HTS coils
Target
Thermal shield
G10/SS support
MLI
Current terminals
72 mm
Solenoid stack
Cryocooler
Current leads
Pb mass
1.07 m
CAD design: S. Mueller, T. Michlmayr

## Slide 13
Fault scenario:
Coolers stop
Open circuit
Stored magnetic energy gets
Dissipated in coils+buffers
R_turnturn
HTS path
Around 0.7 MJ stored in
the magnetic field

## Slide 14: Buffer sizing
Less mass
more mass
Slow ramp-down

## Slide 15: Buffer sizing
Less mass
more mass
Slow ramp-down
Quench

## Slide 16: Mechanical
Stress [MPa]
d) Hoop
c) Mises
b) Axial
a) Radial
Frictional
interface
Field’s metal
Axial plate
HTS tapes
Stainless steel flange
Copper terminal plate
Stainless steel
overband
Tape structure explicitly modeled to capture
-differential thermal contraction
-plasticity
Max radial stress 2 MPa
Min axial stress -150 MPa
Max hoop stress (substrate) 373 MPa

## Slide 17
Non-insulated coils
P3 solenoid design
P3 solenoid assembly and testing

## Slide 18: Coil manufacturing & testing
Coil manufacturing:
H. Garcia Rodrigues
M. Duda, H. Garcia Rodrigues

## Slide 19: Assembly
Assembly team: M. Duda, H. Garcia Rodrigues,
T. Michlmayr, Y. Studer, N. Strohmaier, M. Zykova, J. Haack

## Slide 20: Magnet being commissioned
Magnetic field measurements:
R. Riciolli, G. Montenero, R. Deckardt
First-of-a-kind system: after reaching 77% of nominal current, we introduced some enhancements. Testing restarted this week.
Pressure
Bore field
Measurements: M. Duda

## Slide 21: Conclusions
experiment aims to demonstrate high yield positron source
Positron source ideal application for NI HTS
experiment will feature a NI HTS solenoid, 15 T bore,
at 15-20 K, 1.3 kA, conduction-cooled in cryogen-free
cryostat
Extra thermal mass helps prevent quenches in case of
external faults
Magnet commissioning underway. Currently at 77% of nominal

## Slide 22: Radiation
P^3 (unshielded) | FCC-ee (2 cm Tungsten)
18 kGy/year | 23 MGy/year
DPA/year 1 W 6 GeV drive beam | DPA/year ~10 kW 6 GeV drive bream
P^3 (unshielded) | FCC-ee (2 cm Tungsten)
18 kGy/year | 23 MGy/year
will demonstrate high yield,
but not radiation robustness
B. Humann, doi:10.18429/JACoW-IPAC2022-THPOTK048
Radiation damage on Epoxy

## Slide 23
Non-insulated (NI) HTS
100 mm
Rapidly develop infrastructure
via license agreement with
Tokamak Energy
4x 12 mm wide coil
Axial current injection

## Slide 24: FCC-ee injector
Flux Concentrator (FC)
Pulsed copper device
We want to do better by using HTS
P. Martyshkin, BINP
Yield=[3]
Yield=
[3] N. Vallis https://doi.org/10.18429/JACoW-LINAC2022-TUPORI16
Electrons shot at target produce particles
Charged particles are captured by a magnet

## Slide 25: FCC-ee injector
Field profile and target location result from
numeric and analytical optimization
Y Zhao. Optimisation of the FCC-ee Positron Source Using a HTS Solenoid Matching Device, 2022.
Y Zhao. Comparison of Different Matching Device Field Profiles for the FCC-ee Positron Source, 2021.
R. Chehab et al., “An adiabatic matching device for the Orsay linear positron accelerator”, IEEE Trans. Nucl. Sci., 1983.