## Slide 1: SMACC2: feasibility study and initiative on Nb-Ti wire and cable with low copper content
PSI/CERN LTS WP Progress Meeting
D. Araujo, B. Auchmann, A. Brem, N. Kehl, C. Lindner, T. Michlmayr, C. Müller, I. S. P. Peixoto,
A. Stampfli and J. Van den Eijnden.
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program. This work was partially funded by the HFM program.
November 2025

## Slide 2
Agenda
Feasibility study
Initiative on Nb-Ti wire and cable with low copper content

## Slide 3: Magnet Parameters (V4)
parameter | value | unit
Bore | 50 | mm
Intra-beam | 400 | mm
Top | 1.9 | K
B0 | 13.97 | T
Bpeak | 14.63 | T
Iop | 10.5 | kA
Load line Margin | 18 | %
Fx | 17.8 | MN/m
Fy | 0.5 | MN/m
1
2
3
4
5

## Slide 4: Magnet Parameters (V4)
@14 T Multi poles | value | unit
a2 | 2.6 | 10-4
a4 | -8.5 | 
a6 | 10.7 | 
a8 | 2.7 | 
b3 | 12.0 | 
b5 | -1.6 | 
b7 | -2.6 | 
b9 | -0.8 | 
1
2
3
4
5

## Slide 5: Cable Parameters (V4)
Layer | LTS Type | Turns
1 | Nb3Sn | 10
2 |  | 43
3 |  | 64
4 | NbTi | 6 + 49
5 |  | 
1
2
3
4
5
Layer | Number of strands | Strand type and diameter in mm
1 | 21 | RRP 162/169 - 1.1
2 |  | 
3 | 34 | RRP 78/91 - 0.7
4 - LF | 34 | Nb-Ti 0.7
5 - LF |  | 
4 - HF | 21 | Nb-Ti 1.1
5 - HF |  | 
Nb-Ti
Nb3Sn
In this version, the Nb₃Sn and Nb-Ti HF and LF cables have the same number of strands and the same strand diameter.

## Slide 6: Magnet Parameters (V4)
1
2
3
4
5
Layer 4 thin conductor peak field >
On Layer 4 thick conductor
The inner blocks could use the thin conductor

## Slide 7
Hot-spot temperature as a function of total reaction time
The total reaction time tR is the sum of quench detection time, validation time, and trigger time.
The adiabatic hot-spot temperature can be kept
<300 K with tR<18 ms
<350 K with tR<27 ms

## Slide 8
SMACC2_V4 parametric study – Varying Cu/noCu in L3 and L4-9
Margin 1-Iop/ISS in L3-9
Hot-spot temperature
19%
18%
17%
16%
15%
325 K
300 K
275 K
350 K
375 K

## Slide 9: Magnet Parameters (V4&V5)
1
2
3
4
5
1
2
3
4
5
parameter | V4 | V5
Bore | 50 mm | 
Intra-beam | 400 mm | 
Top | 1.9 K | 
B0 | 14 T | 
Bpeak | 14.63 | 14.61
Iop in kA | 10.5 | 10.78
Load line Margin in % | 18.5 | 19.5 + 1 %
Strand Area in mm2 | 13667 | 14822 + 8.5%
V4
V5

## Slide 10
SMACC2_V5 parametric study – Varying Cu/noCu in L3 and L4-9
Margin 1-Iop/ISS in L3-9
Hot-spot temperature
19%
18%
17%
16%
15%
20%
325 K
300 K
275 K
250 K
350 K

## Slide 11
Agenda
Feasibility study
Initiative on Nb-Ti wire and cable with low copper content

## Slide 12: Nb-Ti Conductor
We discussed with Nb-Ti wire manufactures and the conductor with a Cu/Non-Cu ratio of 0.9 to match the SMACC2 requirements can be produced.
Such a wire is not an existing product and would require 8 to 10 months of lead time.
The manufacturability of the Rutherford cable, due to the low copper content, which may require post-heat-treatment optimization, is to be studied.
One of the manufactures currently has Nb-Ti conductor (diameter of ~1.5 mm) with a Cu/Non-Cu ratio of 0.85 but lower Ic available off the shelf. This material could be used to manufacture a test cable and to try different post-heat-treatment to assess manufacturability and Ic degradation due to cabling.

## Slide 13: Nb-Ti / Nb3Sn Conductor: tentative plan
 | Q3/2025 | Q4/2025 | Q1/2026 | Q2/2026 | Q3/2026 | Q4/2026 | Q1/2027 | Q2/2027 | Q3/2027 | Q4/2027 | Q1/2028
Procurement of existent Nb-Ti 0.85 Cu/Ncu |  |  |  |  |  |  |  |  |  |  | 
Cabling with 2 or 3 different heat treatments |  |  |  |  |  |  |  |  |  |  | 
Ic round vs extracted samples |  |  |  |  |  |  |  |  |  |  | 
Winding trials |  |  |  |  |  |  |  |  |  |  | 
Finalize SMACC2 Cable Design |  |  |  |  |  |  |  |  |  |  | 
Procurement of final wire |  |  |  |  |  |  |  |  |  |  | 
Cabling with final wire and insulation Nb-Ti type 1 |  |  |  |  |  |  |  |  |  |  | 
Cabling with final wire and insulation Nb-Ti type 2 |  |  |  |  |  |  |  |  |  |  | 
Beginning of SMACC2 Nb-Ti coils production |  |  |  |  |  |  |  |  |  |  | 
Nb3Sn Cable manufacturing and insulation run type 1 |  |  |  |  |  |  |  |  |  |  | 
Nb3Sn Cable manufacturing and insulation run type 2 |  |  |  |  |  |  |  |  |  |  | 
Beginning of SMACC2 Nb3Sn coils production |  |  |  |  |  |  |  |  |  |  | 
The PO for Nb-Ti wire for post-heat-treatment, sharp-bending tests,
cabling, and Ic-reduction studies has been placed.