## Slide 1: SMACC1: open questions
PSI/CERN LTS WP Progress Meeting
D. Araujo, B. Auchmann, A. Brem, N. Kehl, C. Lindner, T. Michlmayr, C. Müller, I. S. P. Peixoto,
A. Stampfli and J. Van den Eijnden.
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program. This work was partially funded by the HFM program.
November 2025

## Slide 2
Agenda
Requests to CERN
316 LN plates
I Iron pole raw material
Kapton for SMACC1 coils
SMACC1 spare conductor

## Slide 3: Cable Unit Lengths
Type | High-Field | Low-Field
Wire type | Nb3Sn RRP® 162/169 | Nb3Sn RRP® 78/91
CERN Wire Denomination | DEM-1.1 | ERMC-0.7
N wire x dia in mm | 21 x 1.1 | 34 x 0.7
Cu/nCu | 0.9 | 1.2
Bare Cable dimensions in mm | 12.74 x 2.06 | 12.74 x 1.31
Insulation thickness in mm | 0.155 | 0.155
Cable Originally Designed for | R2D2 HF | SMACC1 LF
Design based on existent cable
Layers | 1 | 2 | 3/4
Cable Type | High-field | High-field | Low-field
Number of turns | 9 | 39 | 52/52
*Coil unit length in m | 15 | 75 | 100
Weq in mm | 20.1 |  | 19.1
Area of insulated cable in mm2 | 2954 |  | 4367
1 2 3 4

## Slide 4: Use of R2D2 LF cable
For the low-field cable, an alternative would be to use the R2D2 low-field cable (layer 4), based on a Cu/nCu conductor of 1.8 instead of 1.2 (SMACC1 low-field cables). This would represent a reduction by 5% of the load line margin.
Possible risk mitigation, tbd:
Mutualizing the spare conductor between SMACC1 and R2D2.
Producing spare cables on “need basis”.