## Slide 1: Mechanical analysis of the 2024 CS coil designs (SPC variant)
15.01.2026
J. Greenwood
MAG-S.01.04-T021-D001

## Slide 2
Outline
Mechanical analyses to support SPC’s CS design for LAR-DEMO:
Crack growth studies
2D winding pack analysis
2D precompression structure analysis

## Slide 3: FCGR Studies
Cracks are iteratively grown in plates according to the Paris Law
The same safety factors and assumptions were used. No relaxation
71 mm wide plates
Residual stress 240 MPa
Initial defect size: 2 mm2 (surface), 5 mm2 (embedded)
2 load cycles per plasma cycle
2x number of cycles (safety factor)
2x initial area (safety factor)
…
Material | (m/cycle) |  | (MPam1/2)
316LN |  |  | 
Incoloy 908 |  |  | 
Incoloy 718 |  |  | 
JK2LB |  |  | 
N50H (≤ MPam0.5) |  |  | 
N50H (> MPam0.5) |  |  | 
Material |  |  | 
316LN |  |  | 
Incoloy 908 |  |  | 
Incoloy 718 |  |  | 
JK2LB |  |  | 
W: 71 mm
T: 16 mm
Surface Crack
(Initial size 2mm2)

## Slide 4: Maximum Hoop Stresses for 30,000 Plasma Cycles

## Slide 5: FCGR Results & Observations
For T=16 mm, surface cracks generally lead to failure first
There is little lifetime to be gained by thickening the jacket wall beyond ~16 mm
316LN, JK2LB, and N50H were considered for SPC’s CS
Material | Maximum Hoop Stress for 30,000 Plasma Cycles
316LN | 250 MPa
JK2LB/Inconel/Incoloy | ~300 MPa
N50H | 380 MPa

## Slide 6: 2D Winding Pack Analysis

## Slide 7: 2D Winding Pack Analysis
Axisymmetric simulation; axial and radial forces are included.
Average and peak stresses are extracted for each layer.

## Slide 8: Key Coil Design Parameters – 316 LN Design
Parameter | UCD | SC graded | SC + steel graded
Total current (MAt) | 76.27 | 76.27 | 76.27
Conductor current (kA) | 60.53 | 60.53 | 60.53
WP Ri (m) | 1.415 | 1.417 | 1.399
WP Ro (m) | 2.62 | 2.62 | 2.62
SC material in sub-coils (RE-123/Nb3Sn/Nb-Ti) | 14/0/0 | 4/8/2 | 4/8/2
Peak B field (T) | 14.86 | 14.86 | 14.83
CS flux during premagnetisation (Wb) | 192.0 | 192.4 (+0.2%) | 215.0 (+12%)

## Slide 9: Insulation Stresses & Strains
A preliminary assessment of the insulation stress/strain state was made
The insulation was assumed to be bonded no stress relief allowed
Stress/strain limits were exceeded at some conduit and strip corners

## Slide 10: Precompression Structure

## Slide 11: Module Force Directions in Different Scenarios
U3
U2
1
L2
L3
Premagnetisation
Start of Flat Top

## Slide 12: Precompression Structure
Material | Radial thickness (mm) | 
 | Inner tie plates | Outer tie plates
Nitronic 50 | 148 | 92
316 LN | 210 | 110
CS1
CSU2
CSU3
CSL2
CSL3
Tie plates
 | Premag. | SOF | EOF
Fz, CSU3 (MN) | -651.95 | -2.55 | -155.76
Fz, CSU2 (MN) | -124.71 | 25.87 | -460.68
Fz, CS1 (MN) | -5.55 | -5.63 | -140.92
Fz, CSL2 (MN) | 78.96 | 130.07 | 337.85
Fz, CSL3 (MN) | 786.10 | -156.07 | 465.75
Forces calculated for SPC’s CS with 316LN jackets (215 Wb)

## Slide 13: Smeared Properties
Unit cell:
1 conductor
Co-wound strip (if present)
Insulation
All components are bonded
Property | Sub-coil number |  |  |  |  |  | 
 | SC01 | SC02 | SC03 | SC04 | SC05 | SC06 | SC07
Ex (GPa) | 100.26 | 100.19 | 99.78 | 85.62 | 72.11 | 28.30 | 27.49
Ey (GPa) | 127.09 | 127.19 | 128.08 | 118.31 | 104.68 | 81.86 | 83.56
Ez (GPa) | 171.79 | 171.87 | 172.37 | 163.20 | 151.6 | 112.13 | 113.24
Gxy (GPa) | 31.36 | 31.40 | 31.49 | 27.19 | 22.68 | 6.27 | 6.29
Gyz (GPa) | 49.32 | 49.50 | 49.74 | 46.59 | 42.57 | 33.05 | 33.64
Gxz (GPa) | 40.41 | 40.32 | 40.28 | 34.80 | 29.69 | 14.87 | 14.59
xy | 0.227 | 0.227 | 0.225 | 0.218 | 0.221 | 0.140 | 0.140
yz | 0.1215 | 0.215 | 0.216 | 0.210 | 0.200 | 0.210 | 0.212
xz | 0.175 | 0.175 | 0.174 | 0.159 | 0.146 | 0.0789 | 0.0761
x (1/K) | 1.10×10-5 | 1.10×10-5 | 1.10×10-5 | 1.12×10-5 | 1.15×10-5 | 1.20×10-5 | 1.20×10-5
y (1/K) | 1.06×10-5 | 1.06×10-5 | 1.06×10-5 | 1.06×10-5 | 1.05×10-5 | 1.04×10-5 | 1.04×10-5
z (1/K) | 1.01×10-5 | 1.01×10-5 | 1.01×10-5 | 1.01×10-5 | 1.00×10-5 | 9.95×10-6 | 9.94×10-6

## Slide 14: Results and Observations
Contact
Pressure
(Pa)
ITER criteria:
≥25% of module boundaries remain in contact
Contact forces are ≥ 15 MN
Tie plates do not exceed membrane stress limits at room temperature
Both 316LN and N50 tie plates are viable
Fatigue lifetimes of plates have not yet been considered in detail


 | Radial thickness (mm) | 
 | Inner tie plates | Outer tie plates
Nitronic 50 | 148 | 92
316 LN | 210 | 110

## Slide 15: Summary
FCGR studies:
Winding pack analyses: grading the steel and including thick co-wound strips (or multiple strips) leads to a ~10% increase in flux. For 316LN (and Ro=2.62 m), the premagnetisation flux is 215 Wb. Some insulation stress/strain issues remain.
Precompression structure: viable solutions using 316LN or N50 tie plates have been found, with ≤115 mm radial space for the outer tie plates. The precompression is limited by the room temperature stress.
Material | Maximum Hoop Stress for 30,000 Plasma Cycles (16 mm thick jacket wall)
316LN | 250 MPa
JK2LB/Inconel/Incoloy | ~300 MPa
N50H | 380 MPa
Notes: To summarise…

## Slide 16: Conductor Dimensions - 316LN
Layer | Lcond (mm) | dcond (mm) | dcable (mm) | tsteel (mm) | dstrip (mm)
1 & 2 | 71.0 | 58.2 | 26.2 | 16.0 | 60.0
3 & 4 | 71.0 | 58.0 | 26.0 | 16.0 | 60.0
5 & 6 | 71.0 | 56.8 | 24.8 | 16.0 | 60.0
7 & 8 | 71.0 | 56.8 | 24.8 | 16.0 | 30.0
9 & 10 | 71.0 | 56.8 | 24.8 | 16.0 | 8.0
11 & 12 | 71.0 | 30.8 | 15.8 | 7.5 | -
13 & 14 | 71.0 | 29.7 | 14.8 | 7.5 | -
HTS
R&W Nb3Sn
Nb-Ti
A large amount of steel grading using thick co-wound steel strips (or multiple thin strips) is needed just to achieve 215 Wb of flux

## Slide 17: Example: Surface Crack Growth
The iterative model terminates when:
the stress concentration factor somewhere around the crack perimeter exceeds the safe limit
or
the crack has grown sufficiently large
The inputs/assumptions/safety factors are the same as those used in previous SPC analyses:
71 mm wide plate
Initial defect size: 2 mm2 (surface), 5 mm2 (embedded)
2 load cycles per plasma cycle
2x number of cycles (safety factor)
2x initial area (safety factor)
…
Hoop stress: 400 MPa
[1] J. Lorenzo and X. Sarasola, "Fatigue Stress Assessment via crack growth analysis based on LEFM," 2021. Available: https://idm.euro-fusion.org/?uid=2PBDRG

## Slide 18: Crack Growth in N50H Jackets
Both embedded and surface cracks are considered
,
[1] ITER Structural Material Database. Art. 2 Metallic Material Database. https://user.iter.org/?uid=223BAC
[2] J. Lorenzo and X. Sarasola, "Fatigue Stress Assessment via crack growth analysis based on LEFM," 2021. Available: https://idm.euro-fusion.org/?uid=2PBDRG