## Slide 1: Thermo-mechanical analyses and tests on laser welding process
Rafal Ortwein, Jakub Tabin, Tomasz Ślęzak
WPMAG 2025 Final meeting (14-16.01.2025)
Acknowledgement: Xabier Sarasola (SPC), Kamil Sedlak (SPC), Montanstahl

## Slide 2: Content 1. Introduction 2. FEM model of welding 3. Residual stresses: measurements vs FEM 4. Sensitivity study 5. Welding trial (July 2025) – lessons learned 6. New thermal model 7. Residual stress measurements 8. Conclusions/next steps

## Slide 3
Mechanical analysis of the DEMO winding packs (2023) (2RCXLZ v1.1)
EOF Stress intensity
[Pa]
1. Introduction & motivation (1/4)

## Slide 4
Layer [-] | ~Jacket length [m] | Length of seam weld [m]
1 | 847 | 1694
2 | 852 | 1704
3 | 857 | 1714
4 | 863 | 1725
5 | 868 | 1736
6 | 874 | 1747
7 | 879 | 1759
8 | 787 | 1573
 | Total | 13652
1. Introduction & motivation (1/4)

## Slide 5
Seam (longitudinal weld) – laser welding
Automatic method
1. Introduction & motivation (1/4)
History of welding trials:
Cryotech (2023)
Montanstahl (2025)
Continuous pieces of 100 m length, manufactured with hot rolling

## Slide 6
2. FEM model of welding
Moving heat source model
Thermal model
Mechanical model
Equilibrium equations
Constitutive equations
Yield function
Thermal strain
Strain-displacement relations
For the laser welding

## Slide 7
Parameters:
re – radius at the top
ri – radius at the bottom
- laser velocity
P – laser power [W]
– laser efficiency (assumed 1)
2. FEM model of welding
Green – parameters related to the size of the laser beam
Red – laser velocity

## Slide 8
 | References | Year
1 | J.R. Chukkan et al. Simulation of laser butt welding of AISI 316L stainless steel sheet using various heat sources and experimental validation. Journal of Materials Processing Technology, 219 2015, 48-59 | 2015
2. FEM model of welding
Temperatures above melting are of no importance for the residual stress analysis
Chart: T [C]
| 30.167545288547601 | 112.52259558879101 | 212.450083509172 | 312.211469509415 | 414.435746049638 | 519.03986216977205 | 616.25530666996497 | 715.85059075006995 | 817.90876537015504 | 917.25489657005198 | 1016.85018065015 | 1121.12209293001 | 1220.55127508998 | 1441.4926033096599 | 1507.5582101315299 | 2049.3941289271602 | 2295.7662338852501 | 2544.4351274631699
k_Re1 | 13.1885 | 14.542 | 16.3127 | 17.8742 | 19.4354 | 20.8917 | 22.3487 | 23.7008 | 25.0528 | 26.0909 | 27.4431 | 28.4809 | 29.6237 | 31.8029 | 65.3904 | 65.345 | 65.429 | 65.3036
Chart: T [C]
| 56.660801550590001 | 139.51415761124801 | 239.690798411836 | 339.86743921242402 | 440.044080013013 | 542.84971327371898 | 645.32314269414996 | 748.04572499478695 | 848.139314835307 | 950.86189713594501 | 1048.4095454764099 | 1151.1321277770501 | 1256.31760061766 | 1476.7062103789599 | 1524.0023002252101 | 2568.26788917679
cp_Ref1 | 465.6997 | 485.5141 | 506.3604 | 527.2068 | 548.0532 | 570.9904 | 589.7418 | 611.6325 | 631.4324 | 653.3232 | 672.0787 | 693.9695 | 715.8582 | 761.7202 | 862.3256 | 863.3721
Chart: T [C]
| 82.821853972355996 | 2557.8034682080902
ro_Ref1 | 7953.2898 | 7283.7319
Thermal properties of 316L

## Slide 9
H=2.4
Chart: T [C]
2. FEM model of welding

## Slide 10
2. FEM model of welding
Moving heat source model
Thermal model
Mechanical model
Equilibrium equations
Constitutive equations
Yield function
Thermal strain
Strain-displacement relations
For the laser welding

## Slide 11
2. FEM model of welding
Chart: T [C]
| 26.85 | 126.85 | 226.85 | 326.85000000000002 | 426.85 | 526.85 | 726.85 | 826.85 | 926.85 | 1026.9000000000001 | 1126.9000000000001 | 1226.9000000000001 | 1372
Ref4 | 194.7 | 190 | 184.5 | 178.2 | 171 | 161.7 | 141 | 127.3 | 112.5 | 95 | 73 | 51 | 51
Chart: T [C]
| 26.85 | 126.85 | 226.85 | 326.85000000000002 | 426.85 | 526.85 | 726.85 | 826.85 | 926.85 | 1026.9000000000001 | 1126.9000000000001 | 1226.9000000000001 | 1372
Ref4 | 0.25 | 0.23 | 0.285 | 0.319 | 0.322 | 0.305 | 0.291 | 0.24 | 0.24 | 0.24 | 0.24 | 0.24 | 0.24
Chart: T [C]
| 26.85 | 126.85 | 226.85 | 326.85000000000002 | 426.85 | 526.85 | 726.85 | 826.85 | 926.85 | 1026.9000000000001 | 1126.9000000000001 | 1226.9000000000001 | 1372
Ref4, Ref5 | 1.48e-05 | 1.56e-05 | 1.63e-05 | 1.69e-05 | 1.74e-05 | 1.79e-05 | 1.87e-05 | 1.9e-05 | 1.93e-05 | 1.95e-05 | 1.96e-05 | 1.98e-05 | 1.99e-05
Chart: T [C]
| 26.85 | 126.85 | 226.85 | 326.85000000000002 | 426.85 | 526.85 | 726.85 | 826.85 | 926.85 | 1026.9000000000001 | 1126.9000000000001 | 1226.9000000000001 | 1372
Ref4 | 246 | 217.4 | 188.8 | 165.2 | 154.9 | 144.7 | 124.2 | 111.1 | 73.6 | 36 | 18.4 | 15 | 15
Chart: T [C]
| 26.85 | 126.85 | 226.85 | 326.85000000000002 | 426.85 | 526.85 | 726.85 | 826.85 | 926.85 | 1026.9000000000001 | 1126.9000000000001 | 1226.9000000000001 | 1372
Ref4 | 2281 | 2023 | 1765 | 1531 | 1363 | 1195 | 858.6 | 693.6 | 558.2 | 423 | 293.4 | 265 | 265
Ref4 | FEM analysis of thermal and residual stress profile in selective laser melting of 316L stainless steel
Ref5 | Experimental and numerical study on residual stress and geometric distortion in powder bed fusion process

## Slide 12
2. FEM model of welding
Chart: Plastic strain [-]
| 0 | 0.2
T1 | 246 | 702.2
T2 | 217.4 | 622
T3 | 188.8 | 541.8
T4 | 165.2 | 471.4
T5 | 154.9 | 427.5
T6 | 144.7 | 383.7
T7 | 124.2 | 295.92
T8 | 111.1 | 249.82
T9 | 73.6 | 185.24
T10 | 36 | 120.6
T11 | 18.4 | 77.08
T12 | 15 | 68
T [◦C] | E [ Gpa] | Poisson’s ratio [-] | sig0 [Mpa] | Tan. Mod [Mpa] | CTE [1/K)
26.85 | 194.7 | 0.25 | 246 | 2281 | 1.48E-05
126.85 | 190 | 0.23 | 217.4 | 2023 | 1.56E-05
226.85 | 184.5 | 0.285 | 188.8 | 1765 | 1.63E-05
326.85 | 178.2 | 0.319 | 165.2 | 1531 | 1.69E-05
426.85 | 171 | 0.322 | 154.9 | 1363 | 1.74E-05
526.85 | 161.7 | 0.305 | 144.7 | 1195 | 1.79E-05
726.85 | 141 | 0.291 | 124.2 | 858.6 | 1.87E-05
826.85 | 127.3 | 0.24 | 111.1 | 693.6 | 1.90E-05
926.85 | 112.5 | 0.24 | 73.6 | 558.2 | 1.93E-05
1026.9 | 95 | 0.24 | 36 | 423 | 1.95E-05
1126.9 | 73 | 0.24 | 18.4 | 293.4 | 1.96E-05
1226.9 | 51 | 0.24 | 15 | 265 | 1.98E-05
1372 | 51 | 0.24 | 15 | 265 | 1.99E-05
 | T1 | T2 | T3 | T4 | T5 | T6 | T7 | T8 | T9 | T10 | T11 | T12 | T13
Plastic str. | 26.85 | 126.85 | 226.85 | 326.85 | 426.85 | 526.85 | 726.85 | 826.85 | 926.85 | 1026.9 | 1126.9 | 1226.9 | 1372
0 | 246 | 217.4 | 188.8 | 165.2 | 154.9 | 144.7 | 124.2 | 111.1 | 73.6 | 36 | 18.4 | 15 | 15
0.2 | 702 | 622 | 541.8 | 471.4 | 427.5 | 383.7 | 295.92 | 249.82 | 185.24 | 120.6 | 77.08 | 68 | 68

## Slide 13
2. FEM model of welding

## Slide 14
3. Residual stresses: measurements vs FEM
J. Tabin et al. Microstructure, mechanical properties and residual stress of welded stainless-steel jackets for React & Wind conductor in EU-DEMO. Fusion Engineering and Design 222 (2026) 115503
Hole drilling strain gauge method
Depth ~0.25 mm
Depth 0.5-0.8 mm
3.5±0.5 mm

## Slide 15
3. Residual stresses: measurements vs FEM
σZ (σ1) [Pa]
σY (σ2) [Pa]
353 MPa
160 MPa
σY (σ2) [Pa]
190 MPa

## Slide 16
4. Sensitivity study
σZ (σ1)
=0.6 m/s
=1.5 m/s
=1.8 m/s
=2.4 m/s
=0.9 m/s
=1.2 m/s
Stress σZ
σZ [Pa]
Welding velocity

## Slide 17
4. Sensitivity study
σZ (σ1)
Laser power
σZ [Pa]
σZ [Pa]
σZ [Pa]
σZ [Pa]
σZ [Pa]

## Slide 18
4. Sensitivity study
σZ [Pa]
Laser beam size

## Slide 19
5. Welding trial (July 2025) – lessons learned
Spooling +
air cooling
hot rolling
Machining to tolerance welding surfaces
Straightening
Bending in the hall
Laser welding

## Slide 20
5. Welding trial (July 2025) – lessons learned
Test at Montanstahl
Test at ICAS

## Slide 21
5. Welding trial (July 2025) – lessons learned

## Slide 22
5. Welding trial (July 2025) – lessons learned
Laser welding
Vertical compression with a force of ~2.7 kN

## Slide 23
5. Welding trial (July 2025) – lessons learned
Laser 2 | Laser 1
1000 W | 1500 W
3300 W | 3700 W
Laser 1
Laser 2
Laser size
0.4-0.5 mm
Laser velocity
2 m/min

## Slide 24
5. Welding trial (July 2025) – lessons learned
~70 cm
~50 cm
Ultrasound system
~90 cm
Table with rollers
Up to ~120 C
~40 m

## Slide 25
5. Welding trial (July 2025) – lessons learned
~70 cm
~42.1 m
~2.1 m
V=2 m/min=0.033 m/s
t=63 s
t=21 s
t=1263 s

## Slide 26
5. Welding trial (July 2025) – lessons learned

## Slide 27
6. New thermal model
=+

## Slide 28
6. New thermal model
200 mm long piece (4x longer than the previous model)
re=1.2e-3
ri=0.5e-3
75% power on the sample

## Slide 29
7. Residual stress measurements
LW1
Mill cutter broke at 0.2 mm
Mill cutter broke at 0.7 mm
Stresses in both directions are positive (tensile), which are more dangerous than compressive

## Slide 30
7. Residual stress measurements
After welding by ICAS:
After welding by Montanstahl
Possible reason:
Work hardening of the material due to hot rolling and bending before welding, causing higher yield stress

## Slide 31
8. Conclusions and next steps
For this task:
Performing mechanical analysis for the Montanstahl like set-up
Including higher heat transfer coefficient
Including the vertical pressure from the rollers
Future work:
Thermal simulation of the full RW conductor, to see the values of temperatures and the potential for damage.
Measuring mechanical properties of the welded material (316L) at high temperatures -> to better calibrate the model