## Slide 1: WPMAG - CEA IRFM HWRC (CORC-like) Properties 15/01/2025
A.Torre, J. Pavan

## Slide 2: 2025 CEA TS HWRC (CORC-like) Properties
MAG-S.01.01-T025-D001
EU-CN: Deliverable on 2025 CEA CORC Conductor Performances Analyses

## Slide 3: 2025 CEA TS HWRC (CORC-like) Properties
Already presented at EUCN meeting by C. Nguyen

## Slide 4: 2025 CEA HWRC (CORC-like) Properties
Geometrical description of Helically Wound Rebco Cables (HWRC)
Description of structures and as function of layer parameters
LpLi = Twist pitch
NtLi = # tapes
RLi = cabling radius
eLi = Gap
WLi = Tape Width
Important features for electrical/thermal models need to be deduced from geometrical considerations:
Contact lenghts:
Contacts surface:
Contacts posistions:

## Slide 5: 2025 CEA HWRC (CORC-like) Properties
Tape properties fit
General parameters |  |  | ab-axis parameters |  |  |  sensitivity |  | 
TC0 | [K] | 93 | Bi0,ab | [T] | 250 |  | [-] | 0.857
n | [-] | 1 |  | [MA.T/mm2] | 84 | g0 | [-] | -0.005
c-axis parameters |  |  | pab | [-] | 1.02 | g1 | [-] | 0.094
Bi0,c | [T] | 140 | qab | [-] | 4.45 | g2 | [-] | -0.0008
 | [MA.T/mm2] | 1.41 |  | [-] | 4.73 | g3 | [-] | 0.0039
pc | [-] | 0.31 | n1 | [-] | 1.77 | REBCO properties |  | 
qc | [-] | 0.87 | n2 | [-] | 4.1 | t | [m] | 1.5
 | [-] | 3.09 | a | [-] | 0.1 | w | [mm] | 4
Fit of SST properties using CERN 2014 scaling law
Deducing individual tapes critical current
Fit is OK within 10-15 %
Effective parameters (angle) can be deduced

## Slide 6: 2025 CEA HWRC (CORC-like) Properties
Cable properties
Definition of two analytical limiting cases:
Cable limiting cases between 20kA and 26kA (as expected)
SULTAN test program refined
Parametric study of dropouts impact
Extrapolated performance at given operating points

## Slide 7: 2025 CEA HWRC (CORC-like) Properties
DC Electrical model for current re-distribution (CARMEN)
Resistive network model developed (only resistive): CARMEN tool
Full E(I) curve confirms Ic~21kA
Electrical model able to see very small redistribution (negligible)
Performances confirmed around Ic=20kA

## Slide 8: 2025 CEA HWRC (CORC-like) Properties
Perspectives
Continue modelling (maybe smaller units, faster computation)
Vary the current injection (imbalance)
Maybe couple to Thermohydraulic model