## Slide 1: Manufacturing of HTS SECAS samples and preliminary tests in LN2
M. Bombardieri, G. Celentano, S. Chiarelli, V. Corato, G. De Marzi, R. Freda, F. Maierna, M. Marchetti, A. Masi, L. Merli, M. Seri, A. della Corte, A. Formichetti, R. Righetti, M. Breschi, G. Colombo, M. A. Caponero, A. Polimadei, W. Hong
WPMAG 2025 Final Meeting
Villigen PSI; January 14th - 16th, 2026
L. Muzzi (on behalf of the ENEA team)

## Slide 2: Main Task Objective
BRAided Stack
(BRAST)
SECtor ASsembled cable
(SECAS) CICC concept
Cu sector
L. Muzzi, et al., IEEE TAS 2023
Multi-Stage Cable Processing
Manufacture of a SECAS Sample for SULTAN test, incl. qualification tests at LN2

## Slide 3: BRAST-SECAS Prototypes Qualification steps
BRAST in spirally machined slot, and closing filler
BRAST assembled in straight sector, then inserted in spirally machined slot
BRAST #3
SECAS #1
BRAST of 10 Tapes, 12 mm x 0.08 mm

## Slide 4: Initial qualification – BRAST (77K – s.f. tests) - bending
BRAST was extracted from Bent conductor and re-tested
BRAST #3
(non soldered stack)
Effect of Conductor bending:
Apparently, the tape stack was not damaged during the bending

## Slide 5: Initial qualification – BRAST (77K – s.f. tests) - bending
BRAST was extracted from Bent conductor and re-tested
BRAST #3
(non soldered stack)
Voltage development is different on the different tapes within the stack. Effects of self-field, and effects of current distribution / re-distribution (at terminations, in these samples) should be clarified.
Either through modelling, or by means of dedicated tests.
Electric field along different tapes
Same qualitative behaviour observed an all tested prototypes

## Slide 6: Current distribution study in BRAST (77K – s.f. tests)
Sat-Af-Spe1-04
V termination
V tape
Sample for current distribution study: «free-standing» BRAST with 9 tapes (SST) 12 mm wide
Voltage taps welded on tapes:
Soldered terminations with staggered tapes
Voltage between termination and tape, as well as along each tape, can be measured
V_TERM-TAPE

## Slide 7: Current distribution study in BRAST (77K – s.f. tests)
Complex current re-distribution among tapes (in these samples, occurring at terminations); self-field effects also play a role.
Same qualitative behaviour as observed on the BRAST extracted from the bent conductor prototype, tested as well in «stand-alone» mode.
V after subtraction of the resistive component
Raw data
Voltage along each tape during current ramp
Voltage between termination and each tape
Wide transition «spectrum» for the different tapes.
Resistance distribution at terminations.

## Slide 8: Current distribution in BRAST @77 K & self-field
Non-homogenous transition of the stack
H-form. model by
Dr. W. Hong (ASIPP)
Simulation results accurately reproduce this trend, indicating that in these non-soldered, short samples, the presence of inhomogeneous tape terminal resistances have a strong effect on the distribution of current among the tapes.

## Slide 9: SECAS - SULTAN sample
SULTAN equivalent electromagnetic load  11 T, 100 kA
Cu fillers
Steel capillary for FOS
LEG 1
6 sectors with 1 BRAST
wt. 9 x 12 mm-wide tapes
3.7 mm
Cu sectors
LEG 2
6 sectors with 3 BRASTs
wt. 7 x 4 mm-wide tapes
EU DEMO target: stable operation
@ 60 kA, 4.5 K, 18 T

## Slide 10: SULTAN sample preparation: some key steps
BRAST manufacture at:
Using the existing in-line braid machine

## Slide 11: SULTAN sample preparation: some key steps
BRAST manufacture at:
BRAST 12 mm tapes  60 m
BRAST 4 mm tapes  60 m

## Slide 12: SULTAN sample preparation: some key steps
Cable assembly trials:
Twisting of Cu sectors
Short piece of assembled SECAS
Extruded Cu sector
Extruded by KME (D)
Unit lenth 5 m
Hundreds of m produced

## Slide 13: SULTAN sample preparation: some key steps
Cable assembly trials:
Twisting of Cu sectors
Short piece of assembled SECAS
Sectors assembled, and wrapped in SS tape
Nominal twist pitch
of 1200 mm
SULTAN sample manufacturing:
Post-twist check at 77 K, self-field
shows no evident sign of degradation
8-tapes dummy
9-tapes extracted

## Slide 14: SECAS - SULTAN sample compaction
Jacketing and compaction:
4-mm-wide tapes
12-mm-wide tapes

## Slide 15: SECAS – SULTAN sample DFOS QD
SS capillaries for DFOS
One leg has been equipped with 4 SS capillary tubes for distributed or quasi-distributed temperature monitoring:
3 DOFS
1 FBG array
Bottom termination
Fiber feedthroughs
He inlet
Leaking problems at fibers feedthroughs 
DFOS no more adopted in this cable
It will be implemented for the third SULTAN leg (currently in preparation)

## Slide 16: SECAS - SULTAN termination manufacturing
Pre-tinned HTS tapes
Conductor is inserted in the pre-tinned copper terminal
Solder crucible
Copper termination heaters
air
solder
Jacket heaters
The termination is soldered via impregnation while heated stably at 200 °C
Bath and termination temperature controller
Jacket heaters power supply
Conductor

## Slide 17: SECAS - SULTAN termination manufacturing
Solder crucible
Copper termination heaters
air
solder
Jacket heaters
The termination is soldered via impregnation while heated stably at 200 °C
Bath and termination temperature controller
Jacket heaters power supply
Conductor
Sample
Shipped to SPC in late Sept. ‘25
Sample «assembly», incl. clamps and instrumentation installation, by SPC

## Slide 18: SECAS - SULTAN sample
Cu fillers
Steel capillary for FOS
LEG 1
6 sectors with 1 BRAST
wt. 9 x 12 mm-wide tapes
LEG 3
6 sectors with 1 BRAST
wt. 9 x 12 mm-wide tapes
Now in preparation:
BUT with sector twisting applied before insertion of tape stacks, simulating a very different possible processing approach.
CICC length is ready; terminations still to be manufactured.
 Ready by the end of February 2026.

## Slide 19: Next Steps
- manufacture of a third SECAS prototype length is on-going.
- assembly of the full-size sample  SPC
- test of the full-size sample.
- a new sample for KIT FBI facility is also under preparation.
- modelling activities are also on-going, to help clarify the observed effects of current re-distribution among tapes occurring at terminations in short samples.