## Slide 1
Investigation of AC loss in filamentized coated conductor tapes 4 mm and 12 mm wide, with the filaments of 500 µm and 250 µm, prepared by industrial process
F. Gömöry, J. Šouc, M. Solovyov, M. Kucharovič
Institute of Electrical Engineering, Slovak Academy of Sciences, Bratislava, Slovakia
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
PRD-3.HTS.01-T022-D001

## Slide 2
Initial remarks
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
REBCO deposited by low-cost industrial 2LUPS process utilizing the 3D filamentized metal tape as substrate
A Wulff et al., Supercond. Sci. Technol. 28 (2015) 072001
A R Insinga et al., IEEE Trans. Appl. Supercond.. 28 (2018) 6601705
A R Insinga et al., IEEE Trans. Appl. Supercond.. 29 (2019) 8200704
standard
substrate
buffer(s)
REBCO
striation
(mechanical, chemical,…
patterned substrate
Ag, Cu
Bac
Relevant AC magnetization regime:
Samples prepared within Eurostars-2 project “Filaments4Fusion”

## Slide 3
Optimization of tape architecture
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
current redistribution around a defect :
standard CC tape
fiamentized CC tape
fiamentized CC tape
with Cu in gaps
Cu
circulation of currents through metallic gaps: coupling AC loss
wf
L
high-field approximation:
df
hysteresis loss reduced in proportion to Nf :
Bac
Bac

## Slide 4
Optimization of tape architecture
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
L
w
t
wf
wg
dg
df
Bmax sin(t)
Sample characterisation:
geometry: L, w, t, wf ,wg ,dg ,df
materials:
      gap resistivity
      resistivity of metallic overlayer(s)
AC loss reporting:
magnetization loss: Qm/L [J/m/cycle]
AC susceptibility
(imaginary part) :

## Slide 5
Experiments vs. theory
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
Hysteresis loss:
Y Mawatari, Phys. Rev. B 54 (1996) 13215
x-array of strips
Coupling loss:
F Gömöry et al., Superconductivity 15 (2025) 100193
effective medium approach
Eddy current loss:
metallic strip
E. H. Brandt, Phys. Rev. B 50 (1994) 13833

## Slide 6
Hysteresis loss vs. filamentary architecture
Y Mawatari, Phys. Rev. B 54 (1996) 13215
Tape 12 mm wide
wf [µm]
Ic = 300 A, gaps 50 µm
wg [µm]
Ic = 300 A, filaments 495 µm
Ic [A]
gaps 50 µm, filaments 495 µm
narrower filaments  lower hysteresis loss
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute

## Slide 7
Coupling loss vs. filamentary architecture
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
W J Carr Jr, Supercond. Sci. Technol. 20 (2007) 168
in reality a fitting parameter
ρCu = 210-9 m
low frequency limit:
(practical use)

## Slide 8
Tapes 12 mm wide – filament width & metallization
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
Sample | Nf | wf [mm] | wg [mm] | Cu [µm] | Ic [A]
A-2 | 6 | 1.82 | 0.19 | 0 | 340
C-2 | 6 | 1.82 | 0.19 | 3 | 340
A-1 | 11 | 0.98 | 0.12 | 0 | 300
C-1 | 11 | 0.98 | 0.12 | 3 | 300
A-05 | 20 | 0.55 | 0.05 | 0 | 220
C-05 | 20 | 0.55 | 0.05 | 3 | 220
Cu
Ag
REBCO 3.5 µm
buffer 3.5 µm
A
C
wf
wg

## Slide 9
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
6 filaments
11 filaments
20 filaments
Bmax [T]
Bmax [T]
Bmax [T]
rCu = 210-9 m
A: rg = 40 rCu
C: rg = 3.7 rCu
A: rg = 25 rCu
C: rg = 3.7 rCu
A: rg = 15 rCu
C: rg = 7 rCu
Tapes 12 mm wide – filament width & metallization

## Slide 10
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
rCu = 210-9 m
A: rg = 40 rCu
C: rg = 3.7 rCu
A: rg = 25 rCu
C: rg = 3.7 rCu
A: rg = 15 rCu
C: rg = 7 rCu
6 filaments
11 filaments
20 filaments
Tapes 12 mm wide – filament width & metallization

## Slide 11
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
Tapes 12 mm wide, 500 µm filaments – gap width & metallization
Sample | wf [µm] | wg [µm] | Ag [µm] | Cu [µm] | dg [µm] | kg | Ic [A]
B-3 | 500 | 80 | 1.3 | 3.9 | 5.2 | 12 | 244
B-4 | 498 | 116 | 1.9 | 14.7 | 16.6 | 3.2 | 264
B-5 | 484 | 69 | 1.35 | 9.2 | 10.55 | 3.3 | 260
ρCu = 210-9 m

## Slide 12
Tapes 4 mm wide
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
7 filaments 500 µm, 3.56 m Ag + 13.7 m Cu, Ic = 90 A
rg = 5.6 rCu
reddy = 1 rCu

## Slide 13
Tapes 4 mm wide
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
7 filaments 500 µm, 3.56 m Ag + 13.7 m Cu, Ic = 90 A
Bmax = 5 mT
rg = 5.6 rCu
reddy = 1 rCu

## Slide 14
Tapes 4 mm wide
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
12 filaments 250 µm, 4.3 m Ag + 13.3 m Cu, Ic = 70 A
rg = 6  rCu
reddy = 1 rCu

## Slide 15
Tapes 4 mm wide
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
12 filaments 250 µm, 4.3 m Ag + 13.3 m Cu, Ic = 70 A
rg = 6  rCu
reddy = 1 rCu
Bmax = 5 mT

## Slide 16
Conclusions and outlook
WPMAG EUROfusion Final Meeting 14–16 Jan 2026, Paul Scherrer Institute
Magnetization loss of filamentized tapes prepared by 2LUPS technology in 12 mm and 4 mm versions:
controllable by tape architecture
predictable by theory (transverse resistivity remaining the only fitting parameter)
Outlook for 2026-27:
manufacturing of laboratory models of round cables from MF tapes
experimental testing of magnetization loss, verification of theoretical predcitions