## Slide 1: Feasibility study of the system for transport measurements during cryogenic gamma irradiation
PRD-3.HTS.01-T023 - D002
Valentina Pinto / FUSEN-COND
WPMAG Final Meeting 2025 16/01/2026

## Slide 2: Acknowledgments
Superconductivity Laboratory-ENEA
G. Celentano, R. Freda, A. Masi, A. Angrisani Armenio
Calliope Facility-ENEA
A. Cemmi, R. Carcione, I. Di Sarcina, G. Ferrara, A. Verna, J. Scifo
Tor Vergata University- Rome
Prof. M. Tomellini, M. De Angelis
TASK PRD-3.HTS.01-T023: Understanding neutron and secondary radiation effects on the superconducting state and on the microstructure of HTS 2G tapes
Task Coordinator: F. Laviano (POLITO)
IRAD Laboratory-ENEA
D. Casagrande, E. Palumbo

## Slide 3: Gamma Irradiation Effect on HTS Film
Origin of some contradictions in the literature data:
Scarce statistical significance (often no or few replicates are studied)
Irradiated samples are compared to a reference control sample
Few details on the experimental conditions

## Slide 4: Starting Point: 2024 Activity
Gamma irradiation of REBCO CCs, BiSCCO wires and lab-scale YBCO films at fusion relevant conditions (dose equal to 7.1 MGy)
60Co gamma source
HTS samples

## Slide 5: What Emerged by 2024 Activity
Absolute necessity of experiments carried out in the real operative conditions
Samples degradation due to secondary reactions of photons with the test environment
In situ measurements during cryogenic irradiation

## Slide 6: 2025 Activity
Feasibility study of the proper system for transport measurements during cryogenic irradiation

## Slide 7: Towards in-situ measurements during gamma irradiation
Gamma irradiation of liquid nitrogen. A real problem?
In-situ measurements of Superpower tapes in LN2 irradiated up to 3.5 kGy.
Risks of LN2 explosions after a dose of 10 kGy were reported [Chislett, UKAEA report 2023].
Chislett et al [SUST, 2023]

## Slide 8: Towards in-situ measurements during gamma irradiation
Duke et al [IEEE, 2024] reported irradiation study of fiber optics in LN2 up to 1.2 MGy and 60 kGy/h. No explosion occurred.
Gamma irradiation of liquid nitrogen. A real problem?
Tests of LN2 irradiation to verify the safety of the apparatus for in-situ transport measurements

## Slide 9: 2025 Activity: Design of the Cryostat
High Density Sintered Expanded Polystyrene (HD-EPS)

## Slide 10: 2025 Activity: Design of the Cryostat

## Slide 11: 2025 Activity: Liquid Nitrogen Irradiation
Dosimeter | Dose rate (water) (Gy/h) | Dose rate (air) (Gy/h)
1 | 2953 | 2541
2 | 3078 | 2642
3 | 2863 | 2463
4 | 2384 | 2049
5 | 2305 | 1991
6 | 1916 | 1647
Test at Calliope Facility

## Slide 12: 2025 Activity: Liquid Nitrogen Irradiation
Dosimeter | Dose rate (water) (Gy/h) | Dose rate (air) (Gy/h)
1 | 2953 | 2541
2 | 3078 | 2642
3 | 2863 | 2463
4 | 2384 | 2049
5 | 2305 | 1991
6 | 1916 | 1647

## Slide 13: 2025 Activity: Liquid Nitrogen Irradiation
Dose [kGy] | Dose/rate (air) [kGy/h] | LN2 volume [L]
1 | 0.8 | 2
1.5 | 0.8 | 2
5.1 | 2.6 | 19
11.1 | 2.6 | 19
No explosion occurred up to 11.1 kGy
LN2 5.0 grade with a purity ≥ 99,999% and a level of O2 contamination < 10 ppmv

## Slide 14: 2025 Activity: Tests of Cable Radiation Hardness
No changes up to 1.6 MGy and 2.8 kGy/h
Test of radiation hardness of cable for voltage measurement

## Slide 15: Conclusions
A cryostat was designed, realized and used for the test of LN2 irradiation
LN2 can be used as cryogenic liquid up to 11 kGy with no risk of explosions
Tests on radiation hardness of cable for voltage measurement are currently ongoing
The procurement of other necessary equipment, such as source meter, nanovoltmeter and thermometers, has started.

## Slide 16
THANK YOU

## Slide 17
Valentina Pinto
valentina.pinto@enea.it

## Slide 18: Backup

## Slide 19: Irradiation Test
Commercial HTS:
EuBCO+BaHfO3 by Shanghai Superconducting Tech. (#2 different APCs content). Cu stabilizer thickness of 10 μm
GdBCO, SCN04220, by Sunam. Cu stabilizer thickness of 15 μm each side.
BiSCCO 2223, by Sumitomo. Ag/Ag-alloy matrix.
Chemically deposited film used as reference:
YBCO on STO and LAO
YBCO-Gd10% on LAO

## Slide 20: Calliope Facility at ENEA
Pool-type irradiation plant in a large volume (7x6x3.9 m3) shielded cell.
Plane rack, active area: 40 cm × 75 cm .
60Co gamma source with a maximum dose rate value of about 5.5 kGy·h-1 (June 2024).
Large dimensions
Fusion relevant dose/rate

## Slide 21: Calliope Plant Main Features

## Slide 22: Irradiation test with fusion relevant conditions
Dose: 7.1 MGy (corresponding to 5.9 MGyYBCO)
Dose rate: 3.9 kGy/h
ITER Qualifications: doses up to 8 MGy
‘’the 5 MGy dose was chosen to enable evaluation of prolonged gamma irradiation effects’’ (Campbell et al [J. of Superconductivity and Novel Magnetism, 2024])
60Co gamma source
HTS samples