## Slide 1
Modeling of threshold photoemission and degradation of semiconductor photocathode
Pengwei Huang
Tsinghua University, Beijing, China
2019.09.13
EWPAA 2019, 11-13 September 2019, Villigen

## Slide 2
Threshold photoemission
Low mean transverse energy (MTE) cathodes will be favored by XFEL and UED/UEM, which can greatly benefit from low thermal emittance. Threshold photoemission has been experimentally proved to be an effective method to achieve ultralow MTE.
Cathode | Threshold(eV) | Photon (eV) | Thermal emittance (mm.mrad/mm) | Quantum efficiency
GaAs[1] | 1.42 | 1.44 | 0.24 | ~10-3
Cs3Sb[2] | 1.9 | 1.8 | 0.27 | ~510-4
Na2KSb[3] | 1.9 | 1.8 | 0.26 | ~10-4
Cathode | Threshold(eV) | Photon (eV) | Thermal emittance (mm.mrad/mm) | Quantum efficiency
GaAs[1] | 1.42 | 1.44 | 0.24 | ~10-3
Cs3Sb[2] | 1.9 | 1.8 | 0.27 | 
Na2KSb[3] | 1.9 | 1.8 | 0.26 | ~10-4
[1]I. Bazarov , et al. Journal of Applied Physics, 2008, 103(5): 054901.
[2]L. Cultrera , et al. Physical Review Special Topics-Accelerators and Beams, 2015, 18(11): 113401.
[3] J. Maxson, et al. Appl. Phys. Lett. 106, 234102 (2015)
Low MTE condition is delicate and easily affected by many factors, setting a lower limit to the achievable MTE.

## Slide 3
Limitation towards low MTE
Temperature
Cs3Sb
Cu
L. Cultrera, et al, PRSTAB 18, 113401(2015)
S. Karkare’s talk in P3, 2018
Roughness
G. Gevorkyan, et al, PRAB 21, 093401 (2018)
S. Karkare and I. Bazarov, PR Applied 4, 024015 (2015)
Surface state
Multiphoton emission
Z. Zhang and C. Tang, PRSTAB 18, 053401 (2015)
High E field – Physical roughness
Low E field – Chemical roughness
S. Karkare et al, PRL 118, 164802 (2017)
The electrons from surface state may result in a higher MTE at smaller excess energy.
Working at low temperature is helpful to achieve low MTE.
C An et al, AIP ADVANCES 8, 055225 (2018)
J.K. Bae et al, J. Appl. Phys. 124, 244903 (2018)
The multiphoton emission significantly increase MTE at well below threshold emission with high fluence laser.

## Slide 4
Evidence of the intermediate energy level
The model in this talk more focuses on the effect of intermediate energy level.
The presence of the intermediate energy level (donors for n-typed and acceptors for p-typed) might be one of the reasons to cause the discrepancy of QE between 300 K and 77 K near the threshold region.
T. Sakata, J.Phys.Soc.Japan 8 (1953) 793~795
300 K
77 K
300 K
77 K
Cs3Sb
The plot of resistance against temperature confirms the existence of the intermediate energy level. For Cs3Sb, it locates roughly at 0.5 eV above the filled band.
W.E. Spicer, Phys. Rev. 112, 114
W.E. Spicer, Phys. Rev. 112, 114

## Slide 5
Threshold photoemission model
The lattice imperfections, like a foreign atom or vacancy, can result in a donor or acceptor in the band gap.
Since most of the photocathodes used in the electron gun are p-typed semiconductors, only acceptor level is considered.
Excitation: valance band and acceptor level
Transport
Emission
Part of acceptor level will be occupied with electrons due to the thermal excitation. Higher occupation possibility is expected at higher temperature.
Acceptor level
Valance band
The density will be negligible at very low temperature, like 90 K.

## Slide 6
The first term is the contribution from acceptor level. The electrons from acceptor level have higher energy than the valance band electrons.
Threshold photoemission model
The contribution from the acceptor level should not be negligible when
Photon energy comparable to the threshold
Moderate number of electrons occupied at the acceptor level
Acceptor density
Temperature
The distribution of the excited electrons with energy E

## Slide 7
Threshold photoemission model
Excitation
Transport : scattering with phonon
Emission
p
Phonon scattering is the main scattering during the electron’s transport, accompanied with energy change due to phonon absorption and emission.
Energy loss:
Trajectory
analytical
– traveling time, – scattering rate, - phonon energy
MC
Apart from analytical model, a Monte Carlo simulation script is developed to evaluate not only the energy gain and loss but also the trajectory change due to the scattering.

## Slide 8
Jensen et al. J. Appl. Phys. 104, 044907 (2008)
Reflect
Tunnel
Semiconductor
Vacuum
Threshold photoemission model
Excitation
Transport: band bending
Emission: overcome the vacuum barrier
Triangular model is used.
Band bending at the surface
Example:
p-typed bulk; n-typed surface

## Slide 9
Equations to analyze the QE and MTE
Threshold photoemission model

## Slide 10
The model is able to explain one example of Cs3Sb cathode with photon energy 1.8 eV (threshold 1.9 eV) at 300 K and 90 K, corresponding to the conditions of occupied and empty acceptor level.
Cultrera et al, PRSTAB 18, 113401(2015)
Results
The calculated results agree with the experiments.
The presence of the electrons from acceptor level results in a higher MTE
300 K
90 K
300 K
90 K
Excess energy =
Gupta, Cultrera, and Bazarov, J. Appl. Phys. 121, 215702 (2017)

## Slide 11
2. The model can give reasonable results for the non-threshold photoemission
E-experiment M-model
L. Cultrera et al, Appl. Phys. Lett. 99, 152110 (2011)
Results
Filippetto, Qian, and Sannibale, Appl. Phys. Lett. 107, 042104 (2015)
Cs3Sb
Cs2Te
The model has been adapted to Cs2Te with the corresponding parameters.

## Slide 12
Degradation of semiconductor
Reasons for the QE degradation:
Residual gases, ion back bombardment, thermally activated decomposition ……
Ion back bombardment
C. K. Sinclair et al. PRSTAB 10, 023501 (2007)
The bombardment degrades the QE and shorten the lifetime.
Thermally activated decomposition
Z. Ding et al. PRAB 20, 113401 (2017)
High temperature induces material decomposition and cesium loss, leading to a shorter lifetime
Residual gases
Contamination with residual gases is an important reason for the cathode degradation in the RF electron gun and cathode storage system. It is present under any circumstances.
D. Sertore’ s talk in EWPAA 2017
M. Poelker’s talk in USPAS course, 2011

## Slide 13
Contamination with residual gases
Oxygen is believed to be the most poisonous one for most of the materials
Experiments have indicated that some changes of MTE (thermal emittance) take place during the QE degradation.
A model to analyze the cathode performance during the degradation is missing.
GaAs
Cs3Sb
GaAsP
GaAsP
[1] V. Pavlenko et al, AIP Advances 6, 115008 (2016)
[2] D. Sertore’ s talk in EWPAA 2017
[3] Jones et al, J. Appl. Phys. 121, 225703 (2017)

## Slide 14
The physical picture of degradation due to residual gases
The surface layer becomes thicker, leading to the reduction of the emission probability.
The electron affinity increases with time.
Degradation model of semiconductor

## Slide 15
1、The electron affinity increases with time
The time relationship of the change of electron affinity
Electron affinity
Time
Degradation model of semiconductor
The gas molecules in the vacuum environment stay at thermal equilibrium state, following the ideal gas equation and Maxwell-Boltzmann distribution
Characteristic time estimation
N
n
x
y
z
Electron affinity evolution ():

## Slide 16
Surface layer
Scatter with defects
Recombine with holes
2、The reduction rate of emission possibility due to the formation of the surface layer
Vacuum
Degradation model of semiconductor
Ld is attenuation length. dmax is the maximum thickness the surface layer can reach.

## Slide 17
The degradation model can fit with the experiments data of QE and predict the evolution of intrinsic emittance.
1. Cs3Sb with controlled contamination of O2(10-9Torr), photon energy 3.06eV.
Pavlenko, AIP Advances 6, 115008 (2016)
The application of the degradation model

## Slide 18
2. The evolution of the electron affinity, QE and MTE with the oxygen dose of GaAsP. The laser wavelength is 532 nm (2.33 eV).
The results from the model have good agreement with the experiment.
The application of the degradation model
All the experiment data come from J. Appl. Phys. 121, 225703 (2017)
L. B. Jones et al, J. Appl. Phys. 121, 225703 (2017)

## Slide 19
3. The predictions of the cathode performance at threshold photoemission in the degradation state. Take Cs3Sb as an example.
(1.8 eV, 4 MV/m) The emittance grows with degradation. The high energy electrons from acceptor level account for a significant part.
(1.8 eV, 50 MV/m) The high electric field compensates the growth of barrier.
(1.9 eV, 4 MV/m) The higher photon energy enables electrons from valance band dominate.
The participation of acceptor level may result in a higher intrinsic emittance at threshold photoemission under fully degradation. Higher field or higher photon energy can suppress its influence
The application of the degradation model
QE up
MTE down
QE up
MTE down

## Slide 20
Summary
1. Acceptor level emission is added into the 3-step photoemission model.
Explain the threshold emission experiment data for Cs3Sb at 300 K and 90 K
  acceptor level emission in room temperature contributes to threshold photoemission, leading to higher MTE
The model also gives consistent results to experiments beyond threshold photoemission. Examples have been given with Cs3Sb and Cs2Te
2. A degradation model is built to describe the cathode degradation process due to surface contamination, especially by O2.
The model fits well to the experiment for Cs3Sb and GaAsP
The model predicts cathode contamination at low field may increase the MTE for threshold photoemission and it can be suppressed by high field or high photon energy.
Thanks for your attention